Biofabrication, Antimicrobial Activity and Applications of Silver Nanoparticles (AgNPs): An Updated Review

Dr. Jasmeet Kaur Sohal1,*, Dr. Ashish Saraf2, Dr. Meghna Shrivastava3 and Dr. Kamlesh Kumar Shukla4

1,3 Assistant Professor, MATS School of Sciences, MATS University, Raipur C.G. India

2 Professor and Head, MATS School of Sciences, MATS University, Raipur C.G. India

4 Assistant Professor, SoS In Biotechnolgy, Pt. Ravishankar Shukla University, Raipur C.G. India

Abstract: Nanotechnology is a discipline of science concerned with the atomic level framing of materials in order to produce unique qualities that may subsequently be controlled for desired uses. Silver nanoparticles, out of all the metallic nanoparticles, attracts the most attention due to its unique physical, chemical, and biological characteristics. With a diverse set of applications in a variety of fields, including the pharmaceutical business. The development of an environmentally benign approach for nanoparticle production has been a big step forward in nanotechnology. To overcome the limitation of conventional methods used for synthesizing nanoparticles green chemistry has emerged as an alternative, which includes the use of biological entities like microorganisms, whole plants or plant extracts. Biodiversity-rich countries require the collection and translation of data about biological assets into processes, relationships, techniques, and instruments that must be linked with biological diversity's long-term usage. As a result, this review article summarises the relevant investigations of AgNPs biosynthesis and its antimicrobial properties against microorganisms and their applications in several fields, including medicine and agriculture.

Keywords: Silver nanoparticles, biofabrication, antimicrobial activity, applications

INTRODUCTION

Nanotechnology is one of the fastest-growing areas, with potential applications in catalysis, energy, chemistry, and medicine. Nanotechnology is largely concerned with the creation, characterisation, and investigation of nanoparticles of various types. A particle with a diameter of less than 100 nanometers is referred to as a nanoparticle. The word "nano" comes from a Greek word that means "dwarf" or "very small" [1]. Because of their vast surface area, they respond differently than bigger particles of the same composition, allowing them to be employed in innovative applications [2]. They may be thought of as the nanotechnology's fundamental building block [3]. In his historic address "there's plenty of room at the bottom," physicist Professor Richard Feynman presented the concept of nanotechnology [4], however the term nanotechnology was coined by Professor Norio Taniguchi of Tokyo Science University [5].

Due to the ease of use of sophisticated characterisation techniques and the huge number of synthesis methods for nanomaterials, the area of nanotechnology has evolved significantly in recent years, particularly in the last two decades.

Organic nanoparticles and inorganic nanoparticles are the two types of nanoparticles that can be generically classed. Carbon nanoparticles (fullerenes) are an example of an organic nanoparticle, whereas magnetic nanoparticles, noble nanoparticles (Au and Ag), and semiconductor nanoparticles are examples of inorganic nanoparticles (TiO2 and ZnO). Inorganic nanoparticles, in particular, have attracted interest due to their exceptional material characteristics and diverse uses. It is conveniently employed for chemical imaging pharmaceuticals, agents, and medications due to its nano size. Because of their extensive availability, diverse activity, and outstanding biocompatibility, inorganic nanoparticles are exploited for cellular distribution. They're also useful for controlled medication release and focused drug delivery. As a result, entirely beneficial materials for medical science (for example, mesoporous silica mixed with molecular medications produces a fantastic image on drug release). Cheon and Horace (2009) found that gold nanoparticles are an effective carrier for biological target thermotherapy [6]. Silver nanoparticles have antibacterial properties that help in wound healing and the treatment of infectious disorders. Nanotechnology is concerned about nanoparticle synthesis because of its changeable size, morphologies, chemical composition, and controlled dispersity, as well as their prospective application in medical research for improved human treatment.

Silver nanoparticles stand out among all metallic nanoparticles due to its unique physical, chemical, and biological capabilities. They are one of the nanotechnology industry's most promising products. Silver nanoparticles have been widely used in medicine administration, medical devices, sensing and diagnostics, and other applications due to their anticoagulant, antimicrobial, orthopaedic, anticancer and thrombolytic capabilities. AgNPs are extremely important because of their catalytic activity, optical and thermal properties, chemical and thermal stability, and antibacterial properties [7]. The development of consistent processes for the synthesis of silver nanoparticles is the focus of current nanotechnology research. Physical, chemical, and biological approaches are all depicted in various literatures as ways to generate silver nanoparticles. Due to the use of hazardous solvents and strict processes, the physical and chemical methods used to synthesise nanoparticles are not only energy-intensive but also non-eco-friendly [8]. As a result, in recent years, green synthesis methods have largely superseded different physical and chemical approaches for nanoparticle production in order to reduce toxicity and improve quality. The goal of green synthesis of nanoparticles is to reduce waste, use less energy, use renewable ingredients, and use risk-avoidant procedures. The three fundamental ideas in the green synthesis strategy are choice of the solvent medium (ideally water), an ecologically friendly reducing agent, and a non-hazardous substance for nanoparticle stabilisation are [9]. A number of bio-sources, such as bacteria, algae, fungi, and plants, can be employed in the green synthesis of AgNPs, each with its own set of benefits and downsides [10].

In light of their efficacy and applicability of, this review article summarises the relevant investigations of AgNPs biosynthesis and its antimicrobial properties against microorganisms and their applications in several fields, including medicine and agriculture.

BACTERIAL MEDIATED SYNTHESIS OF AgNPs

Inorganic nanomaterials (particularly Se, Au, and Ag) with appealing properties have been widely synthesised using bacterial strains in the last decade for the development of third-generation biosensors, promising diagnostic applications (cell imaging and biolabeling, voltametric sensory devices), and non-surface coating applications such as thin-film formation and annealing. Bacterial-mediated biosynthesized nanoparticles have exhibited in vitro antimicrobial efficiency against pathogenic microbial strains, as well as antioxidant, anticoagulant, anticancer, antimigration, and antiproliferative properties [11]. Bacteria for its survival reduces metal ions or forms complexes with metal ions, when exposed to high metal ion concentrations. Metal ions, which are required for microbe growth and responsible for the bioconversion of metal ions into nanoparticles, are connected to metabolic pathways in some microorganisms [12]. A range of cellular transporters and oxidoreductase enzymes are involved in internal and extracellular biocatalytic synthesis, including NADH-dependent nitrate reductase, NADPH dependent sulfite reductase flavoprotein subunit α, and cysteine desulfhydrase [11]. Bacterial species have also shown the ability to synthesise new organic nanoparticles. It has previously been generated a three-dimensional cellulose nanofibril network of aerobic acetic bacteria-like bacterial nanocellulose related to the species Gluconacetobacter, the most competent bacteria for nanocellulose synthesis. In compared to nanocrystalline cellulose and nanofibrillated cellulose, bacterial nanocellulose has higher purity, crystallinity, and mechanical consistency [13]. As a result, bacterial nanocellulose has piqued interest for usage in biomedical applications (such as antibacterial agents, tissue engineering scaffolds, and drug delivery systems), as well as biosensor platforms [14]. In the year 2020, Saeed and colleagues investigated bacterial-mediated AgNPs, which showed promising results against human infections. Bacterial strains were used to investigate secondary metabolite production (Escherichia coli MF754138, Exiguobacterium aurantiacumm MF754139, and Brevundimons diminuta MF754140). With a 10–28 mm zone of inhibition, the bacterial strains utilised in the study showed promise as antimicrobial agents against methicillin-resistant Staphylococcus aureus (MRSA) and other multidrug-resistant (MDR) pathogens. The research demonstrated an environmentally friendly method for generating AgNPs, which will aid in the prevention of MRSA and other human pathogen-related nosocomial infections [15]. In a simple and environmentally friendly AgNP formulation approach, Huq used Lysinbacillus xylanilyticus MAHUQ-40 to target antibiotic-resistant human pathogens Vibrio parahaemolyticus and Salmonella typhimurium. To validate and characterise AgNPs, researchers utilised UV–visible spectroscopy, X-ray diffraction (XRD), Fourier-transform infrared (FTIR), field emission–transmission electron microscopy (FE-TEM), and dynamic light scattering (DLS) [16]. Ma et al. (2018) investigated the extracellular production of AgNPs by Streptomyces coelicoflavus KS-3. The AgNPs were mostly spherical or nearly spherical, with a few triangular, quadrangular, and hexagonal particles ranging in size from 2.33 to 91.3 nm. Furthermore, a comparable investigation on the cytotoxic effects of AgNPs found that AgNPs were effective against HTB-182 and A549 cells in a dose-dependent manner at concentrations ranging from 1 to 50 µg/mL [17].

FUNGAL MEDIATED SYNTHESIS OF AgNPs

Fungi have a huge potential for producing a wide range of compounds. Microscopic filamentous or nonfilamentous fungus species are known to produce around 6400 bioactive compounds [18]. Fungal species are commonly utilised as stabilising and reducing agents due to their heavy metal uptake and capacity to internalise and bioaccumulate metals. Fungi can also manufacture NPs with controlled size and morphology on a large scale in "nanofactories" [19,20]. Fungal biosynthesis can produce intracellular or extracellular nanoparticles. Although various studies have been conducted on the generation of AgNPs using fungus, the particular mechanisms have yet to be fully characterised. Extracellular NP generation is considered to occur when enzymes in the fungal filtrate work at a nanometric scale to convert silver ions to elemental silver (Ag0) [21,22]. NADH and NADH-dependent nitrate reductase are the enzymes mainly engaged in the creation of metallic nanoparticles [23,24]. Endophytic AgNPs were synthesised using an aqueous extract of endophytic fungi (Lasiodiplodia theobromae) protected by Cinnamomum zeylanicum (EFNps). Minimum inhibitory concentration (MIC), minimum bacterial concentration (MBC), agar well diffusion, pyocyanin, antibiofilm, and time kill curve tests were performed on P. aeruginosa ATCC (27853) and an antibiotic-resistant clinical strain. The findings suggested that EFNps could be a viable alternative to antibiotics in the treatment of P. aeruginosa infections. The biosynthesis of AgNPs by fungi is a sanitary, safe, ecologically friendly, dependable, inexpensive, and green approach that can be used in a number of everyday applications [25]. Ammar et al. (2021) used yeast metabolites to study the production, characterisation, and medicinal applications of AgNPs. AgNPsK and AgNPsU were made using the yeast strains Pichia kudriavzevii HA-NY1 and Saccharomyces uvarum HA-NY3, respectively. Gram-positive bacteria (Staphylococcus aureus ATCC29213 and Bacillus subtilis ATCC6633) and Gram-negative bacteria (Pseudomonas aeruginosa ATCC27953), as well as fungal species (Fusarium oxysporium NRC21 and Candida tropicalis ATCC750), were found to be extremely sensitive to AgNPs. In this study, AgNPsK and AgNPsU were found to have anticancer activity against PC3 (prostate cell line) and HCT-116 (colon cell line), with IC50 values of 0.57, 0.50 µg/mL and 0.29, 0.24 µg/mL, respectively. AgNPs did not cause ulcers in rats, showing that they are safe for the gastric profile. [26].

ALGAL MEDIATED SYNTHESIS OF AgNPs

Algae has long been utilised in food, feed, cosmetics, fertilisers, additives, and pharmaceuticals. The generation of nanoparticles by algae has recently become the subject of research. Algae are simple to produce, scalable, and have a fast growth rate, making them a good source of secondary metabolites. As a result of these facts, the interest in algal-mediated nanoparticle production is growing fast [27]. AgNPs have been synthesised using algae ranging in size from microscopic (picoplankton) to macroscopic (rhodophyta). Algal strains like Tetraselmis kochinensis, Desmodesmus, and Scenedesmus have been employed to make novel metal nanoparticles biologically. Antimicrobials, drug administration, electronics, catalysis, and other biomedical applications all use these NPs [11]. Algae have the potential to gather heavy metals and change them into new, varied forms. Because of their appealing features, algae have been employed to make a range of nanomaterials. Algal-mediated nanoparticle formation is described by the ability to control the dimensions and processes of nucleation, structure stabilisation, and regulation by reducing agents [28], biomolecules [29], and enzymes [30]. Merin et al. (2010) used marine algae as a reducing and stabilising agent in the formulation of AgNPs [31]. A biomineralized silica cell wall called a frustule is present in unicellular microalgae (diatoms), which generates a periodic and hierarchical 3D porous micro-nanostructure of diverse patterns. Mechanical protection, UV shielding of DNA, biological protection, filtration, and light harvesting improvement are all common frustule functions [32,33]. Increased biocompatibility, ease of purification, and lesser toxicity are among the benefits of diatom frustules over silica materials (e.g., MCM-4). The primary metal has been stabilised, capped, and reduced using algal secondary metabolites, resulting in metal, metal oxide, or bimetallic nanoparticles. The most fully investigated algae for the creation of nanoparticles are red (Rhodophyceae), brown (Phaeophyceae), blue-green (Cyanophyceae), micro- and macro-green algae. To date, silver nanoparticles have been made from more than 20 different green microalgal species. Algal-mediated biosynthesized AgNPs have remarkable and diversified physico-chemical properties when studied utilising a variety of microscopic and spectroscopic techniques (SEM, XRD, FTIR, EDX, DLS) [28,34,35]. Due to the presence of various useful compounds that are responsible for the reduction and capping of nanoparticles, green macro-algae are regarded as bio-factories for the synthesis of metallic NPs. The most common green alga utilised to make nanosized colloids is Ulva fasciata [36]. With the help of terpenoids, peptides, and flavonoids, Chaetomorpha linum is a key macro-algal green seaweed species used to create silver nanoparticles by promoting the reduction of Ag+ to Ag0. The biological importance of C. linum in regulating nutrient accessibility in its environment is well established [27]. Ulagesan et al. (2021) investigated the biogenic synthesis of AgNPs using an aqueous extract from marine red algae (Pyropia yezoensis). The presence of spherical silver nanoparticles with an average crystallographic size of 20–22 nm was established. Gram-positive and Gram-negative bacteria strains were used to test AgNPs' antibacterial properties. At doses of 200 and 400 µg/mL, Pyropia yezoensis AgNPs suppressed the growth of Pseudomonas aeruginosa [37].

PLANT MEDIATED SYNTHESIS OF AgNPs

Plant-mediated biosynthesis of AgNPs is a simple, highly effective, and fast process. Plants have the capacity to reduce and stabilise nanoparticles due to the existence of various metabolites (phenols, ketones, proteins, aldehydes, amides, and carboxylic acids). Almost every plant part has been mined for active compounds in the production of AgNPs, including leaves, seeds, roots, and flowers [10]. Close examination of recent studies on the biosynthesis of AgNPs reveals that interest is shifting dramatically toward the use of medicinal flora for nanoparticle synthesis. Because of the presence of reducing components (H+), the green leaves of medicinal plants have the greatest potential to reduce and stabilise AgNPs [38]. Medicinal plants have yielded a variety of natural chemicals that have been shown to be effective against microbes, malignant cells, and neurological illnesses. As a result, including medicinal plants into biosynthesis research may go beyond simply being a green chemistry method, potentially increasing nanoparticle biological properties [10]. Several investigations on the synthesis of AgNPs from medicinal plants for various uses have been published in this respect. The first attempt to synthesise metallic nanoparticles using plants was with Medicago sativa (alfalfa) sprouts (Gardea-Torresdey et al., 2003), which was the first report on the creation of AgNPs in a living plant system. Alfalfa roots have been proven to carry Ag from agar media to the plant's shoots in the same oxidation state. These Ag atoms organised themselves to create nanoparticles in the shoots [39]. Jain and Mehata (2017) reported the production of AgNPs using Ocimum sanctum leaf extract due to its excellent antibacterial and germicidal properties. The inclusion of hydroxyl and ketone groups in tulsi leaf extract reduced AgNPs and showed improved antibacterial action against E. coli [40]. The plant Azadirachta indica was used to make AgNPs, and antibacterial activity against S. aureus and E. coli was discovered [41]. AgNP production was investigated in Teucrium polium and Ocimum basilicum, with possible antibacterial, anticancer, and antioxidant properties. The cytotoxic capabilities of biosynthesized AgNPs against the HEP G2 cell line were also investigated [42]. Rao and Tang (2017) reported the green synthesis of silver nanoparticles (AgNPs) from silver nitrate solution and aqueous Eriobotrya japonica leaf extract using an environmentally friendly technique. TEM was used to confirm the synthesis of AgNPs, which showed good antibacterial activity against E. coli and S. aureus [43]. Shaik et al. (2018) used an aqueous solution of Origanum vulgare L. plant extract as a bioreducing agent to synthesise AgNPs (2-25 nm). Antibacterial activity against Gram-positive (M. luteus, S. epidermidis, Methicillin-resistant Staphylococcus aureus (MRSA), and S. aureus) as well as Gram-negative (E. coli, S. typhi, P. aeruginosa, and S. sonnei) bacteria and antifungal activity against pathogenic fungi were discovered in the synthesised AgNPs (A. flavus, A. alternate, P. alba, and P. variotii) [44]. Sohal et al. (2019) reported the green synthesis of AgNPs using Aloe vera gel extract, which showed an excellent antibacterial activity against Gram-positive and Gram-negative bacteria [45]. Ghramh et al. (2020) used an ethanolic extract of Ruta graveolens to make spherical AgNPs with a diameter of 40–45 nm and investigated the biological activities, immunological modulation, anticancer, and insecticidal potential of the extracts. The extract containing AgNPs showed insecticidal action against Culex pipiens [46]. The antibacterial properties of Carissa carandas biosynthesized AgNPs against human pathogenic bacteria were reported by Singh et al. (2021) [47].

ANTIMICROBIAL ACTIVITY OF AgNPs

The discovery of Antibiotics was the most important medical breakthrough of the twentieth century, since they were helpful in treating patients with cancer, diabetes, microbiological infections, and surgical problems [48]. Unfortunately, this accomplishment has resulted in the evolution of antibiotic resistance (AMR). Excessive use of antimicrobial drugs against hazardous bacteria has resulted in the creation of multidrug-resistant microorganisms (MDRM) [49]. Pathogenic resistance is a critical issue that pharmacists and healthcare providers must deal with. A sepsis with multidrug-resistant bacteria (MDR) cannot be healed since it requires treatment with a variety of medicines [50]. According to the World Health Organization (WHO), drug-resistant infections cause a high death rate during disease pandemics [51]. As a result, in recent years, there has been a lot of interest in developing and modifying antimicrobial agents that have better absorption. The biological applications of metallic nanoparticles generated from metals such as Ag, Au, Cu, Pt, and others have been the subject of research in recent decades. Out of which AgNPs have gotten a lot of attention because of their unusual antimicrobial characteristics. Silver's antimicrobial property is due to the fact that microbes cannot develop resistance to it as they can to conventional and narrow-target antibiotics because it attacks a broad range of targets in the organisms, requiring microbes to develop a slew of mutations at the same time to protect themselves [52]. Silver is commonly employed in its nitrate form to produce antimicrobial effects, but when nanoparticles of silver are created, the surface to volume ratio increases dramatically, making it a great antimicrobial agent. The specific mechanism by which silver nanoparticles exert antimicrobial activity is unknown and remains a source of discussion till date. Although there are several theories regarding the microbicidal impact of silver nanoparticles on microorganisms. Following are the four main processes that explain antimicrobial activity of AgNPs':

- Adhesion of AgNPs to Cell Wall and Membrane Surfaces: Silver nanoparticles' capacity to stick to and subsequently enter the bacterial cell wall produces structural alterations in the cell membrane, affecting membrane structure and permeability, causing cellular content and ATP leakage, and decreased transport function, ultimately leading to cell death [53].

- Intracellular Penetration of AgNPs and Destabilization of Intracellular Structures and Biomolecules: Another reason that suggests AgNPs have antimicrobial properties is that they are thought to infiltrate within cells and disrupt essential cellular functions [54,55]. It has the potential to interact with biomolecules like proteins, lipids, and DNA, as well as cellular structures. Microbes are negatively affected by interactions with cellular structures and macromolecules. AgNPs, on the other hand, are assumed to be the source of mitochondrial malfunction. When AgNPs come into contact with ribosomes, they denaturize them, inhibiting protein synthesis and translation [56,57,58]. Silver ions are thought to interact with the functional areas of proteins, rendering them inert. Furthermore, AgNP interactions with DNA may result in DNA breakage or denaturation, as well as cell division interruption [59,60].

- AgNPs Induced Cellular Toxicity and Oxidative Stress: Another mechanism linking silver nanoparticles to its antimicrobial activity is the formation of free radicals and reactive oxygen species (ROS) in cells, which leads to an increase in oxidative stress. Electron spin resonance spectroscopy investigations reveal that, when the silver nanoparticles come into to with a microbial cell, free radicals are formed. Hyperoxidation of lipids, proteins, and DNA occurs as a result of increased oxidative stress, resulting in cell death.

- Modulation of Signal Transduction Pathways: AgNPs are thought to suppress microbial growth by dephosphorylating tyrosine residues on essential bacterial peptide substrates and thereby modulating cellular signaling [61]. (Figure 1).

Figure 1: The four prominent routes of antimicrobial action of AgNPs [62].

APPLICATIONS OF AgNPs

Because of their unique features, biosynthesized AgNPs have been shown to have potential applications in agriculture, health, food, and industry in recent decades.

AgNPs IN AGRICULTURE

Biopesticides were developed after the first green revolution to fight the indiscriminate usage and negative consequences of chemical pesticides [63]. Because of their particular antibacterial capabilities, AgNPs are mostly employed for plant disease management [64]. Many researchers have advocated taking advantage of AgNPs' antibacterial properties, which make them antagonistic to a range of plant diseases. The focus of research has been on direct applications of AgNPs in agriculture, such as root elongation, seed germination, nanofertilizers, nanopesticides, and plant modification (cytotoxicity or cellular oxidative stress) in the presence of metal NPs [65,66], as well as indirect applications based on NP antimicrobial activities [67]. Scientists have documented broad-spectrum phytopathogenicity of AgNPs against a variety of phytopathogens, including Scalerotinia sclerotiorum, Fusarium culmorum, Trichoderma sp., Botrytis cinerea, Colletotrichum gloeosporioides, Rhizoctonia solani, Biploaris sorokinniana, Sphaerotheca pannasa, Phythium ultimum, Phoma and Megnaporthe grisea [68,69,70]. In a study using nanopriming technology, phytosynthesized (kaffir lime leaf extract) AgNPs were found to improve the germination and starch metabolism of developed rice seeds [71].

FOOD AND AgNPs

In the food industry around the world, nanopotentials have been discovered to improve food qualities, safety, and production efficiency. AgNPs' antibacterial activity has been extensively studied in the food industry. Greenly produced AgNPs are thought to be safer or less harmful for food applications [72]. The United States Food and Drug Administration (USFDA) has approved the use of a variety of Ag-containing food packaging materials in order to increase the shelf life of foods while maintaining direct contact with them [73]. One of the most serious issues in the agri-food industry is the safety and freshness of fruits and vegetables. Protein and weight loss occur during long-term preservation of fruits and vegetables due to natural wax coatings' incapacity to prevent water loss and reduce respiration rate. The use of various protective nanocoatings and appropriate packaging materials can greatly extend the shelf life of numerous food items [74].

BIOMEDICAL APPLICATIONS OF AgNPs

AgNPs have a wide range of biological applications, including pharmacology, drug transport, diagnostics, anticancer, and so on, because of their unique physicochemical and antibacterial properties. Garcia-Contreras et al. (2011) investigated the application of AgNPs in dental treatments such as dental implants, endodontic retrofill cement and restorative material [75]. Because the alkaloid or flavonoid contents act as capping agents and provide additional pharmacological effects, biologically produced AgNPs have anti-inflammatory capabilities. A study was conducted to assess the anti-inflammatory properties of AgNPs produced by the Leucas aspera plant. L. aspera biosynthesized AgNPs were found to have excellent anti-inflammatory properties [76]. Kim et al. (2007) used Muller Hinton agar plates to test AgNPs' antibacterial activities against E. coli, Staphylococcus aureus and yeast, revealing that they are suitable for a variety of medical devices and antimicrobial control systems [77].

ENVIRONMENT AND AgNPs

Biosynthesized AgNPs have emerged as cutting-edge tools for creating nanobiosensors that detect pollutants in the environment. The surface modification of nanoparticles with an appropriate chemical has made it feasible to identify residual pesticides in environmental samples. Nanotechnology-based colorimetric approaches for pesticide detection have various advantages, including accuracy, the lack of specialist equipment, simplicity, and reduced time consumption. The specificity and sensitivity of nanoparticle-based colorimetric detection methodology are determined by the chemical and molecular interactions between the surface-modified nanoparticle and target pesticides [78]. Silver (Ag) has a high extinction coefficient and a strong surface plasmon resonance, making it a good candidate for detecting pesticide residues in the environment [79,80]. Using calixarene-modified AgNPs, Xiong and Li described a colorimetric probe for detecting residual pesticides quantitatively. A one-pot synthesis approach was used to make very hard calixarene-modified silver nanoparticles (pSC4-Ag NPs), which were subsequently analysed. With an optunal down to a concentration of 10-7 M, pSC4-Ag NPs have been presented as a novel sensor for the colorimetric identification of residual pesticides in water [81]. Menon et al. (2013) used p-sulphonate calyx resorcinarene tailored silver nanoparticles (pSC4R-Ag NPs) to develop a simple and highly sensitive approach for detecting dimethoate herbicides in industrial wastewater [82].

REFERENCES

- Rai M, Yadav A, Gade A. CRC 675—current trends in phytosynthesis of metal nanoparticles. Critical reviews in biotechnology. 2008 Jan 1;28(4):277-84.

- Abou El-Nour KM, Eftaiha AA, Al-Warthan A, Ammar RA. Synthesis and applications of silver nanoparticles. Arabian journal of chemistry. 2010 Jul 1;3(3):135-40.

- Vahabi K, Mansoori GA, Karimi S. Biosynthesis of silver nanoparticles by fungus Trichoderma reesei (a route for large-scale production of AgNPs). Insciences J.. 2011;1(1):65-79.

- Feynman R. Lecture at the California Institute of Technology.

- Taniguchi, N. (1974). On the basic concept of nano-technology. In Proc. Intl. Conf. Prod.

London, 1974. British Society of Precision Engineering.

- Cheon J, Underwood HG. Inorganic nanoparticles for biological sensing, imaging and therapeutics. Journal of Materials Chemistry. 2009;19(35):6249-50.

- Tehri, N.; Kaur, R.; Maity, M.; Chauhan, A.; Hooda, V.; Vashishth, A.; Kumar, G. Biosynthesis, characterization, bactericidal and sporicidal activity of silver nanoparticles using the leaves extract of Litchi chinensis. Prep. Biochem. Biotechnol. 2020, 50, 865–873.

- Sohal JK, Saraf A, Shukla KK. Green synthesis of silver nanoparticles (ag-nps) using plant extract for antimicrobial and antioxidant applications: A review. International Journal of Advanced Research in Science and Engineering. 2017;6(10):766-77.

- Raveendran P, Fu J, Wallen SL. Completely “green” synthesis and stabilization of metal nanoparticles. Journal of the American Chemical Society. 2003 Nov 19;125(46):13940-1.

- Moradi, F.; Sedaghat, S.; Moradi, O.; Salmanabadi, S.A. Review on green nano-biosynthesis of silver nanoparticles and their biological activities: With an emphasis on medicinal plants. Inorg. Nano Met. Chem. 2020, 51, 133–142.

- Grasso, G.; Zane, D.; Dragone, R. Microbial Nanotechnology: Challenges and Prospects for Green Biocatalytic Synthesis of Nanoscale Materials for Sensoristic and Biomedical Applications. Nanomaterials 2019, 10, 11.

- Poulose, S.; Panda, T.; Nair, P.P.; Théodore, T. Biosynthesis of Silver Nanoparticles. J. Nanosci. Nanotechnol. 2014, 14, 2038–2049.

- Golmohammadi, H.; Morales-Narváez, E.; Naghdi, T.; Merkoçi, A. Nanocellulose in Sensing and Biosensing. Chem. Mater. 2017, 29, 5426–5446.

- Pourreza, N.; Golmohammadi, H.; Naghdi, T.; Yousefi, H. Green in-situ synthesized silver nanoparticles embedded in bacterial cellulose nanopaper as a bionanocomposite plasmonic sensor. Biosens. Bioelectron. 2015, 74, 353–359.

- Saeed, S.; Iqbal, A.; Ashraf, M.A. Bacterial-mediated synthesis of silver nanoparticles and their significant effect against pathogens. Environ. Sci. Pollut. Res. 2020, 27, 37347–37356.

- Huq, M.A. Biogenic silver nanoparticles synthesized by Lysinibacillus xylanilyticus mahuq-40 to control antibiotic-resistant human pathogens vibrio parahaemolyticus and Salmonella typhimurium. Front. Bioeng. Biotechnol. 2020, 8, 1407.

- Ma, L.; Liu, J.; Su, W.; Zeng, X.; Liu, X.; Li, W.; Deng, J.; Tang, J. Extracellular Biosynthesis, Characterization and Cytotoxic Effect of Silver Nanoparticles by Streptomyces coelicoflavus KS-3. J. Nanosci. Nanotechnol. 2018, 18, 8133–8141.

- Berdy, J. Bioactive microbial metabolites: A personal view. J. Antibiot. 2005, 58, 1–26.

- Azmath, P.; Baker, S.; Rakshith, D.; Satish, S. Mycosynthesis of silver nanoparticles bearing antibacterial activity. Saudi Pharm. J. 2016, 24, 140–146.

- Khan, N.T.; Jameel, J.; Rheman, S.U.A. An Overview: Biological Organisms that Serves as Nanofactories for Metallic Nanoparticles Synthesis and Fungi Being the Most Appropriate. Bioceram. Dev. Appl. 2017, 7, 101.

- Ahmad, A.; Mukherjee, P.; Senapati, S.; Mandal, D.; Khan, M.; Kumar, R.; Sastry, M. Extracellular biosynthesis of silver nanoparticles using the fungus Fusarium oxysporum. Colloids Surf. B Biointerfaces 2003, 28, 313–318.

- Elamawi, R.M.; Al-Harbi, R.E.; Hendi, A.A. Biosynthesis and characterization of silver nanoparticles using Trichoderma longibrachiatum and their effect on phytopathogenic fungi. Egypt. J. Biol. Pest Control 2018, 28, 28.

- Baymiller, M.; Huang, F.; Rogelj, S. Rapid one-step synthesis of gold nanoparticles using the ubiquitous coenzyme NADH. Matters 2017, 3.

- Zomorodian, K.; Pourshahid, S.; Sadatsharifi, A.; Mehryar, P.; Pakshir, K.; Rahimi, M.J.; Monfared, A.A. Biosynthesis and Characterization of Silver Nanoparticles by Aspergillus Species. BioMed Res. Int. 2016, 2016, 1–6.

- Ranjani, S.; Ahmed, M.S.; Mohd, A.; Kumar, N.S.; Ruckmani, K.; Hemalatha, S. Synthesis, characterization and applications of endophytic fungal nanoparticles. Inorg. Nano Met. Chem. 2020, 51, 280–287.

- Ammar, H.A.; El Aty, A.A.A.; El Awdan, S.A. Extracellular myco-synthesis of nano-silver using the fermentable yeasts Pichia kudriavzeviiHA-NY2 and Saccharomyces uvarumHA-NY3, and their effective biomedical applications. Bioprocess Biosyst. Eng. 2021, 44, 841–854.

- Chaudhary, R.; Nawaz, K.; Khan, A.K.; Hano, C.; Abbasi, B.H.; Anjum, S. An Overview of the Algae-Mediated Biosynthesis of Nanoparticles and Their Biomedical Applications. Biomolecules 2020, 10, 1498.

- Jena, J.; Pradhan, N.; Nayak, R.R.; Dash, B.P.; Sukla, L.B.; Panda, P.K.; Mishra, B.K. Microalga Scenedesmus sp.: A Potential Low-Cost Green Machine for Silver Nanoparticle Synthesis. J. Microbiol. Biotechnol. 2014, 24, 522–533.

- Yilmaz Öztürk, B. Intracellular and extracellular green synthesis of silver nanoparticles using Desmodesmus sp.: Their antibacterial and antifungal effects. Caryologia 2019, 72, 29–43.

- Senapati, S.; Syed, A.; Moeez, S.; Kumar, A.; Ahmad, A. Intracellular synthesis of gold nanoparticles using alga Tetraselmis kochinensis. Mater. Lett. 2012, 79, 116–118.

- Merin, D.D.; Prakash, S.; Bhimba, B.V. Antibacterial screening of silver nanoparticles synthesized by marine micro algae. Asian Pac. J. Trop. Med. 2010, 3, 797–799.

- Losic, D.; Mitchell, J.G.; Voelcker, N. Diatomaceous Lessons in Nanotechnology and Advanced Materials. Adv. Mater. 2009, 21, 2947–2958.

- Aguirre, L.E.; Ouyang, L.; Elfwing, A.; Hedblom, M.; Wulff, A.; Inganäs, O. Diatom frustules protect DNA from ultraviolet light. Sci. Rep. 2018, 8, 5138.

- Sinha, S.N.; Paul, D.; Halder, N.; Sengupta, D.; Patra, S.K. Green synthesis of silver nanoparticles using fresh water green alga Pithophora oedogonia (Mont.) Wittrock and evaluation of their antibacterial activity. Appl. Nanosci. 2014, 5, 703–709.

- Khanna, P.; Kaur, A.; Goyal, D. Algae-based metallic nanoparticles: Synthesis, characterization and applications. J. Microbiol. Methods 2019, 163, 105656.

- El-Rafie, H.; El-Rafie, M.; Zahran, M. Green synthesis of silver nanoparticles using polysaccharides extracted from marine macro algae. Carbohydr. Polym. 2013, 96, 403–410.

- Ulagesan, S.; Nam, T.-J.; Choi, Y.-H. Biogenic preparation and characterization of Pyropia yezoensis silver nanoparticles (P.y AgNPs) and their antibacterial activity against Pseudomonas aeruginosa. Bioprocess Biosyst. Eng. 2020, 44, 443–452.

- Mousavi, S.M.; Hashemi, S.A.; Ghasemi, Y.; Atapour, A.; Amani, A.M.; Dashtaki, A.S.; Babapoor, A.; Arjmand, O. Green synthesis of silver nanoparticles toward bio and medical applications: Review study. Artif. Cells Nanomed. Biotechnol. 2018, 46, S855–S872.

- Gardea-Torresdey JL, Gomez E, Peralta-Videa JR, Parsons JG, Troiani H, Jose-Yacaman M. Alfalfa sprouts: a natural source for the synthesis of silver nanoparticles. Langmuir. 2003 Feb 18;19(4):1357-61.

- Jain, S.; Mehata, M.S. Medicinal Plant Leaf Extract and Pure Flavonoid Mediated Green Synthesis of Silver Nanoparticles and their Enhanced Antibacterial Property. Sci. Rep. 2017, 7, 1–13.

- Ahmed, S.; Saifullah, A.M.; Swami, B.L.; Ikram, S. Green synthesis of silver nanoparticles using Azadirachta indica aqueous leaf extract. J. Radiat. Res. Appl. Sci. 2016, 9, 1–7.

- Moradi, F.; Sedaghat, S.; Arab-Salmanabadi, S.; Moradi, O. Biosynthesis of silver-montmorillonite nanocomposites using Ocimum Basilicum and Teucrium Polium; A comparative study. Mater. Res. Express 2019, 6, 125008.

- Rao B, Tang RC. Green synthesis of silver nanoparticles with antibacterial activities using aqueous Eriobotrya japonica leaf extract. Advances in natural sciences: Nanoscience and nanotechnology. 2017 Mar 2;8(1):015014.

- Shaik MR, Khan M, Kuniyil M, Al-Warthan A, Alkhathlan HZ, Siddiqui MR, Shaik JP, Ahamed A, Mahmood A, Khan M, Adil SF. Plant-extract-assisted green synthesis of silver nanoparticles using Origanum vulgare L. extract and their microbicidal activities. Sustainability. 2018 Apr;10(4):913.

- Sohal JK, Saraf A, Shukla KK. Antimicrobial activity of biochemically synthesized silver nanoparticles (AgNPs) using Aloe vera gel extract.

- Ghramh, H.A.; Ibrahim, E.H.; Kilnay, M.; Ahmad, Z.; Alhag, S.K.; Khan, K.A.; Taha, R.; Asiri, F.M. Silver Nanoparticle Production by Ruta graveolens and Testing Its Safety, Bioactivity, Immune Modulation, Anticancer, and Insecticidal Potentials. Bioinorg. Chem. Appl. 2020, 2020, 1–11.

- Singh, R.; Hano, C.; Nath, G.; Sharma, B. Green biosynthesis of silver nanoparticles using leaf extract of Carissa carandas L. and their antioxidant and antimicrobial activity against human pathogenic bacteria. Biomolecules 2021, 11, 299.

- Salomoni, R.; Léo, P.; Montemor, A.; Rinaldi, B.; Rodrigues, M. Antibacterial effect of silver nanoparticles in Pseudomonas aeruginosa. Nanotechnol. Sci. Appl. 2017, 10, 115–121.

- Fan, W.; Yung, B.; Huang, P.; Chen, X. Nanotechnology for Multimodal Synergistic Cancer Therapy. Chem. Rev. 2017, 117, 13566–13638.

- Supraja, N.; Prasad, T.; Soundariya, M.; Babujanarthanam, R. Synthesis, characterization and dose dependent antimicrobial and anti-cancerous activity of phycogenic silver nanoparticles against human hepatic carcinoma (HepG2) cell line. AIMS Environ. Sci. 2016, 3, 425–440.

- Das, C.A.; Kumar, V.G.; Dhas, T.S.; Karthick, V.; Govindaraju, K.; Joselin, J.M.; Baalamurugan, J. Antibacterial activity of silver nanoparticles (biosynthesis): A short review on recent advances. Biocatal. Agric. Biotechnol. 2020, 27, 101593.

- Pal S, Tak YK, Song JM. Does the antibacterial activity of silver nanoparticles depend on the shape of the nanoparticle? A study of the gram-negative bacterium Escherichia coli. Applied and environmental microbiology. 2007 Mar 15;73(6):1712-20.

- Sondi I, Salopek-Sondi B. Silver nanoparticles as antimicrobial agent: a case study on E. coli as a model for Gram-negative bacteria. Journal of colloid and interface science. 2004 Jul 1;275(1):177-82.

- Singh BR, Singh BN, Singh A, Khan W, Naqvi AH, Singh HB. Mycofabricated biosilver nanoparticles interrupt Pseudomonas aeruginosa quorum sensing systems. Scientific reports. 2015 Sep 8;5(1):1-4.

- Habash MB, Park AJ, Vis EC, Harris RJ, Khursigara CM. Synergy of silver nanoparticles and aztreonam against Pseudomonas aeruginosa PAO1 biofilms. Antimicrobial agents and chemotherapy. 2014 Oct;58(10):5818-30.

- Morones JR, Elechiguerra JL, Camacho A, Holt K, Kouri JB, Ramírez JT, Yacaman MJ. The bactericidal effect of silver nanoparticles. Nanotechnology. 2005 Aug 26;16(10):2346.

- Jung WK, Koo HC, Kim KW, Shin S, Kim SH, Park YH. Antibacterial activity and mechanism of action of the silver ion in Staphylococcus aureus and Escherichia coli. Applied and environmental microbiology. 2008 Apr 1;74(7):2171-8.

- Rai MK, Deshmukh SD, Ingle AP, Gade AK. Silver nanoparticles: the powerful nanoweapon against multidrug‐resistant bacteria. Journal of applied microbiology. 2012 May;112(5):841-52.

- Hsueh YH, Lin KS, Ke WJ, Hsieh CT, Chiang CL, Tzou DY, Liu ST. The antimicrobial properties of silver nanoparticles in Bacillus subtilis are mediated by released Ag+ ions. PloS one. 2015 Dec 15;10(12):e0144306.

- Kumar NI, Das SA, Jyoti AN, Kaushik SA. Synergistic effect of silver nanoparticles with doxycycline against Klebsiella pneumoniae. Int J Pharm Pharm Sci. 2016;8(7):183-6.

- Shrivastava, S. (2008). Nanomedicine: physiological principle of distribution. Dig. J. Nanomater. Bios, 3, 303-308.

- Dakal TC, Kumar A, Majumdar RS, Yadav V. Mechanistic basis of antimicrobial actions of silver nanoparticles. Frontiers in microbiology. 2016:1831.

- Ghormade, V.; Deshpande, M.V.; Paknikar, K. Perspectives for nano-biotechnology enabled protection and nutrition of plants. Biotechnol. Adv. 2011, 29, 792–803.

- Mishra, S.; Singh, H.B. Biosynthesized silver nanoparticles as a nanoweapon against phytopathogens: Exploring their scope and potential in agriculture. Appl. Microbiol. Biotechnol. 2014, 99, 1097–1107.

- Cox, A.; Venkatachalam, P.; Sahi, S.; Sharma, N. Reprint of: Silver and titanium dioxide nanoparticle toxicity in plants: A review of current research. Plant Physiol. Biochem. 2017, 110, 33–49.

- Zhang, X.-F.; Liu, Z.-G.; Shen, W.; Gurunathan, S. Silver nanoparticles: Synthesis, characterization, properties, applications, and therapeutic approaches. Int. J. Mol. Sci. 2016, 17, 1534.

- Marchiol, L.; Mattiello, A.; Poš´ci´c, F.; Giordano, C.; Musetti, R. In Vivo synthesis of nanomaterials in plants: Location of silver nanoparticles and plant metabolism. Nanoscale Res. Lett. 2014, 9, 1–11.

- Abd-Elsalam, K.A.; Prasad, R. Nanobiotechnology Applications in Plant Protection; Springer: Berlin, Germany, 2018; ISBN 978-3-319-91160-1.

- Park, H.-J.; Kim, S.-H.; Kim, H.-J.; Choi, S.-H. A New Composition of Nanosized Silica-Silver for Control of Various Plant Diseases. Plant Pathol. J. 2006, 22, 295–302.

- Gajbhiye, M.; Kesharwani, J.; Ingle, A.; Gade, A.; Rai, M. Fungus-mediated synthesis of silver nanoparticles and their activity against pathogenic fungi in combination with fluconazole. Nanomed. Nanotechnol. Biol. Med. 2009, 5, 382–386.

- Mahakham,W.; Sarmah, A.K.; Maensiri, S.; Theerakulpisut, P. Nanopriming technology for enhancing germination and starch metabolism of aged rice seeds using phytosynthesized silver nanoparticles. Sci. Rep. 2017, 7, 1–21.

- Shankar, S.; Chorachoo, J.; Jaiswal, L.; Voravuthikunchai, S.P. Effect of reducing agent concentrations and temperature on characteristics and antimicrobial activity of silver nanoparticles. Mater. Lett. 2014, 137, 160–163.

- Jaiswal, L.; Shankar, S.; Rhim, J.-W. Applications of nanotechnology in food microbiology. Methods Microbiol. 2019, 46, 43–60.

- Shyam, A.; Chandran, S.S.; Bini, G.; Sreelekha, E. Plant mediated synthesis of AgNPs and its applications: An overview. Inorg. Nano Met. Chem. 2020, 1–17.

- García-Contreras, R.; Argueta-Figueroa, L.; Mejía-Rubalcava, C.; Jiménez-Martínez, R.; Cuevas-Guajardo, S.; Sánchez-Reyna, P.A.; Zeron, H.M. Perspectives for the use of silver nanoparticles in dental practice. Int. Dent. J. 2011, 61, 297–301.

- Sri Kumaran, N.; Vijayaraj, R. BIosynthesis of silver nano particles from Leucas aspera (willd.) link and its anti-inflammatory potential against carrageen induced paw edema in rats. Int. J. Pharm. Sci. Res. 2017, 8, 2588–2593.

- Kim, J.S.; Kuk, E.; Yu, K.N.; Kim, J.-H.; Park, S.; Lee, H.J.; Kim, S.H.; Park, Y.K.; Park, Y.H.; Hwang, C.-Y.; et al. Antimicrobial effects of silver nanoparticles. Nanomed. Nanotechnol. Biol. Med. 2007, 3, 95–101.

- Singh, R.; Thakur, P.; Thakur, A.; Kumar, H.; Chawla, P.; Rohit, J.V.; Kaushik, R.; Kumar, N. Colorimetric sensing approaches of surface-modified gold and silver nanoparticles for detection of residual pesticides: A review. Int. J. Environ. Anal. Chem. 2020, 1–17.

- Zeng, S.; Baillargeat, D.; Ho, H.-P.; Yong, K.-T. Nanomaterials enhanced surface plasmon resonance for biological and chemical sensing applications. Chem. Soc. Rev. 2014, 43, 3426–3452.

- Zhang, D.; Liu, Q. Biosensors and bioelectronics on smartphone for portable biochemical detection. Biosens. Bioelectron. 2016, 75, 273–284.

- Xiong, D.; Li, H. Colorimetric detection of pesticides based on calixarene modified silver nanoparticles in water. Nanotechnology 2008, 19, 465502.

- Menon, S.K.; Modi, N.R.; Pandya, A.; Lodha, A. Ultrasensitive and specific detection of dimethoate using a p-sulphonatocalix[4]resorcinarene functionalized silver nanoprobe in aqueous solution. RSC Adv. 2013, 3, 10623.