From marine origin to nano world: Utilisation of aquatic resources in development of metal nanoparticles

Sreelakshmi K.R., Mohan C.O. and Bindu J.

ICAR-Central Institute of Fisheries Technology, Matsyapuri. P.O, Willingdon island, Cochin, Kerala, India

Corresponding author: K. R. Sreelakshmi, Scientist, Fish Processing Division, ICAR-Central Institute of Fisheries Technology, Matsyapuri. P.O, Willigdon island, Cochin, Kerala, India.

Email: sreecift@gmail.com

Keywords: Aquatic, Nanoparticles, Organisms, Applications, Seaweed

Abstract

Metal nanoparticles synthesised using green technologies can be utilised for biomedical and other environmental applications. Better ways of utilisation of aquatic resources will help to design new technologies of sustainable nature. Aquatic organisms are rich in bioactive and reducing compounds and can effectively be used for the green synthesis of metal nanoparticles. The compounds like chitosan, collagen, gelatin and fish oil from fish waste help in synthesising nanoparticles under both thermal and non-thermal treatments. The extractives from some aquatic organisms can reduce the metal ions without any chemical supplementation. The synthesis of metal nanoparticles was also possible using the phytoconstituents from seaweeds. The marine microbes can synthesise the nanoparticles both intracellularly and extracellularly. These technologies can be scaled up to meet different industrial applications. This review explains the production strategies of metal nanoparticles using different marine compounds and also their applications.

Graphical abstract

Introduction

The word “nano” came from the Greek “nanos” which means dwarf and it is the prefix for 10-9. Those particles that have size of 1-100nm are termed as nanoparticles (Khan et al. 2014). The peculiar physical and chemical characteristics of these materials arise from the special electronic structures and increased surface area resulting in higher reactive efficiency. The applications of nanoparticles include photochemical, chemistry, biomedical and electronics field (Di Guglielmo et al. 2010).  Nanoparticles of inorganic metals or hybrids of inorganic and organic nanoparticles provides them unique characteristics and increases the applicability than pure large sized counterparts (Kim and Jon, 2012). The properties of nanostructures are determined by shape and size, interparticle distance and nature of protective outer shell (Baraton, 2003).

Generally, the methods employed for production of metal nanoparticles can be divided into two, top down approach and bottom up approach. The top down method includes the mechanical reduction of metals to nanostructured colloids and further stabilisation using stabilising agents.   This includes typical solid–state processing of the metals. The breaking up of bulk particles use the physical processes like crushing, grinding or milling. The problem with this approach is imperfection on the structure of surface which affects the physical properties and surface chemistry. Also the challenging use of apparatus involved adds on to the difficulty. Ball milling and metal vapour technique are examples of methods used for synthesis of nanoparticles using top down approach.

The “bottom-up” method includes the building up of a nanoparticle from the bottom. Atom-atom, molecule to molecule or cluster to cluster approach can be involved in this. The chemical reduction of metal salts is the most common way of synthesis. Other techniques like electrochemical pathways and decomposition of organometallics in a controlled manner are also included in this. The use of stabilisers including polymers, donor ligands and surfactants helps to control formation of nanoclusters and further aggregation.

The mechanism of nanoparticle formation includes two stages of nucleation and growth. Nucleation is the embryonic stage where metal salt will get reduced to metal atoms which are zerovalent. These atoms will collide with other ions or atoms or clusters and irreversible ‘seeds’ will be formed which can be of size below 1nm. The seed formation depends on the difference in redox potential of metal salt and reducing agent and also on the bond strength between metal-metal atoms. The deactivation of formed nanoparticles occurs by formation of bulk. This happens mainly by two ways, Ostwald ripening or aggregation. In Ostwald ripening the diffusion of smaller particles on to larger particles will cause the increase in particle size with increase in time. This happens because of the tendency of the system to reduce total energy by reducing size. The aggregation of particles is caused not by diffusion based interaction, but both increases the size of particle. In order to prevent the nanostructured particles from agglomeration, protective/stabilising agents are necessary. The stabilisation can be electrostatic stabilisation where repulsion between electrical double layers prevents the formation of larger clusters. The other type of stabilisation is steric stabilisation which includes formation of a protective layer on metallic surfaces by organic molecules. Another classification of synthesis of nanoparticles given by Iravani et al. (2018) is given in figure 1.

In this article, the use of different materials originated form the aquatic organisms or direct use of those organisms for reducing or stabilising metal nanoparticles are highlighted to emphasize the importance and scope of marine life in nanotechnology.

Figure 1. Methods of nanoparticle synthesis by Iravani et al. (2018)

Synthesis of nanoparticles by marine animals or animal derived compounds

- Chitosan

Chitin is a polymer of acetyl amino-D-glucose and is distributed in nature in crustaceans, insects and fungi. Chitosan (Figure 2.) is a copolymer of b (1-4) 2-acetamido 2-deoxy-b-D-glucopyranose and 2-amino-2- deoxy-b-D-glycopyranose (Rinaudo et al. 2006). Chitosan is produced by the deacetylation of chitin either using chemicals like acids or alkali or using enzymes. The polymer can be characterised by the number of monomer units which defines the molecular weight and the degree of deacetylation of chitosan. It is soluble in acidic solutions and partially soluble in alkaline solutions and the solubility is affected by degree of deacetylation (Filar and Wirick, 1977). The physicochemical properties of chitosan are explained in table 1.

Figure 2. Structure of chitosan

Table 1. Physicochemical characteristics of chitosan (Li et al. 1992)

| Property | Comment |
| --- | --- |
| Degree of deacetylation | - UV spectrophotometry - IR spectrometry - Dye adsorption - Metachromatic titration - Gas chromatography |
| Molecular weight | - Chromatography - Light scattering - Viscometry |
| Viscosity | Affected by, - Ionic strength - Deacetylation time - Molecular weight - Concentration |
| Solubility | Usually dissolved when pH is less than 6 but affected by - Solvent mixing - Deacetylation - Salvation - Chemical modification |
| Coagulating ability | Binding for - Metal ions - Anionic polymers - Amino acids - Proteins - DNA - Cells - Dyes - Solids |

Chitosan- gold nanocomposites

The synthesis of gold nanoparticles in chitosan involves three reactions. In acidic solution, the chitosan chain will get broken and open chain will be formed at part of the end groups (Reaction I). All the polymers from hydrolysed chitosan will exist in dynamic equilibrium and this process is reversible. On addition of Au3+ ions into the system, the oxidation of –CHO groups in the end of chain occurs and form –COOH groups (Reaction II). This step is irreversible and the dynamic equilibrium will get broken, and the reaction will proceed towards a positive reaction. In this manner chitosan chains will be continuously degraded and gold nanoparticles will be formed.  The degradation of chitosan is higher at higher temperatures and increased concentration of gold ions (Sun et al. 2008). The presence of -NH2, -CH2OH and -CHO groups in chitosan, which are associated with chitosan degree of deacetylation (DD) and molecular weight (MW), decide its chelating, reducing and stabilizing characteristics and finally influence the size and shape of the synthesized AuNPs. The synthesis of nanoparticles can also be done using other reducing agents like sodium citrate. The chitosan nanocomposites exhibit pink to wine red colour and the plasmonic peak will be at ~520nm under UV spectral analysis.

Protocol for the synthesis of gold nanoparticles

In the synthesis of gold nanoparticles, chitosan act as both reducing and stabilising agent. The chitosan is dissolved in 1% acetic acid solution and gold precursor is added under continuous stirring and heat (Usually 70ᵒC to 100ᵒC). Continue stirring is applied for required time till a wine red colour is obtained which indicates the formation of nanoparticles. The time of complete reduction of all gold ions depends on the concentration of gold precursor, concentration of chitosan, temperature of treatment and intrinsic characteristics of chitosan. The solution can be stored under refrigerated conditions after cooling to room temperature (Sreelakshmi et al. 2022).

Properties and applications

The antioxidant activity of chitosan gold nanocomposites were 80 times higher than the potential of ascorbic acid (Esumi et al. (2003). The chitosan gold nanocomposite exhibit antitumour activity as they induce different cell death modalities in HeLa and MCF-7 cells which depends on reactive oxygen species production (Martínez-Torres et al. 2018).

The effect of these nanoparticles against both gram negative and gram positive bacteria like P. aeruginosa, E. Coli, S. aureus and Bacillus spp. etc is well established (Regiel-Futyra et al. 2015, Katas et al. 2019).  These nanoparticles can be efficiently used for drug delivery (Bhumkar et al. 2007) and gene delivery (Bhattarai et al. 2008). They can be used for development of sensors for glucose (Du et al. 2007), acetylcholamine, heavymetals (Sugunan et al. 2005) silver ions (Zhao et al. 2019), caffeic acid (De Carlo et al. 2019) organophosphate pesticides (Du et al. 2007), antibiotics (Lai et al. 2017) and Salmonella (Cinti et al. 2017).

Toxicity

The chitosan gold nanoparticles produce no treatment related toxicity on oral administration and the LD 50 value in rats was found to be 2000mg/Kg (Pokharkhar et al. 2009).

Chitosan silver nanocomposites

The Chitosan-silver composites (Figure 3.) can be made with silver in ionic or metallic form. The stabilisation and dispersion of nanoparticles in chitosan depends on the chemical bond between nitrogen in the amino groups of chitosan and the lone pairs in silver orbitals (Latif et al. 2015). Insitu chemical reduction method is the commonly used technique for preparation of chitosan silver nanocomposites where chemicals like NaBH were used as reducing agent.  Different techniques in preparation of silver nanoparticles using chitosan as reducing agent is shown in Table 2. The chitosan silver nanocomposites exhibit yellow to brown colour and the plasmonic peak will be at ~400nm on UV spectral analysis.

Table 2. Different methods of silver nanoparticle synthesis using chitosan

| Reducing and Stabilising agent | Size of AgNps | References |
| --- | --- | --- |
| Thermal method |  |  |
| Chitosan Chitosan Chitosan Chitosan Carboxymethyl chitosan | 20-150 10-50 55-278 80-120 12-18 | Bal et al., 2012 Wang et al., 2012 Jena et al., 2012 Saravanan et al Fouda et al., 2013 |
| Gamma ray method |  |  |
| Chitosan Chitosan | 20-25 7-30 | Yoksan et al. 2010 Yoksan et al., 2009 |
| UV-irradiation method |  |  |
| Chitosan | 3.16-10.97 | Shameli et al. 2010 |
| Electrochemicalmethod |  |  |
| Chitosan | <50 2-16 | Pishbin et al. 2013 Reicha et al. 2012 |

Properties and applications

- Silver nanoparticles exhibit fungicidal activity (Wang et al. 2015) and antibacterial activity against both gram negative and gram positive bacteria (Wei et asl., 2009, Tran et al. 2010). They have antixodant activity (Hajji et al. 2019) and exhibit antiproliferative activities against carcinoma cells (Tran et al. 2010). They can be used for development of gels or nanofibres with wound healing properties (Li et al. 2016) and as sensor for glucose detection (Jiang et al. 2012). These nanoparticles are effective plasmonic substrates for Surface-enhanced Raman spectroscopy detection of nonresonant analytes at the single-molecule level (Potara et al. 2012). These can form a protective film over steel and act as cathodic type inhibitor against corrosion (Solomon et al. 2017) and also has the ability to remove pesticides from water (Saiffudin et al. 2011).

Figure 3. Reduction of AgNPs using NaBH4 and its stabilisation using chitosan (Wang et al. 2015)

Other metal nanocomposites

Chitosan can effectively be utilised for the formation of nanoparticles using metals like zinc, palladium, platinum and copper, either as pure chitosan or as modified forms like carboxymethyl chitosan (Adlim et al. 2004, Zain et al. 2014).

- Collagen

Collagen constitutes the major component of connective tissue membranes that joins the myotomes in fish muscle.  It constitutes about 0.2 to 1.4% of total protein in fish and is highly responsible for the integrity of fillets. The content of collagen increases during maturation of fish without significant changes in extend of crosslinking. The hydroxyproline and proline residues effects the properties of collagen significantly (Sikorski et al. 1984).

Collagen comprises 30% of extracellular matrix proteins in living organisms and hence is the most abundant protein in extracellular matrix.  It functions as a structural component and helps in signalling through the biomolecular interactions. Collagen can interact with many biomolecules including sugars, proteins, polyphenols, proteoglycans and drugs. This helps in selective probing of a number of molecular interactions. As collagen is rigid and naturally exists as a protein scaffold, it can be an ideal protein target for making a protein-nanoparticle scaffold. The structural stability of collagen offers less deviations in structure and function on combination with nanoparticles (Figure 4.) and thus helps in targeted interactions with biomolecules (Unser et al. 2017).

Figure 4. Gold nanoparticle synthesis assisted by collagen

In formation of gold nanoparticles, collagen plays dual role by making complexes on binding to the metal ions besides acting as a capping ligand. The concentration of collagen can be positively correlated with the formation of nanoparticles but also increases aggregation (Kumari et al. 2012). Collagen AuNP composites with nanoparticle dose of <20 ppm and size >20 nm are non-toxic 3T3 fibroblasts and HaCat keratinocytes. Sponges made of these composites have high biocompatibility and wound healing capacity (Akturk et al. 2016). The presence of collagen helps in giving uniform shape to nanoparticles and also the positive charged linear structures will help to assemble nanoparticles on to collagen and thus forming nanoparticle films or matrices (Wei et al. 2007). The silver nanoparticles stabilised with collagen have peculiar shape, size and positive zeta potential which impart antibacterial activity to nanoparticles and collagen hydrogels.

Applications and properties

- The collagen nanoconjugates with gold chloride can be used as colorimetric sensor for large range of targets, eg; the collagen conjugates with 10nm gold nanoparticles can be used as sensor for detecting glucose and heparin (Unser et al. 2017).  The collagen silver nano-composites are non-toxic to human fibroblasts and keratinocytes (Alarcon et al. 2012). The collagen copper nanocomposites also have antibacterial efficiency and can be used for wound healing purpose and is non-toxic (Premalatha and Kothai, 2017). The antimicrobial collagen nanocomposites are biocompatible, biodegradable and are cost effective (Grigore et al. 2017).

- Gelatin

Gelatin is the edible protein derived by hydrolysis of collagen. The applicability of gelatin is vast because of the non-toxicity, lower cost, biocompatilbility and affinity to proteins. The gelatin can stabilize nanoparticles electrostatically and in a steric manner. The gelatin (Figure 5) exists in an ordered α helix conformation at room temperature and remains in unfolded condition at elevated temperatures. The functional groups of gelatin like suspended double bond, -SH, -NH and –COOH makes further modifications of gelatin with other molecules. This makes gelatin ideal for development of nanomaterialised devices. The degradation of gelatin can be caused by the incubation parameters like temperature, pH, salt ions and time which inturn affects the reducing and stabilizing property of gelatin. (van den Bosch & Gielens, 2003). The studies on synthesis of metal nanoparticles using fish gelatin is given as table 3.

Figure 5. Typical gelatin polypeptide (Liu et al. 2011)

Gelatin gold nanocomposites

The synthesis of AuNPs can be affected by gelatin in a time dependent manner. The introduction of gelatin in early stage (nucleation) will slow down the process of reduction using other reducing agents and hence the nanoparticles formed will be larger but fewer. Similarly, the gelatin addition in a later stage, ie; growth stage, will yield smaller but larger number of nanoparticles.  Gelatin will stabilize AuNPs on sustained heating and diffusion barrier caused by gelatin cause a reduction in growth of nanoparticles and colour of the resultant solution changes accordingly. Reduction time, heating time and heating temperature are the major factors affecting the synthesis of nanoparticles (Wang and Gunasekharan, 2012). The synthesis of gold nanoparticles with gelatin as both reducing and stabilizing agent will result in larger irregular particles which disintegrates to smaller particles with increase in time of application of heat.

The concentration of gelatin affects the stability of nanoparticles. A decreased concentration causes a shift in plasmonic peak towards right which can be attributed to the reduced stability leading to aggregation.  This is because few gelatin molecules will be available to bind with the nanoparticles thus reducing the stability. Also the change in concentration of gelatin cause a change in dielectric constant of the medium and this reduces the dipole oscillations in the electrons. The peculiar plasmonic peak of nanoparticles is also affected by the sharp edges which shows the influence of shape on characteristics exhibited by nanocomposites (Mock et al. 2002).

Both acidic and basic functional groups are present in gelatin polypeptides. The amine groups changes to –NH3+ and thus giving a net positive charge to gelatin below the isoelectric point of gelatin ie, Ph 4.7. Similarly, the carboxyl groups and the sulfhydryl groups impart a net negative charge to gelatin at pH higher than 4.7. This changes the electron donating capacity of gelatin and the reduction of Au III to Au II will get affected.  Gelatin cannot act as a reducing agent for AuNPs at pH < 1 or pH > 9 which is attributed to gelatin structure. The glutamic acid and proline interacts well with gold ions and the glutamic acid plays a key role in reducing the ions and stabilising the nanoparticles. The plasmon resonance peak of gelatin gold nanocomposite will remain stable even at altered pH and salt concentration (Liu et al. 2011).

Gelatin silver nanocomposites

The synthesis of silver nanoparticles in gelatin depends on temperature. At higher temperatures the nanoparticles will dissociate forming smaller particles which are stabilized by the amide pendents of gelatin. (Darroudi et al. 2011). On preparation of AgNPs in gelatin using UV irradiation, the increased time of UV application can be attributed to the degradation of gelatin leading to agglomeration of nanoparticles and a broader spectrum.

Table 3. Reports on synthesis of metal nanoparticles using gelatin

| Reducing agent | Stabilizing agent | Temperature | Time | Metal | Size of nanoparticle(nm) | reference |
| --- | --- | --- | --- | --- | --- | --- |
| Gelatin | gelatin | 60ᵒC | 48hrs | silver | 3.78 | Darroudi et al. 2011ͣ |
| Gelatin | gelatin | 80ᵒC | 40min | Gold | 50-80 | Liu et al. 2011 |
| Laser ablation | gelatin | - | - | silver | 8.95-33.76 | Darroudi et al. 2011ᵇ |
| Formic acid | gelatin | Room temperature | 1min | silver | 13-25 | Jeong and Park (2014) |
|  | gelatin | UV irradiation | 48h | silver | 20.99 | Darroudi et al. 2011 |
| Formic acid | gelatin | UV irradiation | 3h | silver | 9-20 | Xu and Zhou, 2008 |
| Sodium citrate | gelatin | - | 15min | gold | 10-15 | Neupane et al. 2011 |

Synthesis of nanoparticles using fish oil

Fish oil is an important source of fatty acids and vitamins especially omega 3 fatty acids, vitamin A and and vitamin D. Omega-3 fatty acids regulate every system in the body, including immune system, cardiovascular system and nervous system. Fish oil can act as both reducing agent and surfactant in formation of nanoparticles (Asmathunisha and Kathiresan, 2013). This property is exhibited mainly because of the carboxylate groups and amines present in fish oil.

Protocol for the synthesis of silver nanoparticles

Heating Fish oil and silver salt (silver nitrate or silver myristate) at 100-140oC for 5h in inert atmosphere can form silver nanoparticles (Khanna and Nair, 2009)

Synthesis of nanoparticle using marine sponge

Marine sponges are known to be gold mines because of the variety of molecules they exhibit. They possess bioactive properties like antitumour, anti-inflammatory, anti-viral and antioxidant properties because of the presence of a variety of biomolecules. Manoalide, dysitrotonic acid, spongothymidine, xestospongin etc. are some of the bioactive molecules present in sponges. Apart from these activities the sponges can synthesis nanoparticles extracellularly. The presence of organic amines in sponge extracts helps to reduce the metal ions and form metal nanoparticles. The nanoparticles are synthesised successfully using extracts of Acanthella elongata (Inbakandan et al. 2010, Inbakandan et al. 2012), Haliclona spp (Hamed et al. 2015) and Axinella sinoxia (Hamed et al. 2017). The silver nanoparticles produced using extract of Heliclona exigua can be used for dental care and for the oral cancer cell lines the half maximal inhibitory concentration  value estimated for these AgNPs is 0.6μg/ml (Inbakandan et al. 2016).

Protocol for the synthesis of gold nanoparticles using marine sponge Acanthella elongata

For the synthesis of gold nanoparticles, the sponge is ground in water and collect the filtrate. Ten millilitres of filtrate can be added to 100ml auric chloride solution and stirred for 4hrs at 45oC for the formation of nanoparticles.

Seaweed in synthesis of metal nanoparticles

Over last 70 years there was a dramatic development in seaweed culture mostly in Asia and also recently in Americas and Europe. Seaweed, also known as marine macroalgae is the common name for uncountable plants in sea, rivers and other water bodies. Seaweeds are among the primary producers of sea and are suppliers of oxygen for other living organisms. They have the capacity to remove pollutants and thus have bioremediation capacity. They possess high survival capabilities under any environmental conditions. They possess good antioxidant, antimicrobial and other bioactive properties. They are widely used in food, cosmetics, fertilisers and for production of hydrocolloids like agar, carrageenan etc. (Chan et al. 2006).

Based on the photosynthetic pigments, storage compounds and composition of cell wall, seaweeds are classified into three phyla namely, rhodophyceae (red seaweeds), pheophyceae (brown seaweeds), and chlorophyceae (green seaweeds). They can be easily distinguished based on the colour of thallus. Green seaweeds are seen in freshwater than in marine water. Both red and brown seaweeds are common in marine waters. Polysaccharides, polyphenolic compounds, proteins and other chelating agents in seaweeds can act as reducing agents for metal ions. Thus the extracts of seaweeds can form better alternative for the other plant sources used for the preparation of metal nanoparticles.

Protocol for synthesis of metal nanoparticles using seaweed

The algal extract is prepared in water or organic solvents. The extract is heated and metal precursor is added to it. The solution is incubated for specific period under controlled conditions for the formation of nanoparticles.

Details of synthesis of nanoparticles using different seaweed are given in tables 4 and 5.

Table 4. Synthesis of silver nanoparticles using seaweeds

| c | size | temperature | Active agent | application | Reference |
| --- | --- | --- | --- | --- | --- |
| Ulva lactuca | 48.59 | RT | Phenolic compounds, amines and aromatic rings | Photocatalytic degradation | Kumar et al. 2013 ͣ |
| Ulva lactuca | 10-30 | 100 | phytochemicals | antibacterial | Raja et al. 2012 |
| Ulva fasciata | 40.05 | RT | Ethyl acetate | antibacterial | Rajesh et al. 2012 |
| Urospora spp. | 20-30 | 70 | phytochemicals | antibacterial | Suriya et al. 2012 |
| Codium capitatum | 3-44 | RT | proteins |  | Kannan et al. 2013 |
| Enteromorpha | 2-32 | RT |  | antimicrobial | Yousefzadi et al. 2014 |
| Caulerpa scalpelliformis |  | RT | Aminoacids and proteins | mosquitocidal | Murugan et al. 2015 ͣ |
| Ulva lactuca |  | RT | Polyphenol | Malaria control | Murugan et al. 2015 ᵇ |
| Acanthophora spicifera | 48 | 60 | Phenolic compounds | Antibiofilm activity | Kumar et al. 2012 ͣ |
| Gracillaria corticata | 18-46 | 60 | Polyphenols and tannins | Antifungal activity | Kumar et al. 2013 ᵇ |
| Gelidiella acerosa | 22 | RT | Aromatic compounds/alkanes/amines | Antifungal activity | Vivek et al. 2011 |
| Hypnea musciformis | 2-55.8 | 28 | Cyclic peptides | Photocatalytic degradation | Ganapathy et al. 2014 |
| Hypnea musciformis | 40-65 | - | In situ oxidation of hydroxyl groups and by the intrinsic carbonyl groups | Larvicidal activity | Roni et al. 2015 |
| Pterocladiella capillacea | 11.4 | RT | Proteins | Anticancer activity | El Kassas et al. 2014 |
| Sargassum longifolium | 30 | RT | Proteins | Anticancer activity | Devi et al. 2013 |
| Padina tetrastromatica | 20 | RT | Aromatic compound or alkanes or amines | - | Jegadeeswaran et al. 2012 |
| Sargassum ilicifolium | 33-44 | 60 | - | Antibacterial and in vitro cytotoxicity | Kumar et al. 2012 ᵇ |
| Sargassum tenerrimum | 20 | 60 | Hydroxyl/methoxy groups, ketones, polysaccharides | Antibacterial activity | Kumar et al. 2012 ᶜ |
| Sargassum polycystum | 50-100 | RT | Carboxylic, amine, phosphate, and hydroxyl groups | Anticancer activity | Thangaraju et al. 2012 |
| Turbinaria conodies | 96 | RT | Polyphenols, polysaccharides, primary amines | Antimicrobial activity | Rajeshkumar et al. 2013 |
| Turbinaria conodies | 2-17 | RT | Free hydroxyl and carboxylic acid groups | Antimicrofouling activity | Vijayan et al. 2014 |
| Cystophora moniliformis | 75 |  |  |  | Prasad et al. 2012 |
| Padina gymnospora | 25-40 |  |  | Antibacterial activity | Shiny et al. 2013 |
| Sargassum muticum | 43-79 | RT | Sulfated and hydroxyl groups | Antibacterial and insecticidal property | Madhiyazhagan et al. 2015 |
| Sargassum cinereum | 45-75 | RT |  | Antibacterial | Mohandass et al. 2013 |
| Sargassum swartzii | 35 | 60 | Alcohol, carboxylic and amide 1 group | Anticancer | Dass et al. 2014 |

Table 5. Synthesis of other metal nanoparticles using seaweed

| Seaweed name | Metal | size | temperature | Active agent | application | reference |
| --- | --- | --- | --- | --- | --- | --- |
| Stoemchospermum marginatum | Gold | 18.7–93.7 nm | RT | Terpenoids, polyphenols and phenolic compounds | Antibacterial activity | Arockiya Aarthi Rajathi et al. 2012 |
| Padina gymnospora | Platinum | 35 nm | 50 | Sulfated polysaccharide | Hemolytic assay | Shiny et al. 2014 |
| Padina gymnospora | Gold | 53nm | 75 | Fucoxanthin or flavanoids | Anticancer activity | Singh et al. 2013 |
| Sargassum muticum | Magnetic Iron-oxide | 18 nm | 25 | Sulfated polysaccharides, hydroxyl, and aldehyde groups |  | Mahadevi et al. 2013 |
| Sargassum muticum | Zinc oxide | 30-57 | 450 | Sulfated polysaccharides |  | Azizi et al. 2014 |
| Sargassum muticum | Gold | 5.42 | 45 | Fucoxanthin or polysaccharides, polyphenol, and other biomolecules | Anticancer activity | Namvar et al. 2014 |
| Sargassum myriocystum | Zinc oxide | 76–186 nm | 80C | Alginic acid, ascorbic acid, protein, carbohydrates, flavanoids, tannins, mannitol, and lipids | Antibacterial activity | Stalin dhas et al. 2012 |
| Turbinaria Connoides | gold | 12-57 |  |  | Catalyst | Ramakrishna et al. 2016 |
| Sargassum tennerimum | gold | 5-45 |  |  | Catalyst | Ramakrishna et al. 2016 |

Synthesis of nanoparticles using marine microorganisms

Marine microorganisms include microalgae, bacteria and fungi are the microbes living in marine environment and are either prokaryotic or eukaryotic organisms. They can synthesis metallic nanoparticles using intracellular or extracellular pathway. The microbially synthesised nanoparticles can be used as therapeutic agents.

Intracellular synthesis

The mechanism of synthesis of nanoparticles intracellularly can’t be explained exactly because of different biomolecules involved in synthesis in different microbes. Hypothetically, the positive charged metal ions are trapped on the surface of cell wall or cytoplasm which contains negative charged ions of enzymes or proteins. The trapped metal ions will get reduced forming nanoparticles. The synthesis of nanoparticles occurs on cell wall (eg: synthesis of silver nanoparticles by fungus, Verticillium sp.), on cytoplasmic membrane (eg: synthesis of gold nanoparticles in Rhodococcus Spp) or both (eg: gold nanoparticles synthesis by algae, Tetraselmis kochinensis).

The protocol for synthesis of nanoparticles using microorganisms intracellularly include the following steps,

- Culturing the microorganisms in growth media

- Washing the microorganisms

- Centrifugation to remove the components of growth media

- Inoculation of the collected mass with metal precursor

- Incubation under specific atmospheric conditions

- Cell lysis and centrifugation for collection of nanoparticles

Extracellular synthesis

The synthesis of nanoparticles extracellularly depend on the microbial proteins or secreted enzymes. In fungus and bacteria the enzyme α-NADPH dependent nitrate reductase plays a key role in formation of nanoparticles. The cofactor NADH is secreted to the enzyme and the electron is transferred from NADH to NADH dependent reductase. Thus the enzyme acts as an electron carrier which is finally transferred to metal ions which get reduced to form nanoparticles. The fungus Fusarium oxysporum and the bacteria Rhodopseudomonas capsulata can synthesis gold nanoparticles in this manner. The microalgae, Chlorella vulgaris reduces silver ions extracellularly, but the mechanism is unknown.

The synthesis of nanoparticles using microorganisms extracellularly can be done using two methods,

- Using cell extract

- Culturing the microbes in growth media

- Washing and centrifugation of cell biomass

- Collection of extract using either lysis of biomass or incubation of biomass in distilled water or using dry biomass extraction

- Centrifuge to collect the cell free extract and inoculate with metal precursor

- Incubation for nanoparticle formation

- Centrifugation for collection of nanoparticles

- Using cells

- Culturing the microorganisms in growth media

- Washing the microorganisms

- Centrifugation to remove the components of growth media

- Inoculation of the collected mass with metal precursor

- Incubation under specific atmospheric conditions

- Cell lysis and centrifugation for collection of nanoparticles

The synthesis of nanoparticles using marine microbes and the potential applications reported are given in table 6.

Table 6. Synthesis of metal nanoparticles using different microorganisms of marine origin (Patil and Kim, 2018)

| Marine microorganism | Species | Type of nanoparticle | Location of nanoparticles | Reaction condition | Size (nm) | Applications |
| --- | --- | --- | --- | --- | --- | --- |
| Actinobacteria | Rhodococcus sp. | gold | intracellular | Active biomass | 5-15 | - |
|  | Streptomyces sp. Al-Dhabi-87 | Silver | extracellular | supernantent | 10-17 | antimicrobial |
| Bacteria | Desulforibrio caledoiensis | Zinc sulfide | extracellular | supernatent | 30 | photocatalysis |
|  | Enterococcus sp | Cadmium sulfide | extracellular | supernatent | 50-180 | antimicrobial |
|  | Escherichia coli VM1 | silver | extracellular | supernatent | 10-15 | anticancer |
|  | Idiomarina sp.PR 58-8 | silver | intracellular | Active biomass | 26 |  |
|  | Marinobactor pelagius | gold | extracellular | Active biomass | 2-6 |  |
|  | Ochrobactrum anthropi | silver | intracellular | Active biomass | 38-85 | antibacterial |
|  | Saccharophagus degradans ATCC 43961 | Manganese dioxide | extracellular | supernatent | 34 |  |
|  | Vibrio alginolyticus | silver | intracellular | Active biomass | 50-100 |  |
| Cyanobacteria | Plectonema boryanum UTEX 485 | silver | intracellular | Active biomass | <10 |  |
|  | Spirulina platensis | gold | extracellular | Dry biomass | 6-10 |  |
| Fungi | Aspergillus sydowii | gold | Intracellular, extracellular | Active biomass | 8.7-15.6 |  |
|  | Aspergillus terreus | silver | extracellular | supernatent | 1-20 |  |
|  | Aspergillus terreus | gold | intracellular | Active biomass |  | cytotoxicity |

Future prospects

. There are more reducing sources available from aquatic resources that are to be investigated. Further studies on utilization of underutilized or unutilized resources for development of nano based structures will help to reduce the environmental pollution. Along with the studies on effect of different sources as reducing agents, the mechanism of formation of nanoparticles using these technologies and their characteristics are not well-known. In the case of use of extracts, the composition of extracts and the components responsible for the reduction of meal ions are to be investigated further. The applications of the nanoparticles formed is to be studied because the characteristics of nano particles synthesized has immense effect on the performance of nanoparticles.

Conclusion

The aquatic environment acts as a store house for a wide variety of with different applicaions. The compounds extracted from fish waste as source of nanoparticle synthesis will help in reducing pollution and improved environmental management. Also the cost of production of nanoparticles can be reduced. The efficient synthesis of nanoparticles using seaweeds creates improved use of seaweed stocks for industrial applications. The techniques for development of nanoparticles using the marine organisms like sponges, seaweeds, microorganisms etc. lead to further investigations for upgradation of aquaculture of the specific species.

References

- Adlim, M., Bakar, M. A., Liew, K. Y., & Ismail, J. (2004). Synthesis of chitosan-stabilized platinum and palladium nanoparticles and their hydrogenation activity. Journal of Molecular Catalysis A: Chemical, 212(1-2), 141-149.

- Akturk, O., Kismet, K., Yasti, A. C., Kuru, S., Duymus, M. E., Kaya, F& Keskin, D. (2016). Collagen/gold nanoparticle nanocomposites: a potential skin wound healing biomaterial. Journal of biomaterials applications, 31(2), 283-301.

- Alarcon, E. I., Udekwu, K., Skog, M., Pacioni, N. L., Stamplecoskie, K. G., González-Béjar, M& Scaiano, J. C. (2012). The biocompatibility and antibacterial properties of collagen-stabilized, photochemically prepared silver nanoparticles. Biomaterials, 33(19), 4947-4956.

- Asmathunisha, N., & Kathiresan, K. (2013). A review on biosynthesis of nanoparticles by marine organisms. Colloids and Surfaces B: Biointerfaces, 103, 283-287.

- Azizi, S., Ahmad, M. B., Namvar, F., & Mohamad, R. (2014). Green biosynthesis and characterization of zinc oxide nanoparticles using brown marine macroalga Sargassum muticum aqueous extract. Materials Letters, 116, 275-277.

- Bal, K. E., Bal, Y., Cote, G., & Chagnes, A. (2012). Morphology and antimicrobial properties of Luffa cylindrica fibers/chitosan biomaterial as micro-reservoirs for silver delivery. Materials Letters, 79, 238-241.

- Bhattarai, S. R., Kc, R. B., Aryal, S., Bhattarai, N., Kim, S. Y., Yi, H. K., ... & Kim, H. Y. (2008). Hydrophobically modified chitosan/gold nanoparticles for DNA delivery. Journal of Nanoparticle Research, 10(1), 151-162.

- Bhumkar, D. R., Joshi, H. M., Sastry, M., & Pokharkar, V. B. (2007). Chitosan reduced gold nanoparticles as novel carriers for transmucosal delivery of insulin. Pharmaceutical research, 24(8), 1415-1426.

- Chan, C. X., Ho, C. L., & Phang, S. M. (2006). Trends in seaweed research. Trends in Plant Science, 11(4), 165-166.

- Cinti, S., Volpe, G., Piermarini, S., Delibato, E., & Palleschi, G. (2017). Electrochemical biosensors for rapid detection of foodborne Salmonella: A critical overview. Sensors, 17(8), 1910.

- Darroudi, M., Ahmad, M. B., Abdullah, A. H., & Ibrahim, N. A. (2011). Green synthesis and characterization of gelatin-based and sugar-reduced silver nanoparticles. International journal of nanomedicine, 6, 569.

- Darroudi, M., Ahmad, M. B., Zak, A. K., Zamiri, R., & Hakimi, M. (2011). Fabrication and characterization of gelatin stabilized silver nanoparticles under UV-light. International journal of molecular sciences, 12(9), 6346-6356.

- Darroudi, M., Ahmad, M. B., Zamiri, R., Abdullah, A. H., Ibrahim, N. A., Shameli, K., & Husin, M. S. (2011). Preparation and characterization of gelatin mediated silver nanoparticles by laser ablation. Journal of Alloys and Compounds, 509(4), 1301-1304.

- Devi, J. S., Bhimba, B. V., & Peter, D. M. (2013). Production of biogenic silver nanoparticles using Sargassum longifolium and its applications. Indian Journal of Marine Science. 2013, 42, 125–130.

- Dhas, T. S., Kumar, V. G., Abraham, L. S., Karthick, V., & Govindaraju, K. (2012). Sargassum myriocystum mediated biosynthesis of gold nanoparticles. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 99, 97-101.

- Dhas, T. S., Kumar, V. G., Karthick, V., Govindaraju, K., & Narayana, T. S. (2014). Biosynthesis of gold nanoparticles using Sargassum swartzii and its cytotoxicity effect on HeLa cells. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 133, 102-106.

- Di Carlo, G., Curulli, A., Toro, R. G., Bianchini, C., De Caro, T., Padeletti, G., ... & Ingo, G. M. (2012). Green synthesis of gold–chitosan nanocomposites for caffeic acid sensing. Langmuir, 28(12), 5471-5479.

- Du, D., Ding, J., Cai, J., & Zhang, A. (2007). One-step electrochemically deposited interface of chitosan–gold nanoparticles for acetylcholinesterase biosensor design. Journal of Electroanalytical Chemistry, 605(1), 53-60.

- Du, Y., Luo, X. L., Xu, J. J., & Chen, H. Y. (2007). A simple method to fabricate a chitosan-gold nanoparticles film and its application in glucose biosensor. Bioelectrochemistry, 70(2), 342-347.

- El Kassas, H. Y., & Attia, A. A. (2014). Bactericidal application and cytotoxic activity of biosynthesized silver nanoparticles with an extract of the red seaweed Pterocladiella capillacea on the HepG2 cell line. Asian Pac J Cancer Prev, 15(15), 1299-1306.

- Esumi, K., Takei, N., & Yoshimura, T. (2003). Antioxidant-potentiality of gold–chitosan nanocomposites. Colloids and Surfaces B: Biointerfaces, 32(2), 117-123.

- Fouda, M. M., El-Aassar, M. R., & Al-Deyab, S. S. (2013). Antimicrobial activity of carboxymethyl chitosan/polyethylene oxide nanofibers embedded silver nanoparticles. Carbohydrate polymers, 92(2), 1012-1017.

- Grigore, M. E., Grumezescu, A. M., Holban, A. M., Mogoşanu, G. D., & Andronescu, E. (2017). Collagen-nanoparticles composites for wound healing and infection control. Metals, 7(12), 516.

- Hajji, S., Khedir, S. B., Hamza-Mnif, I., Hamdi, M., Jedidi, I., Kallel, R., ... & Nasri, M. (2019). Biomedical potential of chitosan-silver nanoparticles with special reference to antioxidant, antibacterial, hemolytic and in vivo cutaneous wound healing effects. Biochimica et Biophysica Acta (BBA)-General Subjects, 1863(1), 241-254.

- Hamed, M. R., Givianrad, M. H., & Moradi, A. M. (2015). Biosynthesis of Silver Nanoparticles Using Marine Sponge. Oriental Journal of Chemistry, 31(4), 1961-1967.

- Hamed, M. R., Givianrad, M. H., & Moradi, A. M. (2017). Green synthesis of silver nanoparticles using marine sponge Axinella sinoxia. 46 (01), 125-130.

- Inbakandan, D., Kumar, C., Bavanilatha, M., Ravindra, D. N., Kirubagaran, R., & Khan, S. A. (2016). Ultrasonic-assisted green synthesis of flower like silver nanocolloids using marine sponge extract and its effect on oral biofilm bacteria and oral cancer cell lines. Microbial pathogenesis, 99, 135-141.

- Inbakandan, D., Sivaleela, G., Peter, D. M., Kiurbagaran, R., Venkatesan, R., & Khan, S. A. (2012). Marine sponge extract assisted biosynthesis of silver nanoparticles. Materials Letters, 87, 66-68.

- Inbakandan, D., Venkatesan, R., & Khan, S. A. (2010). Biosynthesis of gold nanoparticles utilizing marine sponge Acanthella elongata (Dendy, 1905). Colloids and Surfaces B: Biointerfaces, 81(2), 634-639.

- Iravani, S., Thota, S., & Crans, D. C. (2018). Methods for preparation of metal nanoparticles. Metal nanoparticles: synthesis and applications in pharmaceutical sciences, 15-32.

- Jegadeeswaran, P., Shivaraj, R., & Venckatesh, R. (2012). Green synthesis of silver nanoparticles from extract of Padina tetrastromatica leaf. Digest Journal of Nanomaterials and Biostructures, 7(3), 991-998.

- Jena, P., Mohanty, S., Mallick, R., Jacob, B., & Sonawane, A. (2012). Toxicity and antibacterial assessment of chitosancoated silver nanoparticles on human pathogens and macrophage cells. International journal of nanomedicine, 7, 1805.

- Jeong, L., & Park, W. H. (2014). Preparation and characterization of gelatin nanofibers containing silver nanoparticles. International journal of molecular sciences, 15(4), 6857-6879.

- Jiang, H., Chen, Z., Cao, H., & Huang, Y. (2012). Peroxidase-like activity of chitosan stabilized silver nanoparticles for visual and colorimetric detection of glucose. Analyst, 137(23), 5560-5564.

- Kannan, R. R. R., Stirk, W. A., & Van Staden, J. (2013). Synthesis of silver nanoparticles using the seaweed Codium capitatum PC Silva (Chlorophyceae). South African Journal of Botany, 86, 1-4.

- Katas, H., Lim, C. S., Azlan, A. Y. H. N., Buang, F., & Busra, M. F. M. (2019). Antibacterial activity of biosynthesized gold nanoparticles using biomolecules from Lignosus rhinocerotis and chitosan. Saudi Pharmaceutical Journal, 27(2), 283-292.

- Khanna, P. K., & Nair, C. K. K. (2009). Synthesis of silver nanoparticles using cod liver oil (fish oil): green approach to nanotechnology. International Journal of Green Nanotechnology: Physics and Chemistry, 1(1), P3-P9.

- Kumar, P. ͣ, Senthamilselvi, S., Lakshmipraba, A., Premkumar, K., Muthukumaran, R., Visvanathan, P., ... & Govindaraju, M. (2012). Efficacy of bio-synthesized silver nanoparticles using Acanthophora spicifera to encumber biofilm formation. Digest Journal of Nanomaterials and Biostructures, 7(2), 511-522.

- Kumar, P. ᵇ, Selvi, S. S., Praba, A. L., Selvaraj, M., Rani, L. M., Suganthi, P.  Devi B. S. & Govindaraju, M. (2012). Antibacterial activity and in-vitro cytotoxicity assay against brine shrimp using silver nanoparticles synthesized from Sargassum ilicifolium. Digest Journal of Nanomaterials and Biostructures, 7(4), 1447-1455.

- Kumar, P. ᶜ, Senthamil Selvi, S., Lakshmi Prabha, A., Prem Kumar, K., Ganeshkumar, R. S., & Govindaraju, M. (2012). Synthesis of silver nanoparticles from Sargassum tenerrimum and screening phytochemicals for its antibacterial activity. Nano Biomed Eng, 4(1), 12-16.

- Kumar, P. ͣ, Govindaraju, M., Senthamilselvi, S., & Premkumar, K. (2013). Photocatalytic degradation of methyl orange dye using silver (Ag) nanoparticles synthesized from Ulva lactuca. Colloids and Surfaces B: Biointerfaces, 103, 658-661.

- Kumar, P.ᵇ, Selvi, S. S., & Govindaraju, M. (2013). Seaweed-mediated biosynthesis of silver nanoparticles using Gracilaria corticata for its antifungal activity against Candida spp. Applied Nanoscience, 3(6), 495-500.

- Kumari, K., Singh, P., & Mehrotra, G. K. (2012). A facile one pot synthesis of collagen protected gold nanoparticles using Na–malanodialdehyde. Materials Letters, 79, 199-201.

- Lai, C., Liu, X., Qin, L., Zhang, C., Zeng, G., Huang, D & Huang, D. (2017). Chitosan-wrapped gold nanoparticles for hydrogen-bonding recognition and colorimetric determination of the antibiotic kanamycin. Microchimica Acta, 184(7), 2097-2105.

- Latif, U., Al-Rubeaan, K., & Saeb, A. T. (2015). A review on antimicrobial chitosan-silver nanocomposites: a roadmap toward pathogen targeted synthesis. International Journal of Polymeric Materials and Polymeric Biomaterials, 64(9), 448-458.

- Li, C. W., Wang, Q., Li, J., Hu, M., Shi, S. J., Li, Z. W.,& Yu, X. H. (2016). Silver nanoparticles/chitosan oligosaccharide/poly (vinyl alcohol) nanofiber promotes wound healing by activating TGFβ1/Smad signaling pathway. International Journal of Nanomedicine, 11, 373.

- Li, Q., Dunn, E. T., Grandmaison, E. W., & Goosen, M. F. (1992). Applications and properties of chitosan. Journal of Bioactive and Compatible Polymers, 7(4), 370-397.

- Lin, J., He, C., Zhao, Y., & Zhang, S. (2009). One-step synthesis of silver nanoparticles/carbon nanotubes/chitosan film and its application in glucose biosensor. Sensors and Actuators B: Chemical, 137(2), 768-773.

- Liu, Y., Liu, X., & Wang, X. (2011). Biomimetic synthesis of gelatin polypeptide-assisted noble-metal nanoparticles and their interaction study. Nanoscale Res Lett, 6(1), 22.

- Madhiyazhagan, P., Murugan, K., Kumar, A. N., Nataraj, T., Dinesh, D., Panneerselvam, C., ... & Nicoletti, M. (2015). Sargassum muticum-synthesized silver nanoparticles: an effective control tool against mosquito vectors and bacterial pathogens. Parasitology research, 114(11), 4305-4317.

- Mahdavi, M., Namvar, F., Ahmad, M. B., & Mohamad, R. (2013). Green biosynthesis and characterization of magnetic iron oxide (Fe3O4) nanoparticles using seaweed (Sargassum muticum) aqueous extract. Molecules, 18(5), 5954-5964.

- Martínez-Torres, A. C., Zarate-Triviño, D. G., Lorenzo-Anota, H. Y., Ávila-Ávila, A., Rodríguez-Abrego, C., & Rodríguez-Padilla, C. (2018). Chitosan gold nanoparticles induce cell death in HeLa and MCF-7 cells through reactive oxygen species production. International journal of nanomedicine, 13, 3235.

- Mock JJ, Barbic M, Smith DR, Schultz DA, Schultz S (2002) Shape effects in plasmon resonance of individual colloidal silver nanoparticles. J Chem Phys 116:6755–6759

- Mohandass, C., Vijayaraj, A. S., Rajasabapathy, R., Satheeshbabu, S., Rao, S. V., Shiva, C., & De-Mello, I. (2013). Biosynthesis of silver nanoparticles from marine seaweed Sargassum cinereum and their antibacterial activity. Indian journal of pharmaceutical sciences, 75(5), 606.

- Murugan, K.ͣ, Benelli, G., Ayyappan, S., Dinesh, D., Panneerselvam, C., Nicoletti, M., ... & Suresh, U. (2015). Toxicity of seaweed-synthesized silver nanoparticles against the filariasis vector Culex quinquefasciatus and its impact on predation efficiency of the cyclopoid crustacean Mesocyclops longisetus. Parasitology research, 114(6), 2243-2253.

- Murugan, K.ᵇ, Samidoss, C. M., Panneerselvam, C., Higuchi, A., Roni, M., Suresh, U., ... & Rajaganesh, R. (2015). Seaweed-synthesized silver nanoparticles: an eco-friendly tool in the fight against Plasmodium falciparum and its vector Anopheles stephensi?. Parasitology research, 114(11), 4087-4097.

- Namvar, F., Azizi, S., Ahmad, M. B., Shameli, K., Mohamad, R., Mahdavi, M., & Tahir, P. M. (2015). Green synthesis and characterization of gold nanoparticles using the marine macroalgae Sargassum muticum. Research on Chemical Intermediates, 41(8), 5723-5730.

- Neupane, M. P., Lee, S. J., Park, I. S., Lee, M. H., Bae, T. S., Kuboki, Y., ... & Watari, F. (2011). Synthesis of gelatin-capped gold nanoparticles with variable gelatin concentration. Journal of Nanoparticle Research, 13(2), 491-498.

- Patil, M. P., & Kim, G. D. (2018). Marine microorganisms for synthesis of metallic nanoparticles and their biomedical applications. Colloids and Surfaces B: Biointerfaces, 172, 487-495.

- Pishbin, F., Mourino, V., Gilchrist, J. B., McComb, D. W., Kreppel, S., Salih, V., ... & Boccaccini, A. R. (2013). Single-step electrochemical deposition of antimicrobial orthopaedic coatings based on a bioactive glass/chitosan/nano-silver composite system. Acta biomaterialia, 9(7), 7469-7479.

- Pokharkar, V., Dhar, S., Bhumkar, D., Mali, V., Bodhankar, S., & Prasad, B. L. V. (2009). Acute and subacute toxicity studies of chitosan reduced gold nanoparticles: a novel carrier for therapeutic agents. Journal of biomedical nanotechnology, 5(3), 233-239.

- Ponnuchamy, K., & Jacob, J. A. (2016). Metal nanoparticles from marine seaweeds–a review. Nanotechnology Reviews, 5(6), 589-600.

- Potara, M., Baia, M., Farcau, C., & Astilean, S. (2012). Chitosan-coated anisotropic silver nanoparticles as a SERS substrate for single-molecule detection. Nanotechnology, 23(5), 055501.

- Prasad, T. N., Kambala, V. S. R., & Naidu, R. (2013). Phyconanotechnology: synthesis of silver nanoparticles using brown marine algae Cystophora moniliformis and their characterisation. Journal of applied phycology, 25(1), 177-182.

- Premlatha, T. S., & Kothai, S.  (2017) Potential Wound Management by Herb Incorporated Collagen-copper Oxide Nanocomposite. Journal of Chemistry and Chemical Sciences, Vol.7(9), 732-737

- Raja, S. B., Suriya, J., Sekar, V., & Rajasekaran, R. (2012). Biomimetic of silver nanoparticles by Ulva lactuca seaweed and evaluation of its antibacterial activity. International Journal of Pharmacy and Pharmaceutical Science, 4(3), 139-143.

- Rajathi, F. A. A., Parthiban, C., Kumar, V. G., & Anantharaman, P. (2012). Biosynthesis of antibacterial gold nanoparticles using brown alga, Stoechospermum marginatum (kützing). Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 99, 166-173.

- Rajesh, S., Raja, D. P., Rathi, J. M., & Sahayaraj, K. (2012). Biosynthesis of silver nanoparticles using Ulva fasciata (Delile) ethyl acetate extract and its activity against Xanthomonas campestris pv. malvacearum. Journal of Biopesticides, 5, 119.

- Rajeshkumar, S., Malarkodi, C., Gnanajobitha, G., Paulkumar, K., Vanaja, M., Kannan, C., & Annadurai, G. (2013). Seaweed-mediated synthesis of gold nanoparticles using Turbinaria conoides and its characterization. Journal of Nanostructure in Chemistry, 3(1), 44.

- Ramakrishna, M., Babu, D. R., Gengan, R. M., Chandra, S., & Rao, G. N. (2016). Green synthesis of gold nanoparticles using marine algae and evaluation of their catalytic activity. Journal of Nanostructure in Chemistry, 6(1), 1-13.

- Regiel-Futyra, A., Kus-Liśkiewicz, M., Sebastian, V., Irusta, S., Arruebo, M., Stochel, G., & Kyzioł, A. (2015). Development of noncytotoxic chitosan–gold nanocomposites as efficient antibacterial materials. ACS applied materials & interfaces, 7(2), 1087-1099.

- Reicha, F. M., Sarhan, A., Abdel-Hamid, M. I., & El-Sherbiny, I. M. (2012). Preparation of silver nanoparticles in the presence of chitosan by electrochemical method. Carbohydrate polymers, 89(1), 236-244.

- Roni, M., Murugan, K., Panneerselvam, C., Subramaniam, J., Nicoletti, M., Madhiyazhagan, P., ... & Canale, A. (2015). Characterization and biotoxicity of Hypnea musciformis-synthesized silver nanoparticles as potential eco-friendly control tool against Aedes aegypti and Plutella xylostella. Ecotoxicology and Environmental Safety, 121, 31-38.

- Saifuddin, N., Nian, C. Y., Zhan, L. W., & Ning, K. X. (2011). Chitosan-silver nanoparticles composite as point-of-use drinking water filtration system for household to remove pesticides in water. Asian Journal of Biochemistry, 6(2), 142-159.

- Saravanan, S., Nethala, S., Pattnaik, S., Tripathi, A., Moorthi, A., & Selvamurugan, N. (2011). Preparation, characterization and antimicrobial activity of a bio-composite scaffold containing chitosan/nano-hydroxyapatite/nano-silver for bone tissue engineering. International journal of biological macromolecules, 49(2), 188-193.

- Selvam, G. G., & Sivakumar, K. (2015). Phycosynthesis of silver nanoparticles and photocatalytic degradation of methyl orange dye using silver (Ag) nanoparticles synthesized from Hypnea musciformis (Wulfen) JV Lamouroux. Applied Nanoscience, 5(5), 617-622.

- Shameli, K., Ahmad, M. B., Yunus, W. M. Z. W., Rustaiyan, A., Ibrahim, N. A., Zargar, M., & Abdollahi, Y. (2010). Green synthesis of silver/montmorillonite/chitosan bionanocomposites using the UV irradiation method and evaluation of antibacterial activity. International journal of nanomedicine, 5, 875.

- Shiny, P. J., Mukherjee, A., & Chandrasekaran, N. (2013). Marine algae mediated synthesis of the silver nanoparticles and its antibacterial efficiency. Int. J. Pharm. Pharm. Sci, 5, 239-241.

- Shiny, P. J., Mukherjee, A., & Chandrasekaran, N. (2014). Haemocompatibility assessment of synthesised platinum nanoparticles and its implication in biology. Bioprocess and biosystems engineering, 37(6), 991-997.

- Sikorski, Z. E., Scott, D. N., Buisson, D. H., & Love, R. M. (1984). The role of collagen in the quality and processing of fish. Critical Reviews in Food Science & Nutrition, 20(4), 301-343.

- Singh, M., Kalaivani, R., Manikandan, S., Sangeetha, N., & Kumaraguru, A. K. (2013). Facile green synthesis of variable metallic gold nanoparticle using Padina gymnospora, a brown marine macroalga. Applied Nanoscience, 3(2), 145-151.

- Solomon, M. M., Gerengi, H., Kaya, T., & Umoren, S. A. (2017). Performance evaluation of a chitosan/silver nanoparticles composite on St37 steel corrosion in a 15% HCl solution. ACS Sustainable Chemistry & Engineering, 5(1), 809-820.

- Sugunan, A., Thanachayanont, C., Dutta, J., & Hilborn, J. G. (2005). Heavy-metal ion sensors using chitosan-capped gold nanoparticles. Science and Technology of Advanced Materials, 6(3-4), 335.

- Sun, C., Qu, R., Chen, H., Ji, C., Wang, C., Sun, Y., & Wang, B. (2008). Degradation behavior of chitosan chains in the ‘green’ synthesis of gold nanoparticles. Carbohydrate research, 343(15), 2595-2599.

- Suriya, J., Raja, S. B., Sekar, V., & Rajasekaran, R. (2012). Biosynthesis of silver nanoparticles and its antibacterial activity using seaweed Urospora sp. African Journal of Biotechnology, 11(58), 12192-12198.

- Thangaraju, N., Venkatalakshmi, R. P., Chinnasamy, A., & Kannaiyan, P. (2012). Synthesis of silver nanoparticles and the antibacterial and anticancer activities of the crude extract of Sargassum polycystum C. Agardh. Nano Biomed Eng, 4(2), 89-94.

- Torabfam, M., & Jafarizadeh-Malmiri, H. (2018). Microwave-enhanced silver nanoparticle synthesis using chitosan biopolymer: optimization of the process conditions and evaluation of their characteristics. Green Processing and Synthesis, 7(6), 530-537.

- Tran, H. V., Dai Tran, L., Ba, C. T., Vu, H. D., Nguyen, T. N., Pham, D. G., & Nguyen, P. X. (2010). Synthesis, characterization, antibacterial and antiproliferative activities of monodisperse chitosan-based silver nanoparticles. Colloids and Surfaces A: Physicochemical and Engineering Aspects, 360(1-3), 32-40.

- Unser, S., Holcomb, S., Cary, R., & Sagle, L. (2017). Collagen-gold nanoparticle conjugates for versatile biosensing. Sensors, 17(2), 378.

- van den Bosch, E., & Gielens, C. (2003). Gelatin degradation at elevated temperature. International journal of biological macromolecules, 32(3-5), 129-138.

- Vijayan, S. R., Santhiyagu, P., Singamuthu, M., Kumari Ahila, N., Jayaraman, R., & Ethiraj, K. (2014). Synthesis and characterization of silver and gold nanoparticles using aqueous extract of seaweed, Turbinaria conoides, and their antimicrofouling activity. The Scientific World Journal, 2014.

- Vivek, M., Kumar, P. S., Steffi, S., & Sudha, S. (2011). Biogenic silver nanoparticles by Gelidiella acerosa extract and their antifungal effects. Avicenna Journal of Medical Biotechnology, 3(3), 143.

- Wang, B. L., Liu, X. S., Ji, Y., Ren, K. F., & Ji, J. (2012). Fast and long-acting antibacterial properties of chitosan-Ag/polyvinylpyrrolidone nanocomposite films. Carbohydrate polymers, 90(1), 8-15.

- Wang, L. S., Wang, C. Y., Yang, C. H., Hsieh, C. L., Chen, S. Y., Shen, C. Y., ... & Huang, K. S. (2015). Synthesis and anti-fungal effect of silver nanoparticles–chitosan composite particles. International journal of nanomedicine, 10, 2685.

- Wang, L. S., Wang, C. Y., Yang, C. H., Hsieh, C. L., Chen, S. Y., Shen, C. Y., ... & Huang, K. S. (2015). Synthesis and anti-fungal effect of silver nanoparticles–chitosan composite particles. International journal of nanomedicine, 10, 2685.

- Wang, Y. C., & Gunasekaran, S. (2012). Spectroscopic and microscopic investigation of gold nanoparticle nucleation and growth mechanisms using gelatin as a stabilizer. Journal of Nanoparticle Research, 14(10), 1200.

- Wei, D., Sun, W., Qian, W., Ye, Y., & Ma, X. (2009). The synthesis of chitosan-based silver nanoparticles and their antibacterial activity. Carbohydrate research, 344(17), 2375-2382.

- Wei, G., Wang, L., Sun, L., Song, Y., Sun, Y., Guo, C., & Li, Z. (2007). Type I collagen-mediated synthesis and assembly of UV-photoreduced gold nanoparticles and their application in surface-enhanced Raman scattering. The Journal of Physical Chemistry C, 111(5), 1976-1982.

- Xu, X., & Zhou, M. (2008). Antimicrobial gelatin nanofibers containing silver nanoparticles. Fibers and polymers, 9(6), 685-690.

- Yoksan, R., & Chirachanchai, S. (2009). Silver nanoparticles dispersing in chitosan solution: preparation by γ-ray irradiation and their antimicrobial activities. Materials Chemistry and Physics, 115(1), 296-302.

- Yoksan, R., & Chirachanchai, S. (2010). Silver nanoparticle-loaded chitosan–starch based films: Fabrication and evaluation of tensile, barrier and antimicrobial properties. Materials Science and Engineering: C, 30(6), 891-897.

- Yousefzadi, M., Rahimi, Z., & Ghafori, V. (2014). The green synthesis, characterization and antimicrobial activities of silver nanoparticles synthesized from green alga Enteromorpha flexuosa (wulfen) J. Agardh. Materials Letters, 137, 1-4.

- Zain, N. M., Stapley, A. G. F., & Shama, G. (2014). Green synthesis of silver and copper nanoparticles using ascorbic acid and chitosan for antimicrobial applications. Carbohydrate polymers, 112, 195-202.

- Zhao, L., Wang, Y., Li, Z., Deng, Y., Zhao, X., & Xia, Y. (2019). Facile synthesis of chitosan-gold nanocomposite and its application for exclusively sensitive detection of Ag+ ions. Carbohydrate polymers, 226, 115290.