A care study on synthesis of 1,2,3-Triazole derivatives by means of Nanoparticles as a Reusable Heterogeneous Catalyst

D. Raghavendra,a S. Manasa Reddy,b G. B. Dharma Rao,a,*

aDepartment of Chemistry, Siddhartha Institute of Technology & Sciences, Hyderabad-500088, Telangana, India.

bDepartment of Chemistry, Kommuri Pratap Reddy Institute of Technology, Hyderabad-500088, Telangana, India.

Email: *gbdharmarao@gmail.com

Abstract: In recent years, nanotechnology is an emerging trend for the synthesis of medicinally significant and biologically dynamic derivatives as a heterogeneous catalyst because it’s simple and effortless work-up procedure. On the other hand, 1,2,3-triazole derivatives belongs to N-heterocyclic compounds and exhibit enormous biological activities as medicinal important. In this current chapter, the examination on importance and role of nanotechnology in preparation of 1,2,3-triazole analogues has been discussed and it make helpful for synthetic chemists or research scholar’s for the advanced developments in nanotechnology.

Keywords: 1,2,3-Triazoles; Nanoparticles; Heterogeneous catalyst; Medicinal chemistry; N-Heterocyclic compounds.

INTRODUCTION:

Heterocyclic molecules and its derivatives are important class of organic compounds having one or more heteroatoms, such as nitrogen, oxygen, sulfur, or a combination of two or more heteroatoms, along with at least one carbon atom, within their cyclic structure.[1] Heterocyclic derivatives form the principal and mainly diverse group of organic derivatives, holding immense chemical, industrial[2] and biomedical[3] importance. Additionally, these compounds serve as crucial scaffolds for a extensive variety of biologically active natural and synthetic derivatives [4], pharmaceutical drugs [5] and agrochemicals.[6] Nowadays, academic and industrial chemists have revealed the curiosity in special types of nitrogen holding moieties, known as azahetrocyclic systems. Among the accessible N-heterocycles, azoles have become a considerable field of study owing to their exclusive structural properties.

Triazole is a heterocyclic compound containing five membered ring structure composed of 3 nitrogen and 2 carbon atoms. There are two isomers of triazole i.e., 1,2,3 triazole and 1,2,4 triazole as represented in Figure-1.

Figure-1: Isomeric forms of Triazoles

The remarkable stability of the triazole nucleus primarily arises from its structural properties, particularly emphasizing the role of aromaticity and resonance. This aromaticity is a result of the formation of an aromatic sextet, achieved by the donation of one π electron from each atom connected by double bonds, combined with the contribution of two electrons from a nitrogen atom [7]. The resonance stabilization further enhances the stability of the triazole nucleus, as evidenced by its ability to exist in various tautomeric forms. This unique combination of aromaticity and resonance plays a pivotal role in conferring the intriguing characteristics and fascinating properties of triazoles. (Figure 2a & 2b)

Figure 2: a) Tautomeric structures of 1,2,3-Triazole, b) Tautomeric structures of 1,2,4-Triazole.

1,2,3-Triazoles play a crucial role as pharmacophores, intermingle with biological receptors with elevated similarity owing to their unique characteristics. Their dipole nature, hydrogen bonding ability, stiffness, and solubility make them attractive in drug design. As a result, 1,2,3-triazole motifs are integral components of various drugs used in clinical therapy.[8]

Nano-chemistry is an emergent research field owing to their exclusive properties.[9,10] The progress in nanotechnology has led to an escalating the requirement for multifunctional materials. Extremely ordered nanomaterials function as outstanding catalysts due to their elevated surface area and surface functionalities. Therefore, synthesis of nanomaterials has paying attention immense deal of research awareness in the current years. The convention of nano-materials such as heterogeneous catalyst has expanded considerable responsibility in organic synthesis owing to straightforward work-up process, environmentally benevolent nature, recyclability, low expenditure and effortlessness of isolation.[11]

In essence, the pivotal role of heterocycles, notably 1,2,3-triazoles, spans from their structural attributes to diverse applications. They serve as vital pharmacophores in drug design, while also excelling as effective fungicides in agriculture. In the current chapter, we have highlighted the importance of 1,2,3-triazole chemistry synthesis using nano-particles as a heterogeneous catalyst and their enduring importance in advancing scientific and practical domains.

CHEMISTRY OF 1,2,3-TRIAZOLE SYNTNESIS USING NANOTECHNOLOGY :

Mitali Chetia et al.[12] addressed the regioselective synthesis of 1,2,3-triazole derivatives by means of copper nanoparticles bearing heterogeneous nanocellulose as reusable catalyst. To synthesize the Cu NPs bearing nanocellulose, first the suspension of nanocellulose is treated with CuSO4.H2O followed by the drop wise addition of hydrazine hydrate. The synthesized Cu NPs bearing nanocellulose are examined with FT-IR, XRD, TEM, SEM-EDX and it was found that the average size of the particle to be 6-7 nm. The scope of the synthesized Cu NPs bearing nanocellulose was studied for the synthesis of 1,4-disubstituted-1H-1,2,3-triazole as a recyclable heterogeneous catalyst using azide derivatives with acetylene analogues in glycerol as shown in Scheme-1 via 1,3-dipolar Huisgen cycloaddition reaction and found 68-99% yields. The reusability of synthesized catalyst was studied for the same reaction capable of five sets devoid of any significance loss of activity.

Scheme-1: CuNP-NC catalysed cycloaddition reaction of azides and alkynes.

Hashem Sharghi et al.[13] discussed the three component coupling reaction of sodium azide, terminal alkynes and alkyl/benzyl halides for the green synthesis of 1,2,3-triazole analogues employing with copper NPs on charcoal as heterogeneous catalyst in water as a environmental friendly solvent. The catalyst was synthesized by using CuI and active carbon in ethanol and it was observed that the 9.97% copper content in it. The synthesized catalyst was experienced by using XRD, SEM, AFM, FR-IR, ICP and the size of the Cu-NPs on activated carbon was observed to be 283.3 nm. The application of the Cu-NPs on activated carbon was studied in the preparation of 1,2,3-triazole derivatives using catalytalic amount of Cu/C for the coupling reaction between sodium azide, terminal alkynes and alkyl/benzyl halides and found 91-69% yield as described in Scheme-2. The reusability of Cu/C was experiential for the same coupling reaction equal to ten cycles without any importance failure of activity.

Scheme-2: Synthesis of substituted 1,2,3-triazole using Cu/C as heterogeneous catalyst.

Sharghi, H. et al.[14] reported the region-selective synthesis of three constituent coupling reaction of sodium azide, terminal alkynes and wide range of epoxides for the synthesis of β-hydroxy 1,4-disubstituted 1,2,3-triazole derivatives using recyclable heterogeneous catalyst of 1,4-dihydroxyanthraquinone-copper(II) aminopropyl silica gel nanoparticles [Aq2Cu(II)-APSiO2]. The synthesis of novel 1,4-dihydroxyanthraquinone-copper(II) nanoparticle catalyst was addressed in three steps. In first step (4-hydroxy-9,10-dioxo-9,10-dihydroanthracen-1-yloxy)-acetic acid ethyl ester was synthesized using 1,4-dihydroxyanthraquinone, ethyl 2-bromoacetate and t-BuOK. In second step (4-hydroxy-9,10-dioxo-9,10-dihydroanthracen-1-yloxy)-acetic acid ethyl ester was treated with aminopropyl silica gel (APSiO2) to obtained the AQ-APSiO2 heterogeneous ligand followed by the reaction with Cu(OAc)2.H2O in methanol to achieved the target nanoparticles as described in Scheme-3. On the other hand it was totally characterized by ICP, XRD, AFM, SEM, FT-IR and TG analysis for nitrogen adsorption.

Scheme-3: Synthesis of title nanoparticles AQ2Cu(II)-APSiO2.

The scope of the novel catalyst was employed in the synthesis of β-hydroxy 1,4-disubstituted 1,2,3-triazole derivatives in 81-97% yield as shown in Scheme-4. The reusability of the novel heterogeneous catalyst was tested for ten times and found without loss of any catalytic activity.

Scheme-4: Synthesis of 1,4-disubstituted β-hydroxy 1,2,3-triazoles.

Moghaddam F. M. et al.[15] addressed the production of 1,5-disubstituted 1,2,3-trizole derivatives by means of cobalt-copper ferrite nanoparticles (CoCuFe2O4) at room temperature via [3+2] Huisgen cycloaddition reaction. The CoCuFe2O4 nanoparticles were synthesized by using co-precipitation procedure.[16] On the other hand the synthesized CoCuFe2O4 nanoparticles were examined by FT-IR, TEM, EDS, AAS, VSM, SEM and XPS. The metal of Co and Cu present in synthesized CoCuFe2O4 nanoparticles was found to be 5.2 wt% and 10 wt% respectively using AAS technique and moreover the size of the CoCuFe2O4 nanoparticles was observed as 30 nm by applying Scherrer equation using XRD physical technique. To observe the extent of the CoCuFe2O4 nanoparticles, the catalytic amount of the synthesized NPs were employed in Huisgen [3+2] cycloaddition reaction with reactants of terminal alkyene derivatives, alkyl/aryl halides and sodium azide as made known in Scheme-5 with excellent quantitative yields of 76-99%.

Scheme-5: CoCuFe2O4 nanoparticles catalysed [3+2] cycloaddotion reaction.

Anvari, M. et al.[17] illustrated the extremely one-pot synthesis of well-organized 1,2,3-triazole analogues in water as a environmentally benign solvent using novel copper nanoparticles doped in wrinkled fibrous nanosilica (Cu@KCC-1-NH-CS2) as a reusable heterogeneous catalyst. The novel Cu@KCC-1-NH-CS2 was prepared in two step procedure. The primary step expresses the process of KCC-1-NH-CS2 and the second step explains the synthesis of Cu@KCC-1-NH-CS2 by the reaction between the copper(ΙΙ) sulfate solution and KCC-1-NH-CS2 as depicted in Scheme-6. On the other hand, the novel catalyst was fully characterized by physicochemical techniques like FT-IR, SEM, TEM, EDX and it exhibit the 133 m2g-1 as high surface area was calculated by BET equation might be cause the outstanding catalytic performance.

Scheme-6: Preparation of Cu@KCC-1-NH-CS2 heterogeneous catalyst.

The scope of the Cu@KCC-1-NH-CS2 was employed in the synthesis of 1,4-disubstituted 1,2,3-triazole derivatives  using various aryl halides or several aryl azides, terminal alkyene analogues along with sodium azide produces the tremendous yields 92-100% as expressed in Scheme-7. Moreover, the authors studies the reusability of Cu@KCC-1-NH-CS2 nanocatalyst up to five cycles with low lose in its catalytic activity.

Scheme-7: Synthesis of 1,2,3-triazole derivatives using Cu@KCC-1-NH-CS2.

Tamilselvan Abiraman et al.[18] addressed  the straight forward preparation of substituted 1,2,3-triazole analogues by means of Sub 1 nm Poly(acrylic acid)-Capped Copper Nanoparticles [PAACC NPs] as a catalyst via Click chemistry under ultrasound irradiation using alkyl azide analogues and terminal alkyene substrates as depicted in Scheme-8. The synthesis of novel PAACC NPs was carried out as follows,  initially the mixture of copper nitrate trihydrate and poly(acrylic acid) was irradiate under ultrasound followed by the drop wise addition of NaOH to maintain the pH at 9 added and the colour of resulting solution is dark blue. To the above solution add L-ascorbic acid solution and subsequent ultrasound irradiation then the color of the solution turns from blue to yellow consequentially by the production of Cu NPs. The reaction was sustained for an additional 30 min, cooled and dried at room temperature to obtain the Cu NPs. It was observed that the Cu% present on poly(acrylic acid) was 33 as expressed in Scheme-9. The synthesized NPs be fully experienced by XPS, DRS UV-visible, FESEM, PL and HRTEM analytical spectroscopic methods. Furthermore, PAACC NPs exhibit the orange fluorescence at 560 nm peak range.

Scheme-8: PAACC employed synthesis of Triazole derivatives.

Scheme-9: Synthesis of PAACC NPs under ultrasound irradiation.

Ebadi Amin et al.[19] illustrated the straight forward preparation of substituted 1,2,3-triazole analogues using Fe3O4@SiO2/EP.EN.EG.Cu magnetic nanostructured core-shell as heterogeneous catalyst under mild circumstances via cycloaddition of 1,3-dipolar procedure. The preparation of the novel Fe3O4@SiO2/EP.EN.EG.Cu magnetic nanostructured core-shell as depicted in Scheme-10. On the other hand the synthesized catalyst was characterized by using physiochemical techniques and it was observed that the 100 nm is the average size of the nanospheres. To observe the scope of the result, the synthesis of 1,2,3-triazoles compounds was assessed through the reaction of various epoxides, alkyl or benzyl halides with phenylacetylene, azide of  sodium and found outstanding 85-98% yields as addressed in Scheme-11. Moreover, the authors played a more concentration on reusability of catalyst up to seven times with small reduce of catalytic activity.

Scheme-10: Preparation of Fe3O4@SiO2/EP.EN.EG.Cu nanocatalyst.

Scheme-11: Synthesis of 1,2,3-triazole analogues using magnetic Fe3O4@SiO2/EP.EN.EG.Cu nanocatalyst.

Noor Salam et al. described the straight forward one-pot synthesis of 1,2,3-triazole derivatives using recyclable graphene-γ-Fe2O3 magnetic nano-composite materials via [3+2] cycloaddition reaction as prescribed in Scheme-12.[20] Graphene-γ-Fe2O3 magnetic nano-composite materials was prepared by the reaction of graphene oxide in KOH solution with silica coated γ-Fe2O3 followed by the addition of hydrazine solution as depicted in Scheme-13. The extent of the novel synthesized graphene nano-composite catalyst was observed in the synthesis of substitiuted 1,2,3-triazole derivatives using benzyl bromide, phenyl acetylene and azide of sodium in water as a environment friendly solvent and found 70-93% yields.

Scheme-13: Preparation of graphene-γ-Fe2O3 nano-composite.

Scheme-12: Synthesis of 1,2,3-triazole derivatives using graphene-γ-Fe2O3 nano-composite.

Fe3O4 NPs were synthesized by using FeCl3.6H2O and FeCl4.4H2O via co-precipitation method followed by the Stober process for coating on Fe3O4 NPs with silica shell to obtain the Fe3O4@SiO2. The reaction of 3-chloropropyltrimethoxysilane with synthesized Fe3O4@SiO2 followed by the reaction with hydrazine hydrate to obtained the intermediate. Isatoic anhydride is added to the above intermediate to replace the hydrazine. Finally the Cu(II) was loaded by the reaction of copper (II) acetate to obtained the Cu(II)MNPs.

CONCLUSІON:

In summary, 1,2,3-triazole derivatives have employing a extraordinary manifestation for the motivation that of theіr adjustable understanding іn the medіcіnal chemіstry. During this chapter, we have communicated a preparation of 1,2,3-triazole analogues using variety of nanoparticles as reusable heterogeneous catalyst. Thіs chapter can substantiate to be extremely helpful for synthetic chemists or research scholar’s in the progression of new procedures for the enormous synthesіs of medicinally energetic new 1,2,3-triazole analogues and large-scale production of bіologіcally actіve novel 1,2,3-triazole analogues using novel nanoparticles.

CONFLICT OF INTEREST:

The authors have officially approved to incorporate their work as a chapter within the book entitled “Futuristic Trends in Chemical, Material Sciences & Nanotechnology”.

LIST OF ABBREVIATIONS:

ICP: Inductively Coupled Plasma

XRD: X-Ray Diffraction

AFM: Atomic Force Microscopy

SEM: Scanning Electron Microscopy

FT-IR: Fourier transform infrared

TG: Thermo gravimetry

TEM: Transmission electron microscopy

EDS: Energy-dispersive X-ray spectroscopy

AAS: Atomic absorption spectroscopy

VSM: Value stream mapping

XPS: X-ray photoelectron spectroscopy

N2-BET: Nitrogen Brunauer-Emmett-Teller

DRS UV-Visible: Diffuse reflectance spectroscopy Ultraviolet-Visible

FE-SEM: Field emission scanning electron microscopy

HR-TEM: High-resolution transmission electron microscopy

ACKNOWLEGDEMENT:

D. Raghavendra and G. B. Dharma Rao state their heartfelt thankfulness to the Principal and KPRIT management, Hyderabad, Іndіa and S. Manasa Reddy express her unique gratitude to the management of SITS, Hyderabad for providing the facilities to wrіte and recommend thіs chapter for the publication.

REFERENCES:

[1] P. Arora, V. Arora, H. S. Lamba, and D. Wadhwa, ‘Importance Of Heterocyclic Chemistry: A Review’, IJPSR, vol. 3, no. 9, pp. 2947–2954, 2012, [Online]. Available: www.ijpsr.com

[2]	M. A. P. Martins, C. P. Frizzo, D. N. Moreira, N. Zanatta, and H. G. Bonacorso, ‘Ionic liquids in heterocyclic synthesis’, Chemical Reviews, vol. 108, no. 6. pp. 2015–2050, Jun. 2008. doi: 10.1021/cr078399y.

[3]	L. L. Fershtat and E. S. Zhilin, ‘Recent advances in the synthesis and biomedical applications of heterocyclic no-donors’, Molecules, vol. 26, no. 18. MDPI, Sep. 01, 2021. doi: 10.3390/molecules26185705.

[4]	M. S. Saini, A. Kumar, J. Dwivedi, and R. Singh, ‘A Review: Biological Significances Of Heterocyclic Compounds’. Int. J. Pharm. Sci. Res., 2013, 4, 66-77.

[5]	M. M. Heravi and V. Zadsirjan, ‘Prescribed drugs containing nitrogen heterocycles: an overview’, RSC Advances, vol. 10, no. 72. Royal Society of Chemistry, pp. 44247–44311, Nov. 23, 2020. doi: 10.1039/d0ra09198g.

[6]	G. Giacomelli, A. Porcheddu, and L. De Luca, ‘[1,3,5]-Triazine: A Versatile Heterocycle in Current Applications of Organic Chemistry’, 2004.

[7]	M. M. Matin et al., ‘Triazoles and Their Derivatives: Chemistry, Synthesis, and Therapeutic Applications’, Frontiers in Molecular Biosciences, vol. 9. Frontiers Media S.A., Apr. 25, 2022. doi: 10.3389/fmolb.2022.864286.

# [8]. O. Gupta, T. Pradhan, Gita Chawla,“An updated review on diverse range of biological activities of 1,2,4-triazole derivatives: Insight into structure activity relationship”, J. Molecular Structure, 2023, 1274, 134487

# [9] Y. N. Xia, P. D. Yang, Y. G. Sun , Y. Y. Wu, B.Mayers, B. Gates, Y. D. Yin, F. Kin, H. Q.Yan, Adv. Mater. 15 (2003) 353.

# [10]  Z. L. Wang, X. Y. Kong, Y. Ding, P. X. Gao, W. L. Hughes, R. Yang, Y. Zhang, Adv. Funct. Mater. 14, 943 (2004).

# [11] G. B. Dharma Rao, S. Nagakalyan, G. K. Prasad, “Solvent-free synthesis of polyhydroquinoline derivatives employing mesoporous vanadium ion doped titania nanoparticles as a robust heterogeneous catalyst via the Hantzsch reaction”, RSC Adv. 2017,  7, 3611-3616.

# [12] Chetia, M.; Ali, A. A.; Bordoloi, A.; Sarma, D. “Facile route for the regioselective synthesis of 1,4-disubstituted 1,2,3-triazole using copper nanoparticles supported on nanocellulose as recyclable heterogeneous catalyst”. J. Chem. Sci. 2017, 129, 1211–1217.

# [13] Sharghi, H.; Khalifeh, R.; Doroodmand, M. M. “Copper Nanoparticles on Charcoal for Multicomponent Catalytic Synthesis of 1,2,3-Triazole Derivatives from Benzyl Halides or Alkyl Halides, Terminal Alkynes and Sodium Azide in Water as a “Green” Solvent “. Adv. Synth. Catal. 2009, 351, 207 – 218.

# [14] Sharghi, H.; Khoshnood, A.; Doroodmand, M. M.; Khalifeh, R. “1,4-Dihydroxyanthraquinone-copper(II) nanoparticles immobilized on silica gel: a highly efficient, copper scavenger and recyclable heterogeneous nanocatalyst for a click approach to the three-component synthesis of 1,2,3-triazole derivatives in water”. J. Iran Chem. Soc., 2012, 9, 231–250.

# [15] Moghaddam, F. M.; Pourkaveh, R.; Ahangarpour, M. “Cobalt-Copper Ferrite Nanoparticles Catalyzed Click Reaction at Room-Temperature: Green Access to 1,2,3-Triazole Derivatives”. ChemistrySelect 2018, 1, 1–9.

# [16] Zaharieva, K. L.; Milenova, K. I.; Rives, V.; Trujillano, R.; CherkezovaZheleva, Z. P.; Eliyas, A. E.; Tsvetkov, M. P.; Kunev, B. N.; Mitov, I. G.; Bulg. Chem. Commun. 2015, 47, 105–111.

# [17] Anvari, M.; Shadjou, N. “Copper nanoparticles doped in wrinkled fbrous nanosilica as an efcient catalyst for the synthesis of 1,4-disubstituted 1,2,3-triazole in aqueous solution”. Monatshefte für Chemie - Chemical Monthly, 2021, 152, 1277-1284.

# [18] Abiraman, T.; Rajavelu, K.; Rajakumar, P.; Balasubramanian S. “Sub 1 nm Poly(acrylic acid)-Capped Copper Nanoparticles for the Synthesis of 1,2,3-Triazole Compounds”. ACS Omega, 2020, 5, 7815-7822.

# [19] Ebadi, A.; Rajabzadeh, M.; Khalifeh, R. Fe3O4@SiO2/EP.EN.EG.Cu as a Highly Efficient and Recoverable Catalytic System for Synthesis of 1,4-Disubstituted 1,2,3-Triazole Derivatives via the Click Reaction. ChemistrySelect, 2019, 4, 7211 –7218.

# [20] Salam, N.; Sinha, A.; Mondal, P.; Roy, A. S.; Jana, N. R.; Islam, Sk. M. “Efficient and reusable graphene-c-Fe2O3 magnetic nano-composite for selective oxidation and one-pot synthesis of 1,2,3-triazole using a green solvent”. RSC Advance, 2013, 39, 18087-18098.