Adsorption of heavymetal Fe by birdbone particles from the Industry effluent

S.M. Jearmeen*

*Departmentof Advanced Zoology and Biotechnology,GuruNanakCollege, 
Chennai – 600 042, Tamil Nadu, India.

Abstract

Birdbone particles have the ability to remove heavymetal Fe from the titanium industry effluent. 
The binding of Fe by birdbone was found to be mainly influenced by pH, birdbone absorbed the highest quantity of iron at pH 7 and when 5g of adsorbent was leaving only 278.27+0.93 ppm of Fe in the raw untreated effluent. The metal uptake by birdbone particles was maximum at room temperature and 254.71+0.84 ppm of Fe was left in the effluent after adsorption and if temperature increases, Fe uptake get increased.

Keywords:Adsorption, Fe uptake, birdbone powder, titanium industry effluent.

Introduction

Heavy metals released into the environment by industrial activities, become a serious threat to the environment ( Kuppusamy et al., 2004).

Bonechar is an adsorbent, mainly produced by the carbonization of bone (Choy and Mckay, 2005; Smiciklas et al., 2008). It is used in the sugar refining industry to remove the color from sugar solutions (Gary et al., 2007; Ofomaja and Ho, 2007).

Bonechar as an adsorbent is effective and can easily remove heavy metals from large amounts of industrial wastewater at a low cost. Poorly crystallized apatite, such as bone carapatite, might represent a low-cost and readily available phosphate source that could be used as an adsorbent. Bonechar, a mixed adsorbent containing around10 percent carbon and 90 percent calcium phosphate, is mainly produed by the carbonization of bone (Choy and Mckay,2005; Smiciklas et al., 2008)

The main objective of the study was to find out how efficient the birdbone powder was in adsorbing heavy metal Fe.

Materials and Methods

Preparation of bone char

Bird bones collected from common fowls and the boneswere crushed into small fragments in a mechanical crusher and  dried at 60oC in a hot air oven for 24h, then powdered in an electric blender and sifted inan 80 mesh sieve 
(<180 m)

. 
The powdered adsorbents were mixed with the two different types of effluents (rawand treated effluent) in 5 different concentrations(1, 2, 3, 4, and 5 mg/l). The medium was separately maintained at six different pH levels (0.5, 2, 4, 7, 8, and 9). 
Thoroughly mixed with the toxicant solution and the mixture was agitated once in 2 h. The treatment was run for a period of more than 60 days. The Fe content of the effluents was estimated after 60 days of interaction with the bird bone powder.The difference between the initial and final levels indicated the quantity adsorbed.

For assessing the effect of temperature, the reaction mixtures were allowed to interact in a 250ml Erhlen – Meyer flask. The flasks were placed inside separate incubators maintained at 42, 32, and 28oC. The experiments were continued for more than 60 daysthe quantities of Fe wereanalyzed in the raw and untreated effluent.

Estimation of heavy metal (Fe)

An Atomic Absorption Spectrophotometer (ELICO) model with Air-C2H2 flame type, with an average fuel flow rate between 0.8 –4.0 L min-1 and a support gas flow rate between 13.5.-17.5 L min-1 was used for sample analysis. The single-element hollow cathode lamps for respective metals were used. Calibration curves for various elements obtained from these standards were of a first-order reaction. The Fe analysis sample was aspirated with an Automatic sampler's help. The samples were finally injected into an AAS flame and the reading was directly measured.

Result and Discussion

Bird bone powder adsorbed the highest quantity of iron at pH 7 and when 5g of the absorbent was used leaving behind only 278.27+ 0.93ppm of Fe in the raw treated effluent. At pH 
0.5, adsorption of Fe was minimum, and at 5g bird bone powder concentration, the Fe concentration of the raw treated effluent was 291.15 + 0.84 ppm was left in the medium (Table 1).

Thechromium adsorbed at 5g of bird bone at 28oC was highest at 245.30 + 0.92 and the lowest adsorptionat 1g at 42oC was 275.94 + 0.98 of iron left behind in the raw untreated effluent (Table 2).

The pH influenced the adsorption of Fe by bird bone powder. At acidic pH levels, the quantity of Fe absorbed is much less compared to neutral and alkaline pH levels. Thus pH plays a vital role in determining the quantity of Fe adsorbed from the medium by bird bone powder. The pH seemed to modify the adsorption potential of bird bone powder and the pH should be maintained at 7.0 to achieve maximum adsorption of Fe.

The temperature was another significant factor determining the adsorption of heavy metals. At higher temperatures (42oC) adsorption was much less compared to lower temperatures (28oC).

Namasivayam and Senthilkumar (1998) reported thata certain amount of adsorbents does not increase in the adsorption reaching equilibrium.Chojnacka (2005) and Chenet al. (2006) pointed out that cow bone charcoal(when the size of the ion becomes small),as a microporous adsorbent, metals penetratethese pores.

Ibrahim et al. (2012) studied the capacity of chromium and lead and used cow bone charcoal at 30oC. Olaniyi et al. (2012)studied that, cow bone has the effect of temperature for the removal of metals.

Below pH 5.1, hydrogen ions are likely to compete with iron, and at pH values above 8, iron might precipitate. Maximum adsorption using cow bone charcoal was observed atabout pH 5.1 and the adsorption is highly pH dependent.Rana et al. (2009) observed the removal efficiency of chitosan for iron was found nearly 58 percent.

Differentfunctional groups such as carboxyl, hydroxyl, and amide are responsible for the biosorption of metal ions andpotential sites for adsorption and the uptake of metal and their accessibility and affinity between the adsorption site and metal(Han et al. (2007) and Jain et al. (2009).

The temperature was another significant factor determining the adsorption of heavy metals. At higher temperatures (42oC), even 1 g of adsorbent has a high percent of Fe from the titanium industry effluent at the ideal pH of 7.

Moreno et al. (2010) stated that iron removal increasedfrom 0.01 g to 0.02 g cow bone charcoal dosages. At 30oC, cow bone reported the effect of temperature on the removal of metals using an immobilized sorbent obtained from poultry waste(Olaniyi et al. (2012)).

Table 1

Fe Adsorption from Titanium industry effluent(treated) at different  pH

| S. No | Amount (in g)of bird bone powder | Fe in the effluent (ppm) control | Fe (ppm) in effluent |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | pH |  |  |  |  |  |
|  |  |  | 0.5 | 2 | 4 | 7 | 8 | 9 |
| 1 | 1 | 452.25 ± 1.02 | 317.00 ± 0.85 | 312.39 ± 0.54 | 309.55 ± 0.51 | 297.69 ±0.60 (-34.00) | 298.49 ±0.60 | 302.00 ±0.72 |
| 2 | 2 |  | 314.62 ± 0.65 | 307.20 ± 0.84 | 303.37 ± 0.47 | 291.16 ±0.93 (-35.44) | 296.17 ±0.76 | 298.15 ±0.99 |
| 3 | 3 |  | 311.65 ± 0.85 | 302.23 ± 0.65 | 296.85 ± 0.76 | 285.88± 0.73 (-36.60) | 291.41 ±0.98 | 293.68 ±0.92 |
| 4 | 4 |  | 311.10 ± 0.78 | 308.49 ± 0.71 | 306.98 ± 0.65 | 284.23± 0.85 (-36.96) | 286.27 ±0.81 | 289.52 ±0.93 |
| 5 | 5 |  | 291.15 ± 0.84 | 290.31 ± 0.79 | 286.27 + 0.81 | 278.27±0.93 (-38.28) | 281.23 ±0.80 | 283.18 + 0.86 |

Note: Percent decrease in Fe concentration in parentheses

Deviations significant at P <0.05 (t-test)

Table2

FeAbsorption from Titanium industry effluent(raw untreated) at pH 7 at different temperatures

| S.No | Amount (in g) of bird bone powder | Fe in effluent (ppm)control | Fe (ppm) in effluent |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Temperature (° C) |  |  |
|  |  |  | 28 | 32 | 42 |
| 1 | 1 |  | 263.45 ± 0.96 (-41.54) | 274.26 + 0.73 | 275.94 + 0.98 |
| 2 | 2 |  | 258.91 +0.70 (-42.53) | 269.31 ± 0.87 | 271.55 ±0.85 |
| 3 | 3 | 452.25 ± 1.02 | 253.82 +0.65 (-43.65) | 265.17 + 0.80 | 267.53 ± 0.89 |
| 4 | 4 |  | 246.39 + 0.57 (-45.29) | 259.91 + 0.72 | 261.63 ±0.92 |
| 5 | 5 |  | 245.30 + 0.92 (-45.53) | 254.71 +0.84 | 257.77 ±0.75 |

Note: Percent decrease in Fe concentration in parentheses

Deviations significant at P <0.05 (t-test)

References

- Chen, S.B., Zhu, Y.C., Ma, Y.B. and Mekay, G. 2006. Effect of bone char application on Pb contaminated soil. Environ. Pollut.,39: 433 – 439

- Chojnacka, K. 2005. Biosorption of Cr(III) ions by egg shells. Journal of Hazardous Materials,121: 167-173.

- Gary, U.K., Kaur, M.P., Garg, V.K. and Sud, D. 2007. Removal of hexavalent chromium from aqueous solution by agricultural waste biomass. 
J Hazard Mater,40: 60-68.

- Han, X., Wong, Y.S., Wong, M.H. and Tama, N.G. 2007. Biosorption and bioreduction of Cr(vi) by a microalgal isolate. J Hazard Mater,146: 
65-72.

- Ibrahim, O., Sunday, M. and Odoh, R. 2012. Adsorption Study of Cr (VI) and Pb (1) from aqueous solution using animal charcoal derived from cow bone. Pelagia Research Library,3 (3): 648-657.

- Jain, M., Garg, V.K. and Kadirvelu, K. 2009. Chromium (VI) removal from aqueous system using H.annuus stem waste. J.Hazard Mater,162 : 
365-372.

- Kana, M.S., Halim, M.A., Safiullah, S. and Mollah, M.M. 2009. Removal of heavy metal from contaminated water by biopolymer crab shell chitosan. Journal of Applied Sciences,9 (5): 2762-2769.

- Kuppusamy, V., Jegan, J.R., Palanivelu, K. and Velan, M. 2004. Copper removal from aqueous solution by the marine green alga. Electronic J. Biotechnol., 7(11): 61-71.

- Moreno, J.C., Gomez, R. and Giraldo, L. 2010. Removal of Mn, Fe, Ni, and Cu ions from wastewater using cow bone charcoal. Materials,3: 452-466.

- Namasivayam, C. and Senthikumar, S. 1998. Removal of arsenic (v) from aqueous solution using industrial solid waste, adsorption rates, and equilibrium studies. Eng. Chem. Res.,37(12): 4816-4822.

- Ofomaja, A.E., Ho, Y.S. 2007. Effect of pH on cadmium biosorption by coconut meal. Hazard Mater,139: 356-362.

- Olaniyi, I., Moses, S. and Odoh, R. 2012. Adsorption study of Cr (VI) and Pb (11) from aqueous solution using animal charcoal derived from cow bone. Pelagia Research Library,3(3): 648-657.

- Rana, M.S., Halim, M.A., Safiullah, S. and Mollah, M.M. 2009. Removal of heavy metal from contaminated water by biopolymer crab shell chitosan. Journal of Applied Sciences,9 (5): 2762-2769.

- Shim, J.J Park, S.J. and Rju, S.K. 2001. Effect of modificatíon with HNO3 and NaOH by pitch-based activated carbon fibers. Carbon,39: 11

- Smiciklas, I., Dimovic, S., Sljivic, M. and Plecas, I. 2008. The batch study of adsorption by bone char. J. Eviron. Sci. Health,43: 210-217