A Comprehensive Study on Synthesis of Silver Nanoparticles

Dr. Chandra Mohan Kurmarayuni,1* P. Krishna Kumari2, Dr.B.Srikanth3,

Dr. Swarnalatha Kurapati4, Dr. J. Venkateswara Rao4

1. Department of Chemistry, Acharya Nagarjuna University, Guntur, AP, India.

2. Department of Chemistry, Mrs. A.V.N College, Visakhapatnam, AP, India.

3. Lecturer in Chemistry, Govt. Degree College, Cumbum, Prakasam Dist. AP, India

4. Department of Chemistry, Ch. S.D. St. Theresa's College for Women, Eluru, AP, India.

5. S& H department, MVR College of Engineering & Technology, Paritala, Vijayawada, AP India.

Abstract:

For a healthy imminent of nanotechnology, a green synthetic strategy should be adopted for nanoparticle synthesis by using eco-friendly and renewable molecules to get rid of hazards arising out of the use of chemical reducing agents and organic solvents. Colloid based nanotechnological process has been developed to control the size, shape, consistency, and functionality.

1. Introduction

The point sized nanoparticles consist of their exceptional properties when compared to their parent particles. These novel properties depend on the size, shape and morphology of the different Nanoparticles. By utilizing the nanotechnology, we are capable to find the different structures of matter having different dimensions of 1-100 nanometers (i.e. 1000 times smaller than the diameter of the human hair). Nanotechnology is very much helpful to handle the matter on an atomic, molecular, and supramolecular scale. All these properties let this smallest version of particles to interact with the plants, microbes, animals, etc (Husen 2014, Husen A and Siddiqi KS 2014, Siddiqi KS and Husen A 2016, Husen A and Siddiqi KS 2016, Siddiqi KS et al., 2016, Siddiqi KS and Husen A 2017 & Siddiqi and Husen 2016). The nanoparticles of the silver (Ag), also named as Silver nanoparticles (Ag NPs), have shown spectacular bactericidal properties against a immense of micro-organisms (Wei L et al., 2015, Lara HH et al., 2011, Siddiqi KS and Husen A 2016 & Siddiqi KS and Husen A 2016). These particles are prepared either to test their morphology or their perspective characteristics. Few of the authors have tried with the chemical method (Zaheer Z and Rafiuddin 2012) yet they just ended up/mistaken it with the green synthesis. The authors haven't indeed done it with care but got it to happen accidentally. The reason why the Ag NPs are used widely aginst the growth of microorganisms or resist it to a higher extent, therefore Ag NPs are used extensively in electronics, catalysis, and drugs because of these properties (Husen 2014, Wei L et al., 2015, Lara HH et al., 2011&Lokina S et al., 2014). In a process named biogenic synthesis, the Ag NPs contain the use of bacteria, yeast, plant extracts, and fungi/yeast (Husen 2014, Siddiqi KS and Husen A 2016, Siddiqi KS and Husen A.2016, Lokina S et al., 2014, Saifuddin N et al., 2009&Shahverdi AR et al., 2007).

Moreover, the synthesis of gold and silver nanoparticles entails of using of the number of parts of plants such as flowers, fruits (Husen 2014) (excluding enzymes), etc. Synthetic methodology includes the morphology, size and the stability of the nanoparticles, while the strength of the reducing agent and temperature (Husen 2014, Siddiqi KS and Husen A 2017, Siddiqi KS and Husen A 2016 & Siddiqi KS and Husen A 2016) along with the nature/concentration of the solvent also affects it wholly.

Ag NPs make their significant position in all those nanoparticles yet found due to their remarkable features of acting as an antimicrobial agent in the solid state too. This characteristic of Ag NPs was recognized much before but it was used only in the oriental medicine, coins. On average, more than 300 tons of Ag NPs are produced each year and is thereafter used in food products, Nano medical imaging, and bio sensing, (Ahamed M et al., 2010 & Chen X and Schluesener HJ 2008) etc.

Due to the changing environmental conditions, raise in pollution, all those other factors, there is a sure growth in the various bacterial and viral strains that are resistant to multi-drugs. To overcome those resistive microbial infections scientists are applying their efforts in the directions such as to find out the special drugs for the treatment. Apart from the nanoparticles, various metal salts have been also found useful in stopping the growth of many different bacteria. Out of all such metal series, silver and Ag NPs are used as antimicrobial agents from age-old times hence these have gained a bulging place in that certain category of metals (Jones SA et al., 2004&Silver S and Phung LT 1996).

Human beneficial uses of silver salts consists of helping stop the growth of a vast range of bacteria while it is preferably used in cuts, burns or wounds for this property (Catauro M et al., 2004, Crabtree JH et al., 2003 & Das et al., 2011), after research, have reported the exemplary action of small-sized Ag NPs against the growth of certain bacteria.

Ag NPs extracted from the silk sericin (SS) that is a water-soluble protein gained by the silkworms when kept at pH=11 owns hydrophilic proteins having highly polar groups, for example- hydroxyl, amino functional groups, etc. These molecules having the functional groups as explained above, it works as reducing agents for AgNO3 so as to erupt the elemental silver. The hydroxyl groups of silk sericin (SS) are meant to create the complex with the silver ions while preventing their precipitation suggested by the Aramwit et al., 2014, Vigneshwaran N et al., 2006, 2012, 2018 & Shin Y et al., 2009.

The nanoparticles of Ag when in elemental state may get segregated due to the large molecules available in the solvent, yet, the complexes would not form because of the neutral state of both the solvent and the particles. The action of Silk Siricin capped or SS-Capped silver nanoparticles defending the gram-positive and gram-negative bacteria has been recorded or checked over the screen. Those both sorts of microorganisms have MIC falling between 0.001 and 0.008 mm (S. aureus, B. subtilis, P. aeruginosa, A. baumannii and E. coli).

Despite the wide range of  Literature  exists on fabrication or the characterization of the Silver nanoparticles, the author mainly few reporting are available regarding the green synthesis, mechanism of action and the biocidal properties (Wei L et al., 2015, Lara HH et al., 2011, Lokina S et al., 2014, Ahamed M et al., 2010 & Aramwit P et al., 2014). In this chapter, in detail about the biosynthesis of the silver nanoparticles from the herbal extracts, bacteria or fungi, it is our attempt to write about it. Aside to the extraction process, the antimicrobial and the way out of their other actions has been crafted here. This should let everyone know about the comprehensive details about the mechanism and the actions of the Ag NPs against the various microorganisms.

2. Synthesis of Silver nanoparticles (Ag NPs)

Synthesis of Ag NPs are basically two types of methods used to generate or synthesize these NPs (Figure 1). First one is known as- "bottom-up" method and the second one being the "top-down" method (Husen 2014). In the first method, the material is made atom by atom or molecule by molecule (cluster by cluster) from the bottom. The top-down method evolves the cutting or slicing of the top layers of the materials such as to break down the existing materials into the smallest nanoparticles. It is always good to go with the bottom-up method as it is efficient and produces excellent quality nanoparticles. There are catalysts working onto the whole process in the bottom-up method so as to produce the nanoparticles atom-by-atom or molecule-by-molecule/cluster-by-cluster. Thermal decomposition, mechanical grinding, etching, cutting/sputtering are some of the ways that are used in the top-down method so as to breakdown the material into nanoparticles. The nanoparticles such formed through the top-down method have inconsistent or irregular surface and shapes, these defects affect the physical features and chemistry of the nanoparticles. These were the two different ways to the synthesis of Ag NPs but under these categories are three different sorts of methodologies that are utilized. These methodologies include the chemical (Zhang Q et al., 2011, Roldan MV et al., 2013, Sotiriou GA and Pratsinis SE 2010 & Sotiriou GA et al., 2011), physical (Abou El-Nour KMM et al., 2010, Tien DC et al., 2008 & Asanithi P et al., 2012) and biological (Husen 2014 et al., 2016) ways those all either work in bottom-up strategies or top-down strategies. Further dividing the chemical method of synthesis, the sub-divisions are a chemical reduction, electrochemical, irradiation-assisted chemical, and pyrolysis (Zhang W et al., 2007).

Figure 1:  Approach for Metallic Nano Particles Synthesis

To synthesize the Ag NPs in aqueous phase needs to be reducing agents, stabilizing agent or capping agent and the metal precursor. Ascorbic acid, alcohol, borohydride, sodium citrate and hydrazine compounds, these are some of the most often used reducing agents to assist in the formation of Ag NPs in solution. Sotiriou and Pratsinis (Sotiriou GA and Pratsinis SE 2010), they have displayed flame aerosol technology under which the Ag NPs supported on nanostructured SiO2 were obtained. This technology enables the best control over the silver materials and size and is therefore really useful in the best synthesis of Ag-NPs. Another method named flame spray pyrolysis (Sotiriou GA et al., 2011) helps to get the silver/silica nanoparticles consisting of relatively narrow size distribution (Asanithi P et al., 2012). On the other side, the physical methods of synthesis do not require using highly (Asanithi P et al., 2012) reactive chemicals yet the processing time are also faster as compared to other ways. Some of the physical Method for synthesis of Ag-NPs arc-discharge (Tien DC et al., 2008), physical vapour condensation (Abou El-Nour KMM et al., 2010), energy ball milling method (Wright R et al.,2011) and direct current magnetron sputtering (Asanithi P et al., 2012).

Pros of physical methods are that the Ag NPs such formed have narrow size distribution when compared with the chemical methods while the cons of this method are that it consumes a lot of energy and the chemical process utilizes almost half the energy. Biological method is the exemplary way to generate or process the Ag NPs from the herbs and other natural extracts. This procedure involves the working of microorganisms on those herbal extracts so as to form the silver nanoparticles.

This method is an admirable protocol rather than both chemical and physical methods due to its cost effective, a large-scale production and is eco-friendly manner. This methods includes the biosynthesis of metal and metal oxide nanoparticles through using some biological agents such as bacteria, fungi, yeast, plant and algal extracts has therefore gained popularity in the caste of nanotechnology (Husen 2014, Husen A and Siddiqi KS 2014, Siddiqi KS and Husen A 2016, Siddiqi KS, Rahman A et al., 2016, Siddiqi KS and Husen A 2017, Siddiqi KS and Husen A 2016 & Siddiqi KS and Husen A 2016).

Carbohydrates, fats, proteins, nucleic acids, pigments and many other types of secondary metabolites those are present in the herbal extracts or plants take an action as reducing agents and thereafter produces the nanoparticles by reacting to metallic salts. This is completely a biological process and it does not evolve the production or output of any harmful agents while the whole process is eco-friendly. There are biomolecules such as enzymes, proteins, and bio-surfactants that are also present in microorganisms, these biomolecules act as reducing agents.

Some of the previous synthetic approaches from various plant extracts for production of silver nanoparticles with their optimization was depicted in Table 1. Bio-surfactants and or stabilizing agents used during synthesis of silver nanoparticles from various bacterial stains was illustrated in Table 2.

Table 1: Plant-mediated synthesis of silver nanoparticles

| Plant | Plant part | Size and shape | Phyto constituents responsible for reduction of silver nitrate | Key references |
| --- | --- | --- | --- | --- |
| Aloe vera | Leaf gel (removed skin) | 5–50 nm; octahedron | Flavanones and terpenoids | Logaranjan et al., 2016 |
|  | Leaf | 70.7–192.02 nm; spherical (size varies through change of times and temperatures) | Lignin, hemicellulose and pectins | Tippayawat et al., 2016 |
|  | Leaf | Size varies in accordance to different parameters; spherical | Flavonoids, terpenoids and phenols | Moosa et al., 2015 |
| Mangifera indica | Seed | 14 nm; spherical and hexagonal | Phenolic compounds, gallotannins and tannin | Sreekanth et al., 2015 |
| Erigeron bonariensis | Leaf | 13 nm; spherical | Flavonoids, steroids, glycosides, triterpenes, sugars and caffeoyl derivatives | Kumar et al., 2016 |
| Myristicafragrans | Bark and seeds | Spherical, polydispersed | Secondary metabolites | Jelin et al., 2015 |
| Momordica charantia | Leaf | 11 nm; spherical | Momorcharins, momordenol, momordicius, momordin, momordolo, charantin, charine, cucuritanes, cucurbitns, goyaglycosides and goyasaponins | Ajitha et al., 2015 |
| Carambola | Fruit | 16, 13, 12 nm at pH 4, 7, 10 respectively | Polysaccharides, polyols and ascorbic acid | Chowdhury et al., 2015 |
| Rubusglaucus | Fruit | 12–50 nm; spherical | Phenolic groups and flavonoids | Kumar et al., 2017 |
| Prunus serotina | Fruit | 20–80 nm (blue LED) 40–100 nm (white solar); spherical | Chlorogenic acid, catechin, proanthocyanidin, and flavonol glycosides | Kumar et al., 2016 |
| Piper nigrum | Seeds | 10–60 nm; rod shaped | Polysaccharides, amino acids, alkaloids, proteins and vitamins | Mohapatra et al., 2015 |
| Nigella sativa | Leaf | 15 nm; spherical | Alkaloids, ascorbic acid, saponins, glycosides, amino acids, flavonoids like catechin, apigenin, gallic acid and benzoates especially vanillic acid | Amooaghaie et al., 2015 |
| Calotropis gigantean | Flower | 10–50 nm; spherical | – | Pavani et al., 2015 |
| Acmella oleracea | Flower | 2–20 nm; spherical | – | Raj et al., 2016 |
| Piper betle | Leaf | 48–83 nm; spherical | Allylic benzenes, phenolic, amino acids, proteins, alcoholic compounds, terpenes and terpenoids | Kamachandran et al., 2015 |
| Morinda tinctoria | Leaf | 80–100 nm; spherical and rod | Ascorbic acid, niacin, copper and iron | Vennila and Prabha |
| Trigonellafoenum-graecum | Seeds | 20–50 nm; spherical | Saponins and alkaloids | Meena and Chouhan, 2015 |
| Picrasmaquassioides | Bark | 17.5–66.5 nm; spherical | – | Sreekanth et al., 2015 |
| Rosa ‘Andeli’ | Petals | 0.5–1.4 nm; spherical | Polyphenols and flavonoids | Suarez-Cerda et al., 2015 |
| Salvadorapersica | Stem | 1–6 nm; spherical | Phenolic compounds | Tahir et al., 2015 |
| Artemisia absinthium |  | 5–20 nm; round shaped | Phenolic compounds and flavonoids | Ali et al., 2016 |
| Chelidoniummajus | Aerial parts | DLS-253.3 nm; spherical, quasi-spherical | Flavonoids and alkaloids | Barbinta-Patrascu et al., 2016 |
| Calotropis procera | Flower | 35 nm; face centered cubic | Tannins, triterpenes, flavonoids, steroids, alkaloids and cardiac glycosides | Babu and Prabu, 2011 |
| Sterculiaacuminata | Fruit | ~ 10 nm; spherical | Ascorbic acid, gallic acid, phenolic compounds, pyrogallol, methyl gallate and polyphenolic compounds | Bogireddy et al., 2016 |
| Terminalia cuneata | Bark | 25–50 nm; spherical | Tannins, saponins, triterpenoids, flavonoids, gallic acid, ellagic acid and phytosterols | Edison et al., 2016 |
| Cirsium japonicum | Plant | 4–8 nm; spherical | Saponins, proteins and flavonoids | Khan et al., 2016 |
| Isatistinctoria | Plant | 10–15 nm; spherical | Saponins and flavonoids | Ahmad et al., 2016 |
| Aegle marmelos | Fruit | 22.5 nm; spherical, hexagonal, roughly circular | Phytosterols, flavonoids, alkaloids, triterpenoids and amino acids | Velmurugan et al., 2016 |
| Trachyspermumammi | Seeds | 36 nm; cubic | Fatty acids, proteins, flavonoids and alkaloids | Chouhan and Meena 2015 |
| Eucalyptus globulus | Leaf | 1.9–4.3 and 5–25 nm with and without microwave treatment respectively | Alkaloids and flavonoids | Ali et al., 2015 |
| Cydonia oblonga | Seeds | 38 nm; face-centered cubic | Flavonones, terpenoids, proteins and amino acids | Zia et al., 2016 |
| Hydrocotyleasiatica | Leaf | 21 nm; spherical | Flavonoids and glycosides | Devi et al., 2016 |
| Lantana camara | Leaf | 33.8 nm; spherical | Flavonoids, proteins, saccharides secondary metabolites like alkaloids, tannins, saponins, carbohydrates, steroids and triterpenoids | Manjamadha and Muthukumar 2016 |
| Nyctanthes arbor-tristis | Seeds | 50–80 nm; spherical | Carbohydrates and phenolic compounds | Basu et al., 2016 |
| Pennyroyal sp. | Leaf | 19.14 ± 9.791 nm; spherical | – | Sedaghat et al., 2016 |
| Saracaindica | Leaf | 23 ± 2 nm; spherical | Flavonoids and steroids | Perugu et al., 2016 |
| Terminalia chebula | Fruit | 30 nm; distorted spherical | – | Edison et al., 2016 |
| Euphorbia amygdaloides | Plant | 7–20 nm; spherical | – | Cicek et al., 2015 |
| Pedalium murex | Leaf | 50 nm; spherical | Flavonoids, alkaloids, steroids, rosins, saponins and proteins | Anandalakshmi et al., 2016 |
| Chelidoniummajus | Root | 15.42 nm; spherical | – | Alishah et al., 2016 |
| Salacia chinensis | Powdered plant | 20–80 nm; spherical, rods, triangular, hexagonal | Flavonoids, saponins, proteins, carbohydrates and phenolics | Jadhav et al., 2015 |
| Tamarindusindica | Seed coat | ~ 12.73 nm | Flavonoids, tannin and saponins, | Ramamurthi et al., 2015 |
| Parkiaroxburghii | Leaf | 5–25 nm; poly dispersped, quasi-spherical | Proteins | Paul et al., 2016 |
| Aristolochiaindica | Leaf | 32–55 nm; spherical | – | Shanmugam et al., 2016 |
| Cerasus serrulate | Leaf | 10–50 nm; spherical | Alcohol and phenolic compounds and proteins | Karthik et al., 2016 |
| Matricariacamomilia | Flower | 8–35 nm; spherical | Terpenoids, flavones and polysaccharides | Parlinska-Wojtan et al., 2016 |
|  | Flower | ~ 5.5 nm; spherical | Phenolics, carbonyl and amines or alcohol groups | Ocsoy et al., 2017 |
|  | Fruits | ~ 15.4 nm; spherical | Phenolics, flavonoids, terpenoids and vitamins | Swamy et al., 2015 |
| Alpinia calcarata | Root | 5–15 nm; quasi-spherical | Proteins, flavonoids and polyphenols | Pugazhendhi et al., 2015 |
| Salvinia molesta | Leaf | 12.46 nm; spherical | Alkaloids, flavonoids, tannins, phenols, sugars and proteins | Verma et al., 2016 |
| Helicteresisora | Root | 16–95 nm; spherical | Steroids, terpenoids, alkaloids, carbohydrates and phenolic compounds | Bhakya et al., 2016 |
| Mukiamaderaspatana | Leaf | 158 nm; spherical | Phenolic compounds | Harshiny et al., 2015 |
| Ficusbenghalensisand Azadirachtaindica | Bark | 60 nm; spherical | Flavonoids, terpenoids and phenols | Nayak et al., 2015 |
| Azadirachtaindica | Leaf | 34 nm; spherical and irregular shape | Flavanoids and terpenoids | Ahmed et al., 2016 |
| Adathodavasica | Leaf | 10–50 nm; spherical | Alkaloids compounds | Latha et al., 2016 |
| Amaranthus gangeticus | Leaf | 11–15 nm; globular and polycrystalline | Amino acids | Kolya et al., 2015 |
| Phlomis | Leaf | 25 nm; spherical | Glycosides such as flavonoids, iridoids, diterpenoids, triterpenoids and other phenolic compounds | Allafchian et al., 2016 |
| Syzygiumalternifolium | Fruit | 4–48 nm; spherical | Phenols and primary amines of proteins | Yugandhar et al., 2015 |
| Afzeliaquanzensis | Bark | 10–80 nm; spherical | Proteins | Moyo et al., 2015 |
| Allamanda cathartica | Flower | 39 nm; spherical | (E,E)-geranyl linalool, n-pentacosane, 1,8-cineole and n-tricosane | Karunakaran et al., 2016 |
| Carica papaya | Peel | 10–30 nm; spherical | Vitamins (C, K, E), amino acids, carbohydrates, β-carotene, lycopene and polyphenols | Kokila et al., 2016 |
| Vitis vinifera | Leaf | 200 nm; spherical | Hydroxyl groups and phenolic compounds mainly myricetin, ellagic acid, kaempferol and gallic acid | El-Sherbiny et al., 2016 |
| Solanum indicum | Leaf | 10–50 nm; spherical | Phenolic compounds | Sengottaiyan et al., 2016 |
| Tectonagrandis | Leaf | 26–28 nm; spherical | Phenols | Devadiga et al., 2015 |
| Soymidafebrifuga | Leaf | 10–20 nm; spherical | Phenolic groups, amino acids, aliphatic and aromatic amines, amide-I and amide-II | Sowmyyan and Lakshmi 2015 |
| Cardiospermumhalicacabum | Leaf | SEM-less than 100 nm; spherical | Polyphenols and phenol | Sundararajan et al., 2015 |
| Ammanniabaccifera |  | 105–125 nm; spherical | Polyphenols, flavonoids and proteins | Jadhav et al., 2016 |
| Diospyros paniculate | Root | 17 nm (avg); spherical | Phenolics and proteins | Rao et al.,2016 |
| Simarouba glauca | Leaf | 33–50 nm; spherical | Amino groups and hydroxyl groups | Kanchana and Zantye 2016 |
| Origanummajorana and Citrus sinensis | Leaf | 40–70 nm; feather and 26–60 nm; spherical, cubical respectively | Proteins and phenolic compounds | Singh et al., 2016 |
| Salmaliamalabarica | Gum | 7 ± 2 nm; spherical | Carbonyl and hydroxyl group | Krishna et al., 2016 |
| Psidium guajava | Leaf | 10–90 nm; spherical | Leucocyanidin, flavonoids, tannins, saponins, carotenes, vitamin C, B6 and carbohydrates | Bose and Chatterjee 2016 |
| Allium cepa | Bulb | – | – | Balamanikandan et al., 2015 |
| Justicia glauca | Leaf | 10–20 nm; spherical | Phenolic compounds | Awad et al., 2015 |
| Skimmialaureola | Leaf | Irregular, spherical, hexagonal | Tritepenoids, skimmidiol and coumarins | Ahmed et al., 2015 |
| Andrographis echioides | Leaf | ~ 68.06 nm; cubic | Carbohydrates, tannins, saponins, flavonoids, alkaloids, quinones, glycosides, triterpenoids, phenols, steroids, phytosteroids and anthraquinones | Elangovan et al., 2015 |
| Putranjivaroxburghii | Leaf | 5.74 nm; spherical | Amino groups | Ali et al., 2015 |
| Ixora coccinea | Flower | 5–10 nm; spherical | Alkaloids, tannins, glycosides, flavonoids, saponins, terpenes and carbohydrates | Nalvolthula et al., 2015 |
| Emblica officinalis | Fruit | 10–70 nm; spherical | Alkaloids, phenolic compounds, amino acids and tannins | Ramesh et al., 2015 |
| Hibiscus rosa-sinensis | Petals | ~ 18.79 nm; spherical | Proteins | Nayak et al., 2015 |
| Bauhinia variegata | Leaf | 32 nm; spherical, triangular, truncated triangles, decahedral | Reducing sugar, saponins, anthraquinone, alkaloids and terpenoids | Govindarajan et al., 2016 |
| Pteridium aquilinum | Leaf | SEM-35–65 nm; spherical | Phenols, alkaloids, tannins, flavonoids, proteins, carbohydrates, saponins. glycosides, steroids and triterpenoids | Panneerselvam et al., 2015 |
| Aristolochiaindica | Leaf | 30–55 nm; spherical and cubical | Phenols | Murugan et al.. 2016 |
| Cassia roxburghii | Leaf | ~ 32 nm; spherical, triangular, truncated triangles, decahedral | – | Muthukumaran et al., 2014 |
| Anisomeles indica | Leaf | TEM-18–35 nm; SEM-50–100 nm; spherical | Alcohols, phenols and carboxylic group | Govindarajan et al., 2016 |
| Hybanthusenneaspermus | Plant | 16–26 nm; spherical, hexagonal, triangular | Proteins | Suman et al., 2016 |
| Amaranthus dubius | Leaf, stem, root | Stem: 30–35 nm; Root: 18–21 nm; Leaf: 18–21 nm | Polyphenol compounds and aldehydes | Sigamioney et al., 2016 |
| Ziziphusjujuba | Fruit | 25.75 nm; spherical | Alcohols and phenols | Sreekanth et al.,2016 |
| Chrysophyllumoliviforme | Leaf | 25 nm; flower | Flavonoids, saponins, catechic tannins, traces of anthraquinones, reducing sugars and phenolic compounds | Varghese et al., 2015 |
| Plumeria alba | Flowers | ~ 36.19 nm; spherical | Amino, carboxylic and sulfhydryls | Mata et al., 2015 |
| Impatiens balsamina | Flowers | 5–40 nm; spherical | Alkaloids, tannins, glycosides, flavonoids, saponins, terpenes and carbohydrates | Nalavothula et al., 2015 |
| Fraxinus excelsior | Leaf | 25–40 nm; spherical and polydisperse | Flavonoids, alkaloids, glycosides, terpenoids, phenolic compounds, amino acid residues and peptides of proteins | Parveen et al., 2016 |
| Pongamiapinnata | Leaf | AFM-15–35 nm; spherical | Alkaloids, glycosides, flavonoids, saponins, carbohydrates, tannins, phenolic compounds and fat | Priya et al., 2015 |
| Pongamiapinnata | Seed | 5–30 nm; spherical | Pongaflavanol, tunicatachalcone, pongamol, galactoside and glybanchalcone | Beg et al., 2017 |
| Areca catechu | Nut | 18.2 and 24.3 nm; spherical | Polyphenols | Rajan et al., 2015 |
| Ficustalboti | Leaf | 9–12 nm; spherical | Flavonoids, alkaloids, saponins, phenolic compounds, tannins, phytosterol and glycosides | Arunachalam et al., 2015 |
| Sidacordifolia | Leaf | 10–30 nm; spherical, prism | Alkaloids, quinazolines, cryptoleptins, phytosterols, flavonoids and saponins | Srinithya et al., 2016 |
| Clerodendrumphlomidis | Leaf | TEM 10–15 nm; SEM 23–42 nm; spherical | Phenolics, flavonoids, terpenoids and steroids | Sriranjani et al., 2016 |
| Theobroma cacao | Pod husk | 4–32 nm; face-centered cubic | Proteins and phenolic compounds | Lateef et al., 2016 |
| Ficuscarica | Fruit | 20–80 nm (thermal approach), 10–30 nm (ultra sonication approach); spherical | – | Kumar et al., 2016 |
| ParkiaspeciosaHassk | Pod | 20–50 nm; predominantly spherical | – | Fatimah 2016 |
| Boerhaaviadiffusa | Whole plants | 25 nm; spherical |  | Vijay Kumar et al., 2014 |
| Pelargonium endlicherianum | Roots | Different size; spherical | Gallic acid, apocynin and quercetin | Karatoprak et al., 2017 |
| Artocarpusheterophyllus | Seeds | 10.78 nm; irregular | Lectin—a single major protein | Jagtap and Bapat 2013 |
| Ceropegiathwaitesii | Leaf | 100 nm; spherical | Triterpenoids; and methoxy groups of protein | Muthukrishnan et al., 2015 |
| Alternanthera sessilis | Leaf | 30 nm; various shape | Alkaloid, tannins, ascorbic acid, carbohydrates and proteins | Niraimathi et al., 2013 |
| Dryopteris crassirhizoma | Rhizome | 5–60 nm; almost spherical | Alcohol, amines, alkanes, carboxylic acid and or ester | Lee et al.,2016 |
| Leptadenia reticulate | Leaf | 50–70 nm; crystalline, face centered and spherical | Phenolics, terpenoids, polysaccharides and flavones | Swamy et al., 2015 |
| Ipomoea batatas | Root | TEM 30–120 nm; AFM 50–200 nm; polygonal | Glycoalkaloids, mucin, dioscin, choline, polyphenols and anthocyanins | Wang et al.,2016 |
| Sambucus nigra | Fruit | 26 nm; spherical | Polyphenols | Moldovan et al., 2016 |
| Millettiapinnata | Flower | 16–38 nm; spherical | Multi-functional aromatic gropus | Rajakumar et al., 2017 |
| Coptischinensis | Plant extract | 15 nm; spherical | Polyphenols | Ahmad et al., 2017 |
| Lyciumbarbarum | Fruit | 3–15 nm; spherical | Tannias, flavanoids, ascorbic acid and alkaloids | Dong et al., 2017 |
| Embeliaribes | Seed | 20–30 nm; crystalline, uniform and spherical | Alkaloids, quinones, proteins, reducing sugars and saponins | Dhayalan et al., 2017 |
| Zizyphusxylopyrus | Bark | 60–70 nm; spherical | Reducing agents | Maria et al., 2015 |

- Table 2: Bio-surfactants and or stabilizing agents used during synthesis of silver nanoparticles from various bacterial stains

| Bacteria | Size and shape | Biosurfactants and or stabilizing agent | Key references |
| --- | --- | --- | --- |
| Pseudomonas aeruginosaBS-161R | 15.1 ± 5.8 nm; spherical | Rhamnolipids | Kumar et al., 2010 |
| Brevibacteriumcasei MSA19 | – | Biosurfactant | Kiran et al., 2010 |
| Bacillus cereus NK1 | 50–80 nm; spherical | URAK (a fibrinolytic enzyme) | Deepak et al., 2011 |
| Gluconacetobacterxylinum | 5–40 nm | Cellulose | Liu et al., 2012 |
| Streptomyces coelicolor | 28–50 nm; irregular | Actinorhodin pigment | Manikprabhu and Lingappa 2013 |
| Bacillus subtilis MSBN 17 | 60; spherical | Bioflocculant | Sathiyanarayanan et al., 2013 |
| Salmonella typhimurium | 3–11 nm | Flagellin | Gopinathan et al., 2013 |
| Bacillus athrophaeus | 5–30 nm; polydispersed | Spores | Hosseini-Abari et al., 2013 |
| Lactobacillus rhamnosus GG ATCC 53103 | 2–15 nm; spherical, triangular, rod-shaped and hexagonal | Exopolysaccharide | Kanmani and Lim 2013 |
| Nostoc commune | 15–54 nm; spherical | Extracellular polysaccharide/matrix | Morsy et al., 2014 |
| Pseudomonas aeruginosa | 1.13 nm; spherical | Biosurfactant | Farias et al., 2014 |
| Ochrobactrumrhizosphaerae | 10 nm; spherical | Glycolipoprotein | Gahlawat et al., 2016 |
| Gordoniaamicalis HS-11 | 5–25 nm; spherical | Glycolipid | Sowani et al., 2016 |
| Bacillus subtilis | – | Surfactin | Mendrek et al., 2017 |

Syed and co-workers (Syed et al., 2013), reported that the synthesis of Ag NPs from thermophilic fungus Humicola sp in  to the solution or aqueous phase at room temperature. In a test, Mycelia were suspended in 100 mL of 1 mm AgNO3 solution in an Erlenmeyer flask while the temperature was kept at 50 °C, then that mixture was left in a shaker for about 96 h at pH 9. The whole solution was then tested for any colour changes. As a result, the solution colour changed from yellow to brown that is due to the release of Ag nanoparticles (Ahmad A et al., 2003). This is a simple process to production of Ag NPs from the extracellular synthesis from Humicola sp. Thus, the nanoparticles such formed with uniformly spreadly and dispersed and spherical shape between 5 and 25 nm (Chwalibog A et al., 2010). The nanoparticles such formed are crystalline and have a face-centered cubic structure. IR spectrum of Ag NPs in the suspension showed peaks at 1644 and 1523 cm−1 assigned to amide I and amide II bands of protein relative to –C=O and N–H stretches. It was reported by Owaid et al., 2015). The biosynthesis of Ag NPs from those yellow exotic oysters mushroom, Pleurotus cornucopiae var. citrinopileatus happens eventually. The powdered dried basidiocarps were boiled in water and then the supernatant was freeze-dried, then the different concentrations of hot water extract of this lyophilized powder were mixed with 1 mm AgNO3 at 25 °C and incubated for 24 hours, 48 hours and 72 hours. At an absorption peak of 420 and 450 nm in UV–vis region, the solution has shown the change in colour from yellow to yellowish brown. This colour change reflects the availability of spherical silver nanoparticles. Also, the width of the absorption peak suggests the polydispersed nature of these nanoparticles (Sanghi R and Verma P2009). IR spectrum of Ag NPs has also shown absorption peaks at 3304, 2200, 2066, 1969, 1636, 1261, 1094 and 611 cm−1 for various groups. Despites the fact that authors have demonstrated the availability of polysaccharide and protein in the mushroom they have somewhere overlooked their extending frequencies in the IR range. In any case, the crest at 3304 has been doled out to υ (OH) of carboxylic corrosive and those at 2200 and 1969 cm−1 have been ascribed to unsaturated aldehydes. All those different crests underneath 1500 cm−1 are due to the unsaturated alkaloids. The high-goals transmission electron micrograph has proposed that the Ag NPs are spherical while having the normal size going somewhere in the range of 20 and 30 nm.

Al-Bahrani and co-workers (Al-Bahrani et al., 2017) have detailed about the biogenic combination of Ag NPs from tree shellfish mushroom named Pleurotus ostreatus. Dried fluid concentrate of mushroom (1– 6 mg/mL) and 1 mm AgNO3 were blended and then kept for about (6– 40) hrs. There is a visible change of colours from light yellow to dim earthy yellow demonstrating the availability of silver nanoparticles. The UV–vis range has also shown a sharp and expansive ingestion band at 420 nm. These materials that are such found in this way are polydispersed nanoparticles of 10– 40 nm with a normal size of 28 nm. Aspergillus flavus, A. fumigates, Fusarium oxysporum, Fusarium acuminatum, F. culmorum, F. solani, Metarhizium anisopliae, Phoma glomerate, Phytophthora infestans, Trichoderma viride, Verticillium sp., etc, these all have been utilized for additional and intracellular biosynthesis of Ag NPs (Siddiqi KS and Husen A2016, Duran N et al., 2005, Duran N et al., 2007, Vigneshwaran N et al., 2007, Bhainsa KC and DSouza SF 2006, Li G et al., 2012 and Ahmad A et al., 2003) and these nanoparticles are of different sizes and shapes.

3. Synthesis of Ag NPs from plants

Plant-related parts, for example, leaves, stems, blooms, roots, shoots, barks, seeds, and their metabolites have been found to be efficiently utilized for the proficient biosynthesis (Husen A and Siddiqi KS 2014, Husen A 2017) of nanoparticles. Beg et al., (2017) have revealed a green synthesis of Ag NPs from seed separated out of Pongamia pinnata. This arrangement of nanoparticles was affirmed by a retention max at 439 nm. Then the all-around scattered nanoparticles having a size of 16.4 nm had zeta potential equivalent to − 23.7 mV damages the security of the microbes. There's a study, association of Ag NPs with human serum egg whites was researched and it was indicated an unimportant change in α helics. Karatoprak et al., (2017) have announced there is a green synthesis of Ag NPs that is found from the therapeutic plant extract Pelargonium endlicherianum. The plant contains gallic corrosive, apocyanin and quercetin go about as diminishing operators to deliver silver nanoparticles. Phytomediated combination of circular Ag NPs from Sambucus nigra fruit extrate has been accounted for by Moldovan et al. (Moldovan B et al., 2016) XRD examination demonstrated them to be crystalline. The in vivo cancer prevention agent movement was explored against Wistar rodents which demonstrated promising action. It proposes that fictionalization of Ag NPs with common phytochemicals may shield the cell proteins from ROS generation.

Ag NPs have likewise been blended from fluid leaf separate of Artocapus altilis. They were respectably antimicrobial and antioxidant. Thalictrum foliolosum root remove intervened Ag NPs union has been affirmed based on the presence of a sharp top at 420 nm in UV–vis local of the range (Hazarika SN et al., 2016). The monodispersed circular nanoparticle of 15–30 nm had face focused cubic structure. Shape and size ward controlled amalgamation of Ag NPs from Aloe vera plant extracts and their antimicrobial productivity has been accounted for by Logaranjan K et al., 2016. The UV-Vis crest at 420 nm affirmed the development of silver nanoparticles. After microwave light of the example, Ag NPs of 5– 50 nm with octahedral geometry was gotten. About two to four-fold antibacterial actions of Ag NPs was watched contrasted with normally accessible anti-infection drugs. Biosynthesis of Ag NPs from the fluid concentrate of piper longum fruit extricate has been additionally accomplished (Reddy NJ et al., 2014). The nanoparticles were round fit as a fiddle with a normal molecule size of 46 nm dictated by SEM and dynamic light scattering (DLS) analyzer. The polyphenols present in the concentrate are accepted to go about as a stabilizer of silver nanoparticles. The natural product remove and the balanced out nanoparticles indicated cancer prevention agent properties in vitro. The nanoparticles were observed to be stronger against pathogenic microscopic organisms than the blossom separate of P. longum. Ag NPs have been created from leaf extricate of Ceropegia thwaitesii and development was affirmed from the assimilation of SPR at 430 nm. The nanoparticles of about 100 nm measurement were crystalline in nature (Muthukrishnan Set al., 2015). Plant remove of Ocimum tenuiflorum, Solanum tricobatum, Syzygium cumini, Centella asiatica, and Citrus sinensis have been utilized to incorporate Ag NPs of various sizes in colloidal structure.

The extent of all nanoparticles was observed to be 22– 65 nm. They were all steady and very much scattered in an arrangement. Niraimathi and collaborators (Niraimathi KL et al.,  2013) have revealed biosynthesis of Ag NPs from the watery concentrate of Alternanthera sessilis and demonstrated that the concentrate contains alkaloids, tannins, ascorbic corrosive, sugars and proteins which fill in as diminishing just as topping specialists. Biomolecules in the concentrate likewise went about as stabilizers for silver nanoparticles. Ag NPs from seed powder remove of Artocarpus heterophyllus have been integrated (Jagtap UB, Bapat BA.2013). The morphology and crystalline period of the nanoparticles were dictated by SEM, TEM and SAED, EDAX and IR spectroscopy. They were observed to be unpredictable fit as a fiddle. Thus, the available concentrate was found to have those amino acids, amides and these worked or acted as reducing agents for AgNO3 for finally producing the silver nanoparticles. The number of phenols, anthocyanins and benzoic corrosive were resolved in the berry squeezes and were in charge of the change of silver particles to Ag NPs (Puisoa Jet al., 2014). UV– Vis spectra showed an absorbance crest at 486 nm for lingonberry and 520 nm for cranberry containing silver nanoparticles. Since the two ingestion tops are diverse they can't be doled out just to Ag NPs yet additionally halfway to various amounts of the diminishing synthetic compounds present in the juices. Nonetheless, the spectra demonstrated the nearness of polydispersed silver nanoparticles. Puiso et al., (2014) have recommended that because of the illumination of water by UV beams, solid oxidants and reductants as photolysis items are framed. They diminish silver particles to Ag NPs or silver oxide. The photolysis items may deliver oxidant and reductant however it relies on the quantum of radiation and presentation time which may not be sufficient to create an adequate amount of redox synthetic compounds to lessen Ag+  Ag NPs or Ag2O. This theory is theoretically mistaken on the grounds that Ag2O can't be shaped as it requires an exceptionally solid oxidizing operator. Then again, AgNO3 itself is gradually diminished in water, yet within the sight of lessening operators, the response continues at a fast rate. The SPR is subject to the size, shape, and agglomeration of Ag NPs which is reflected from the UV–vis spectra. Mock JJ et al., (2002) have discovered diverse dispersed hues in hyperspectral tiny pictures which are principal because of the distinctive shape and size of silver nanoparticles in the colloidal arrangement. The blue, green, yellow and red hues have been ascribed to circular, pentagonal, round-triangle and triangle shapes, individually.

Zaheer and Rafiuddin (Zaheer Z and Rafiuddin 2012), both of them have detailed the union of Ag NPs utilizing oxalic corrosive as diminishing specialist and mixed up it as green amalgamation. Arrangement of nanoparticles was affirmed by an adjustment in the shade of the arrangement which demonstrated a retention top at 425 nm in the UV noticeable locale. It was additionally noticed that a dissipated silver film was framed on the mass of the holder that sparkles and reflects light which is normal for monodispersed (Henglein A1993 and Henglein A1993) circular Ag NPs. Since the extent of nanoparticles fluctuates somewhere in the range of 7 and 19 nm the silver film isn't uniform. It is unique in relation to the customary silver mirror because of unpredictable shape and size of the nanoparticle. All things considered little size nanoparticles can be acquired when AgNO3 is presented to a decreasing specialist for a more extended span of time (Bakshi MSet al., 2007). The energy and instrument proposed for the arrangement of Ag NPs by oxalic corrosive aren't persuading in light of the fact that oxalic (Zaheer Z and Rafiuddin 2012) corrosive for no situation can create CO2 unless it responds with any carbonate salt or warmed at a high temperature. The creators (Zaheer Z and Rafiuddin 2012) have proposed the following responses to demonstrate that the shade of Ag NPs in an arrangement is because of Ag42+ formation that ingests at 425 nm. The arrangement of Ag42+is exceedingly implausible regardless of whether the above response is actively quick. Likewise, the adjustment of Ag42+ is faulty. This speculation of Ag42+ formation is past creative energy and does not convey any trial proof in its help. The absorbance of Ag NPs in arrangement fluctuates somewhere in the range of 400 and 445 nm relying upon the idea of diminishing operator utilized for their manufacture. The SPR band in UV–vis range is because of electron swaying around the outside of nanoparticles. The decrease procedure is immediate and no further unearthly change happens after 60 min. Demonstrating the fruition of the redox process. Ag NPs are round, triangular, hexagonal and polydispersed at 70 °C. The EDAX and XRD spectra bolster one another.

The amalgamation of Ag NPs from the watery concentrate of Cleistanthus collinus and their portrayal by UV–vis, FTIR, SEM, TEM, and XRD has been accounted for by Kanipandian N et al., (2014). The crystalline Ag NPs of 20–40 nm indicated noteworthy free radical rummaging limit. Tippayawat P et al., (2016) have revealed a green and easy amalgamation of Ag NPs from Aloe-Vera plant remove. They were described by UV– vis, SEM, TEM, and XRD. Creation of Ag NPs was affirmed based on the presence of a sharp top at 420 nm in UV– vis district of the range. What's more, they have announced that the response time and temperature uniquely impact the manufacture of silver nanostructures. Ag NPs were circular fit as a fiddle and molecule estimate went from 70.70 ± 22 to 192.02 ± 53 nm. Their size changes with time and temperature of the response synthesis utilized amid creation.

Green synthesis of Ag NP by Boerhaavia diffusa plant extricate has been accounted for by Vijay Kumar et al. Vijay Kumar PPN et al., (2014) the concentrate went about as both the lessening just as topping operator. The colloidal arrangement of Ag NPs demonstrated ingestion greatest at 418 nm in the UV–Vis range. The XRD and TEM examinations uncovered a face-centered cubic structure with a normal molecule size of 25 nm. Ag NPs of 5– 60 nm have been integrated from Dryopteris crassirhizoma rhizome extricate in the nearness of daylight/LED in 30 min. XRD considers demonstrated face focused cubic structure of silver nanoparticles. Green combination of Ag NPs utilizing 1 mm watery AgNO3 and the leaf remove of Musa balbisiana (banana), Azadirachta indica and Ocimumte.

4. Cytotoxicity of Silver nanoparticles

The cytotoxicity refers to the toxic value of the nanoparticles while closely considering their other factors relatively affecting it. These factors are the size, shape, surface, and capping or coating agent, the major one is the pathogen against which it is being tested. The green method produces more toxic NPs whereas the non-green produces less toxic NPs when compared. There are some pathogens or microbes that are more prone to the nanomaterials, Ag NPs are such materials, and these consist of both the Ag ions as well as Ag-NPs. The Nanoparticles applications have toxic impacts on the environment (Brayner R 2008, Panda KKet al., 2011) and this is not hidden from the public. As the NPs are comparatively more toxic than the forming materials or the bulk material. The NPs work on the cellular and biomolecular levels (Jayasree Let al., 2006), even this toxic action has been tested to produce oxidative stress and severe lipid peroxidation on the fish brain tissues (Oberdorster E2004). It is believed that the reactive oxygen species (ROS) assists in the cytotoxicity of the nanoparticles, reduction in glutathione level and a simultaneous increase in ROS levels that further assists the toxicity. Kim S and Ryu DY (2013) have studied the working of silver nanoparticles on the animal cells; they have found the rise of oxidative stress, apoptosis and genotoxicity actively. The study is done with varying sizes of Ag NPs and various different topics, therefore, the accurate relation cannot be defined. Some researches (Hackenberg Set al., 2011) have also shown the reduced viability of Ag NPs at a dose of 10 µg/mL over 50 nm size in human mesenchymal cells, no toxicity is also seen in some people even at a higher dose (100 µg/mL) (Samberg ME et al., 2012). Aged Ag NPs are more toxic when kept in water for 6 months (Kittler Set al., 2010), this is reported by Hackenberg and co-workers and this has been related to the release of Ag ions (Beer Cet al., 2012). It is found that Ag works more effectively in some cases while the Ag ions are found more effective in many ways (Cronholm Pet al., 2013).

Vijay Kumar PPN et al., (2014) who collected or extracted the Ag NPs from B. diffusa plant extricates tried them against three fish bacterial pathogens. A new discovery came into existence and it was that Ag NPs were best against Flavobacterium branchiophilum. Ag NPs manufactured from P. longum fruit extricate showed cytotoxic impact against MCF-7 bosom malignant growth cell membrane with an IC50 of 67 μg/mL/24 h (Reddy NJ et al., 2014). They additionally displayed cancer prevention agent and antimicrobial impacts. Ag NPs were created by using P. endlicherianum plant separate, and have demonstrated that the inhibitory movement was expanded against gram positive and gram negative microscopic organisms when they were presented to Ag NPs at an exceptionally low portion of 7.81 to 6.25 ppm (Karatoprak GS et al., 2017). Latha Met al., (2016) have created Ag NPs from leaf remove of Adathoda vasica and contemplated their antimicrobial action against Vibrio parahaemolyticus in agar medium. The nanoparticles were observed against V. parahaemolyticus but were nontoxic to Artemia nauplii. V. parahaemolyticus is a common ocean bottom borne enteropathogen which is intently connected with mortality in Siberian tooth carps, milk fish (Austin B and Austin DA1999), abalone (Cai JP et al., 2007) and shrimps (Jayasree L et al., 2006). Vibrio infection in refined fish and shrimps causes vast scale mortality. Regularly, the entire populace perishes. Ag NPs have shown up as a convincing cure which spares shrimps from dying. Ag NPs from seed powder remove of A. heterophyllus  also shown antibacterial movement against gram-positive and gram-negative microorganisms.

Ag NPs manufactured from leaf remove of C. thwaitesii have indicated antibacterial competence against Salmonella typhi, Shigella flexneri and Klbsiella pneumonia. Niraimathi and associates (Niraimathi KL et al., 2013)  have manufactured Ag NPs from the watery concentrate of A. sessilis and demonstrated noteworthy antibacterial and cell reinforcement exercises. Ag NPs from Ocimum tenuiflorum, Solanum tricobatum, Syzygium cumini, Centellaasiatica, and Citrus sinensis have additionally indicated antibacterial action against S. aureus, P. aeruginosa, E. coli (Logeswari P et al., 2015), and K. pneumoniae. Noteworthy action of nanoparticles was watched against S. aureus and E.coli. Antimicrobial action of colloidal Ag NPs was observed to be higher than the plant extract (Lee et al., 2016, Nayak D et al., 2015). Blended Ag NPs from Dryopteris crassirhizoma and observed against B. cereus and P. aeruginosa.

Therefore, Ag NPs that are generated from leaf concentrate of banana, neem and dark tulsi were likewise dynamic against E.coli and Bacillus sp (Banerjee P et al., 2014). Hazarika SN et al., (2016) have performed antimicrobial screening of Ag NPs acquired from T. foliolosum root remove against six microscopic organisms and three parasites which indicated morphological changes in the bacterial cells. Created of Ag NPs from Millettiapinnata flower remove and their portrayal together with hostile to cholinesterase, antibacterial and cytotoxic exercises have been accounted for by Rajakumar et al., (2017) round moulded Ag NPs going from 16 to 38 nm showed incredible inhibitory adequacy against acetyl cholinesterase and butyl cholinesterase. They additionally displayed cytotoxic impacts against saltwater shrimp.

Ag NPs acquired from S. alternifolium has additionally shown elevated lethality towards bacterial and contagious segregates. Ag NPs manufactured from L. Reticulate (Swamy MK et al., 2015) were observed to be lethal to HCT15 malignant growth cell line. Kanipandian et al., (2014) have detailed that Ag NPs got from C. collinus aqueous extricate show portion subordinate impacts against human lung malignant growth cell (A549) and typical cell (HBL-100). The IC50 for malignant growth cells was extremely low (30 µg/mL) yet since Ag NPs integrated from C. collinus were poisonous to ordinary cells they can't be utilized in vivo. In any case, if the plant remove contains a few cancer prevention agents, the entire synthesis may show this property yet the nanoparticles alone are unable to do as such. Ag NPs from Aloe-Vera plant separate have demonstrated changing degrees of anti-bactericidal impacts (Tippayawat Pet al., 2016). Ag NPs acquired at 100 °C for 6 h and 200 °C for 12 h (fluctuating temperature and response time) displayed a change in bacterial cell layer when reached with the nanoparticles. They were progressively powerful for gram negative microorganisms (P. aeruginosa, ATCC27803). Furthermore, they have likewise demonstrated insignificant cytotoxicity to human fringe blood mononuclear cells.

The molecule size, agglomeration, and sedimentation are identified with the cytotoxicity of silver nanoparticles. It has been shown from Alamar Blue (AB) and Lactate dehydrogenase test (LDH) that Ag NPs of 10 nm covered with citrate and PVP independently, are lethal to human lung cells (Gliga AR et al., 2014) when uncovered for 24 h. The abdominal muscle test is a proportion of cell expansion and mitochondrial action. Notwithstanding, the LDH estimates the cytotoxicity of Ag NPs as far as film harm from the cytoplasm. Both the citrate and PVP covered nanoparticles of 10 nm displayed huge poisonous quality after 24 h at the most elevated portion of 50 µg/mL. Ag NPs of bigger measurements did not change cell reasonability (Han X et al., 2011, Holder AL and Marr LC 2013). Cytotoxicity is identified with protein hindrance which is corresponded to the arrival of Ag particles since they restrain the reactant action of LDH.

It has been seen that Ag NPs harmed DNA yet they didn't expand ROS when cells were presented to them for 24 h at a portion of 20 µg/ mL (Han X et al., 2011). Gliga et al., (2012) have proposed that silver particles from AgCl are discharged in the organic liquid (Stebounova L et al., 2011) and complexed. The development of AgCl is conceivable just if the liquid is polluted with Cl− ions, all things considered, it can't ionize to Ag+ and Cl− ions since AgCl is practically insoluble in the fluid medium (Stebounova L et al., 2011). The try different things with extracellularly discharged silver particles in cell medium did not show lethality, maybe it would have responded with Cl− ions to yield insoluble AgCl.

Cytotoxicity is identified with the extent of Ag NPs independent of the covering specialist. Carlson C et al., (2008) have demonstrated an expansion in ROS generation for 15 nm hydrocarbon covered Ag NPs with respect to 55 nm. It has been accounted for by Liu W et al., (2010). That 5 nm Ag nanoparticles were more dangerous than 20 and 50 nm nanoparticles to four cell lines, to be specific, A549, HePG2, MCF-7, and SGC-7901.Wang X et al., (2014) have likewise announced that littler nanoparticles (10–20 nm) actuate more prominent cytotoxicity than the bigger ones (110 nm), and citrate covered 20 nm Ag NPs delivered intense neutrophilic irritation in the lungs of mice contrasted with those with bigger ones. The cell suitability and DNA harm might be clarified by ROS (Li N et al., 2008) age which might be conflicting to discoveries by others in vitro (Kim S and Ryu DY2013) examinations.

It is guessed that unsalvageable DNA harm is because of the cooperation of Ag NPs with fix pathways. Since this work has been done in vitro, the DNA once harmed might not be able to fix. Be that as it may, in living frameworks the cells can experience fix and duplicate yet such trials have only here and there been finished. It is notwithstanding, collectively concurred that both Ag NPs and silver particles are available at the subcellular level. The change of Ag to Ag+ ions happens because of their collaboration with biomolecules in the cell layer. The arrival of essential silver is straightforwardly relative to the extent of nanoparticles in a non-direct style. The size ward harmfulness is identified with the intracellular arrival of silver particles. In spite of the fact that agglomeration of nanoparticles diminishes their discharge, the antibacterial impact was ruined under anaerobic condition, on the grounds that without oxygen, the oxidation procedure Ag → Ag+ ceases to proceed. Ag NPs showed fantastic movement against Y. enterocolitica, P. vulgaris, E. coli, S. aureus, and S. faecalis. Since the nanoparticles are littler than the bacterial cell they may adhere to their cell dividers forbidding penetration of basic supplements prompting the passing of microorganisms. Littler size is identified with the more prominent surface territory of nanoparticles and their agglomeration around the cell divider hinders the cell division of microorganisms.

Other than the application of nanoparticles in various territories, these are widely utilized as cell reinforcement and antimicrobial specialists. The Ag NPs are significantly more dangerous to microorganisms than people. Antibacterial and antifungal functions or actions of Ag NPs were also tried against B. cereus, S. aureus, C. koseri, P. aeruginosa bacteria and C. albicans fungus. The Ag NPs penetrate into the bacterial cell and interface with the thiol, hydroxyl and carboxyl gatherings of the biomolecules present in them, in the end deactivating the revival capacity by discharging Ag+ ions. However, it is not clarified how to Ag+ ions were delivered. We immovably trust that the silver particles are more likely than not been delivered through a redox component and in this manner complexed with electron giving thiol and phosphate bunches restraining the cell replication of pathogens. It is outstanding that silver particles unequivocally tie with sulphur and oxygen-containing electron givers bunches in a living framework and capture the working of imperative organs that lead to the passing of creature.

Silver nanoparticles that have been orchestrated from lingo berry and cranberry juices were tried for their active actions against the organisms ordinarily found in maintenance and nourishment items namely, S. aureus, S. typhi, L. monocytogenes, B. cereus, E. coli, B. subtillis and C. albicans. The results they saw were that the Ag NPs were increasingly viable towards S. aureus, B. subtillis and B. cereus. Effective antibacterial action was screened against B. cereus and S. aureus for the nanoparticles.

5. Conclusion

From this chapter simply, silver nanoparticles were synthesized by modern approaches using various plant part extracts followed by a green approach. Moreover, some of the data for the scope of various synthetic approaches, Cytotoxicity  of silver nanoparticles are inserted in this chapter.

6. References

- Abou El-Nour KMM, Eftaiha A, Al-Warthan A and Ammar RAA. Arab J Chem. 2010;3:135–140.

- Agnihotri S, Mukherji S and Mukherji S. RSC Adv. 2014;4:3974–3983.

- Ahamed M, AlSaalhi MS and Siddiqui MKJ. Clin Chim Acta. 2010;411:1841–1848.

- Ahmad A, Mukherjee P, Senapat S, Mandal D, Khan MI, Kumar R and Sastry M. Coll Surf B Biointerface. 2003;28:313–318.

- Ahmad A, Wei Y, Syed F, Tahir K, Rehman AU, Khan A, Ullah S and Yuan Q. Micro Pathol. 2017;102:133–142.

- Ahmed MJ, Murtaza G, Mehmood A and Bhatti TM. Mater Lett. 2015;153:10–13.

- Ajitha B, Reddy YAK and Reddy PS. J PhotochPhotobio B. 2015;146:1–9.

- Akhavan O and Ghaderi E. ACS Nano. 2010;4:5731–5736.

- Al-Bahrani R, Raman J, Lakshmanan H, Hassan AA and Sabaratnam V. Mat Lett. 2017;186:21–25.

- Ali K, Ahmed B, Dwivedi S, Saquib Q, Al-khedhairy AA and Musarrat JPLoS ONE. 2015;10:e0131178.

- Ali M, Kim B, Belfield KD, Norman D, Brennan M and Ali GS. Mat Sci Eng C. 2016;58:359–365.

- Ali SG, Khan HM, Jalal M, Ansari MA, Mahdi AA and Ahmad MK. Asian J Pharma Clin Res. 2015;8:335–338.

- Allahverdiyev AM, Abamor ES, Bagirova M andRafailovich M. FutMicrob. 2011;6:933–940.

- Allahverdiyev AM, Kon KV, Abamor ES, Bagirova M andRafailovich M. Expert Rev Anti Infect Ther. 2011;9:1035–1052.

- Amooaghaie R, Saeri MR and Azizi M. Ecotoxicol Environ Saf. 2015;120:400–408.

- Amro NA, Kotra LP, Wadu-Mesthrige K, Bulychev A, Mobashery S and Liu G Langmuir. 2000;16:2789–2796.

- Asanithi P, Chaiyakun S and Limsuwan P. J Nanomater. 2012;2012:963609.

- Aymonier C, Schlotterbeck U, Antonietti L, Zacharias P, Thomann R Tiller JC and Mecking S. Chem Commun (Camb) 2002;24:3018–3019.

- Babu SA and Prabu HG. Mat Lett. 2011;65:1675–1677.

- Bai HJ, Yang BS, Chai CJ, Yang GE, Jia WL and Yi ZB. World J Microbiol Biotechnol. 2011;27:2723–2728.

- Bakshi MS, Possmayer F and Petersen NO. J Phys Chem C. 2007;111:14113–14124.

- Banu AN, Balasubramanian C andMoorthi PV. Parasitol Res. 2014;113:311–316.

- Basu S, Maji P and Ganguly J. Appl Nano sci. 2016;6:1–5.

- Beer C, Foldbjerg R, Hayashi Y, Sutherland DS andAutrup H. Toxicol Lett. 2012;208:286–292.

- Beg M, Maji A, Mandal AK, Das S, Aktara MN, Jha PK and Hossain M. J Mol Recognit. 2017;30:e2565.

- Bolla JM, Alibert-Franco S, Handzlik J, Chevalier J, Mahamoud A, Boyer G, Kiec-Kononowicz K and Pages JM. FEBS Lett. 2011;585:1682–1690.

- Bose D and Chatterjee S. ppl Nanosci. 2016;6:895.

- Cai JP, Li J, Thompson KD, Li CX and Han HC. J Basic Microbiol. 2007;47:84–86.

- Carlson C, Hussain SM, Schrand AM, Braydich-Stolle LK, Hess KL, Jones RL and Schlager JJ. J Phys Chem B. 2008;112:13608–13619.

- Chowdhury IH, Ghosh S, Roy M and Naskar MK. J SolGel Sci Technol. 2015;73:199–207.

- Chowdhury S, Basu A and Kundu S. Nano Res Lett. 2014;9:365. [PMC free article]

- Creighton JA, Blatchford CG and Albrecht MG. J Chem Soc Faraday Trans II. 1979;75:790–798.

- Cronholm P, Karlsson HL, Hedberg J, Lowe TA, Winnberg L, Elihn K, Wallinder IO and Moller L. Small. 2013;9:970–982.

- Devi LS and Joshi SR. Mycobiol. 2012;40:27–34.

- Edison TNJI, Lee YR and Sethuraman MG. Spectrochim Acta Mol BiomolSpectrosc. 2016;161:122–129.

- El-Sherbiny IM, El-Shibiny A and  Salih EJ PhotochemPhotobiol B. 2016;160:355–363.

- Farias CBB, Silva AF, Rufino RD, Luna JM, Souza JEG and Sarubbo LA. Electro J Biotechnol. 2014;17:122–125.

- Fatimah I.. J Adv Res. 2016;7:961–969.

- Fayaz AM, GirilalM Rahman M, Venkatesan R andKalaichelvan PT. Process Biochem. 2011;46:1958–1962.

- Furno F, Morley KS, Wong B, Sharp BL, Arnold PL, Howdle SM, Roger Bayston R, Brown PD, Winship PD and Reid HJ. J Antimicrob Chemother. 2004;54:1019–1024.

- Gaidhani SV, Raskar AV, Poddar S, Gosavi S, Sahu PK, Pardesi KR, Bhide SV andChopade BA. Indian J Med Res. 2014;140:665–671.

- Gopinathan P, Ashok AM and Selvakumar R. Appl Surf Sci. 2013;276:717–722.

- Govindarajan M, Rajeswary M, Veerakumar K, Muthukumaran K Hoti SL and Benelli G. Exp Parasitol. 2016;161:40–47.

- Graves JL, Tajkarimi M, Cunningham Q, Campbell A, Nonga H, Harrison SH and Barrick JE. Front Genet. 2015;6:42.

- HamoudNayak D, Ashe S, Rauta PR, Nayak B 2015a T, Myc A, Donovan B, Shih A, Reuter JD and Baker JR. Microbiol Res. 2000;156:1–7.

- Hazarika SN, Gupta K, Shamin KNAM, Bhardwaj P, Boruah R, Yadav KK, Naglot A, Deb P, Mandal M, Doley R, Veer V, Baruah I and Namsa ND. Mat Res Exp. 2016;3:075401.

- Hu W, Peng C, Luo W, Lv M, Li X, Li D, Huang Q and Fan C. ACS Nano. 2010;4:4317–4323.

- Husen A and Siddiqi KS. J Nano Bio Technol. 2014;12:16.

- Jagtap UB and Bapat BA. Ind Crop Prod. 2013;46:132–137.

- Jones SA, Bowler PG, Walker M and Parsons D. Wound Repair Regen. 2004;12:288–294.

- Juan L, Zhimin Z, Anchun M, Lei L andJingchao Z. Int J Nanomed. 2010;5:261–267.

- Juibari MM, Abbasalizadeh S, Jouzani GS andNoruzi M. Mater Lett. 2011;65:1014–1017.

- Kanchana R andZantye P. Asian J Pharm Clin Res. 2016;9:1124–1128.

- Karthik C and Radha KV.  J Nanomater Biostruct. 2012;7:1007–1014.

- Khan ZUH, Khan A, Shah A, Wan P, Chen Y, Khan GM, Khan AU, Tahir K, Muhammad N and Khan HU. J Mol Liq. 2016;220:248–257.

- Kim JS, Kuk E, Yu KN, Kim JH, Park SJ, Lee HJ, Kim SH, Park YK, Park YH, Hwang CY, Kim YK, Lee YS, Jeong DH and Cho MH. Nanomed Nanotechnol Biol Med. 2007;3:95–101.

- Kittler S, Greulich C, Diendorf J, Koller M andEpple M. Chem Mater. 2010;22:4548–4554.

- Kolya H, Maiti P, Pandey A and Tripathy T. J Anal Sci Technol. 2015;6:33.

- Krishnaraj RN andBerchmans S. RSC Adv. 2013;3:8953–8959.

- Kumar B, Smita K, Cumbal L and Debut A. Bio Nano Sci. 2016;6:15–21.

- Kumar CG andMamidyala SK Coll Surf B Biointerface. 2011;84:462–466.

- Kumar SP, Balachandran C, Duraipandiyan V, Ramasamy D, Ignacimuthu S and Al-Dhabi NA. Appl Nanosci. 2015;5:169–180.

- A, Sawosz E, Hotowy A, Szeliga J, Mitura S, Mitura K, Grodzik M, Orlowski P andSokolowska A. Int J Nanomed. 2010;5:1085–1094.

- Li N, Xia T and Nel AE. Free Radic Biol Med. 2008;44:1689–1699.

- Logaranjan K, Raiza AJ, Gopinath SCB, Chen Y and Pandian K. Nano Res Lett. 2016;11:520.

- Logeswari P, Silambarasan S and Abraham J. J Saudi Chem Soc. 2015;19:311–317.

- Maliszewska I, Juraszek A andBielska K. J Clust Sci. 2014;25:989–1004.

- Manivasagan P, Venkatesan J, Senthilkumar K, Sivakumar K and Kim SK. Biomed Res. 2013. 2013:287638. doi:10.1155/2013/287638.

- Manjamadha VP and Muthukumar K. Bioprocess Biosyst Eng. 2016;39:401–411.

- Mata R, Nakkala JR and Sadras SR. Mater Sci Eng C. 2015;51:216–225.

- Meena RK and Chouhan N. Res J Rec Sci. 2015;4:47–52.

- Mendis E, Rajapakse N, Byun HG and Kim SK. Life Sci. 2005;77:2166–2178.

- Mock JJ, Barbic M, Smith DR, Shultz DA and Shultz S. J Chem Phys. 2002;116:6755–6759.

- Morsy FM, Nafady NA, Abd-Alla MH and Elhady DA. Univ J Microbiol Res. 2014;2:36–43.

- Muthukrishnan S, Bhakya S, Senthil Kumar T and Rao MV. Ind Crop Prod. 2015;63:119–124.

- Nalavothula R, Alwala J, Nagati VB andManthurpadigya PR. Inter J Chem Tech Res. 2015;7:2460–2468.

- Nanda A and Saravanan M. Nanomedicine. 2009;5:452–456.

- Nayak D, Ashe S, Rauta PR and Nayak B. Nanobiotechnol. 2015;9:288–293.

- Nel AE, Madler L, Velegol D, Xia T, Hoek EMV, Somasundaran P, Klaessig F, Castranova V and Thompson M. Nat Mater. 2009;8:543–557.

- Niraimathi KL, Sudha V, Lavanya R and Brindha P. Coll Surf B Biointerface. 2013;102:288–291.

- Oberdorster E. Environ Health Perspect. 2004;112:1058–1062.

- Ocsoy I, Temiz M, Celik C, Altinsoy B, Yilmaz V and Duman F. J Mol Liq. 2017;227:147–152.

- Otaqsara SMT. Eur Phys J Appl Phys. 2011;56:30402.

- Otari SV, Patil RM, Nadaf NH, Ghosh SJ and Pawar SH. Environ Sci Pollut Res. 2014;21:1503–1513.

- Owaid MN, Raman J, Lakshmanan H, Al-Saeedi SSS, Sabaratnam V and Abed IA. Mater Lett. 2015;153:186–190.

- Panda KK, Achary VMM, Krishnaveni R, Padhi BK, Sarangi SN, Sahu SN and Panda BB. Toxicol Vitro. 2011;25:1097–1105.

- Panneerselvam C, Murugan K, Roni M, Aziz AT, Suresh U, Rajaganesh R, Madhiyazhagan P, Subramaniam J, Dinesh D, Nicoletti M, Higuchi A, Alarfaj AA, Munusamy MA, Kumar S, Desneux N and Benelli G. Parasitol Res. 2016;115:997–1013.

- Parveen M, Ahmad F, Malla AM andAzaza S Appl Nanosci. 2016;6:267–276.

- Paulkumar K, Rajeshkumar S, Gnanajobitha G, Vanaja M, Malarkodi C and Annadurai G. ISRN Nanomaterials. 2013;317963:8.

- Pavani KV and Gayathramma K. Int J Res Pharm Nano Sci. 2015;4:236–240.

- Pourali P, Baserisalehi M, Afsharnezhad S, Behravan J, Alavi H and Hosseini A. J Pure Appl Microbiol. 2012;6:757–763.

- Priya RS, Geetha D and Ramesh PS. Ecotoxicol Environ Saf. 2015;134:308–318.

- Priyadarshini S, Gopinath V, Meera Priyadharsshini N, Mubarak Ali D and Velusamy P. Coll Surf B Biointerface. 2013;102:232–237.

- Pugazhendhi S, Kirubha E, Palanisamy PK and Gopalakrishnan R. Appl Surf Sci. 2015;357:1801–1808.

- Pugazhenthiran N, Anandan S, Kathiravan G, Prakash NKU, Crawford S andAshokkumar M. J Nanopart Res. 2009;11:1811–1815.

- Puisoa J, Jonkuviene D, Macioniene I, Salomskiene J, Jasutiene I and Kondrotas R. Coll Surf B Biointerface. 2014;121:214–221.

- Rai M, Yadav A and Gade A. Biotechnol Adv. 2009; 27:76–83.

- Raj DR, Prasanth S, Vineeshkumar TV and Sundarsanakumar C. Sen Act B Chem. 2016;224:600–606.

- Rajeshkumar S, Malarkodi C, Paulkumar K, Vanaja M, Gnanajobitha G and Annadurai G. Nanosci Nanotechnol. 2013;3:21–25.

- Ramamurthi V, Geetha S and Prabhu S. J Chem Pharm Res. 2015;7:1022–1032.

- Ramesh PS, Kokila T and Geetha D. Spectrochim Acta Mol Biomol Spectrosc. 2015;142:339–343.

- Reddy AS, Chen CY, Chen CC, Jean JS, Chen HR, Tseng MJ, Fan CW and Wang JC. J Nanosci Nanotechnol. 2010;10:6567–6574.

- Reddy NJ, Vali DN, Rani M and Rani SS. Mat Sci Eng C. 2014;34:115–122.

- Rice-Evan CA and Miller N. Trends Plant Sci. 1997;2:152–159.

- Roldán MV, Pellegri N and DeSanctis O. J Nanopart. 2013;2013:524150.

- Saifuddin N, Wong CW and Yasumira AANe-J Chem. 2009;6:61–70.

- Samberg ME, Loboa EG, Oldenburg SJ and Monteiro-Riviere NA. Nanomedicine. 2012;7:1197–1209.

- Saravanan M, Vemu AK and Barik SK. Coll Surf B. 2011;88:325–331.

- Sathiyanarayanan G, Kiran GS and Selvin J Coll Surf B Biointerface. 2013;102:13–20.

- Sengottaiyan A, Mythili R, Selvankumar T, Aravinthan A, Kamala-Kannan S, Manoharan K, Thiyagarajan P, Govarthanan M and Kim J. Res Chem Intermed. 2016;42:3095–3103.

- Seshadri S, Prakash A andKowshik M. Bull Mater Sci. 2012;35:1201–1205.

- Shaligram NS, Bule A, Bhambure R, Singhal RS, Singh SK, Szakacs G and Pandey A. Process Biochem. 2009;44:939–943.

- Shankar SS, Rai A, Ahmad A and Sastry M. J Coll Interface Sci. 2004;275:496–502.

- Shanmugasundaram T, Radhakrishnan M, Gopikrishnan V, Pazhanimurugan R andBalagurunathan R. Colloids Surf B Biointerfaces. 2013;111:680–687.

- Shanthi S, Jayaseelan BD, Velusamy P, Vijayakumar S, Chih CT and Vaseeharan B. Micro Pathog. 2016;93:70–77.

- Shin Y, Bae IT and Exarhos GJ. Colloids Surf A. 2009; 348:191–195.

- Siddiqi KS and Husen A. Nano Res Lett. 2016;11:363.

- Siddiqi KS and Husen A. Nano Res Lett. 2016;11:98.

- Siddiqi KS and Husen A. Nano Res Lett. 2016;11:482.

- Siddiqi KS and Husen A.. J Trace Elements Med Biol. 2017;40:10–23.

- Siddiqi KS, Rahman A, Tajuddin and Husen A. Nano Res Lett. 2016;11:498.

- Sigamioney M, Shaik S, Govender P and Krishna SBN. S Afr J Bot. 2016;103:230–240.

- Singh D, Rawat D and Isha B. Bioresour Bioprocess. 2016;3:14.

- Soenen SJ, Rivera-Gil P, Montenegro JM, Parak WJ, De Smedt SC and Braeckmans K. Nano Today. 2011;6:446–465.

- Sondi I andSalopek-Sondi B. J Coll Interface Sci. 2004;275:177–182

- Sotiriou GA, Teleki A, Camenzind A, Krumeich F, Meyer A, Panke S and Pratsinis SE. Chem Eng J. 2011;170:547–554.

- Sowmyyan T and Lakshmi GV. World J Pharm Pharm Sci. 2015;5:786–805.

- Sreekanth TVM, Jung M and Eom I. Appl Surf Sci. 2015;361:102–106.

- Sriranjani R, Srinthiya B, Vadivel V, Pemaiah B, Anthony SP, Sivasubramanian A and Muthuraman MS. J Mol Liq. 2016;220:926–930.

- Srivastava SK and Constanti M. J Nanopart Res. 2012;14:831–840.

- Stebounova L, Guio E andGrassian V.. J Nanopart Res. 2011;13:233–244.

- Sundararajan B, Mahendran G, Thamaraiselvi R and Ranjitha Kumari BD. Bull Mater Sci. 2015;39:423–431.

- Tahir K, Nazir S, Li B, Khan AU, Khan ZUH, Ahmad A and Khan FU. SeparPuri Technol. 2015;150:316–324.

- Thomas R, Jasim B, Mathew J and Radhakrishnan EK. Nano Biomed Eng. 2012;4:183–187.

- Thwala N, Musee M and Nota N. J Environ Monit. 2011;13:1164–1183.

- Tippayawat P, Phromviyo N, Boueroy P and  Chompoosor A. Peer J. 2016;4:e2589.

- Vahabi K, Mansoori GA and Karimi S. Insci J. 2011;1:65–79.

- Varghese A, Anandhi P, Arunadevi R, Boovisha A, Sounthari P, Saranya J, Parameswari K and Chitra S. JPSR. 2015;7:266–273.

- Vigneshwaran N and Kathe A. Langmuir. 2007;23:7113–7117.

- Vigneshwaran N, Ashtaputre NM, Varadarajan PV, Nachane RP, Paralikar KM andBalasubramanya RH. Mater Lett. 2007;61:1413–1418.

- Vigneshwaran N, Kathe AA, Varadarajan PV, Nachane RP and Balasubramanya RH. Coll Surf B Interface. 2006;53:55–59.

- Vigneshwaran N, Nachane RP, Balasubramanya RH and Varadarajan PV.  Carbohydr Res. 2006; 341:2012–2018.

- Vijay Kumar PPN, Pammi SVN, Kollu P, Satyanarayana KVV and Shameem U. Ind Crop Prod. 2014;52:562–566.

- Wang C, Kim YJ, Singh P, Mathiyalagan R, Jin Y and Yang DC. Artif Cell Nanomed Biotechnol. 2016;44:1127–1132.

- Wang H, Chen H, Wang Y, Huang J, Kong T, Lin W, Zhou Y, Lin L, Sin D and Li Q. Curr Nanosci. 2012;8:838–846.

- Wang L, Xu H, Gu L, Han TT, Wang S and Meng FB. Mat Technol. 2016;31:437–442.

- Wei L, Lu J, Xu H, Patel A, Chen ZS and Chen G. Drug Discov Today. 2015;20:595–601.

- Wei X, Luo M, Li W, Yang L, Liang X, Xu L, Kong P and Liu H. Bioresour Technol. 2012;103:273–278.

- Wright R, Zhang Q and Kirby P. Mater Chem Phys. 2011;129:1075–1080.

- Xu WP, Zhang LC, Li JP, Lu Y, Li HH, Ma YN, Wang WD and Yu SH. J Mater Chem. 2011;21:4593–4597.

- You J, Zhang Y and Hu Z. Colloids Surf B Biointerfaces. 2011;85:161–167.

- Yugandhar P, Haribabu R and Savithramma N. Biotech. 2015;5:1031–1039.

- Zaheer Z and Rafiuddin. Colloids Surf B Bio Inter Faces. 2012;90:48–52.

- Zhang H, Li Q, Lu Y, Sun D, Lin X, Deng X, He N and Zheng S. J Chem Technol Biotechnol. 2005;80:285–290.

- Zhang Q, Li N, Goebl J, Lu Z and Yin Y. J Am Chem Soc. 2011;133:18931–18939.

- Zhang W, Qiao X and Chen J. Mater Sci Eng B. 2007;142:1–15.

- Zia F, Ghafoor N, Iqbal M and Mehboob SAppl Nanosci. 2016;6:1023.