- CONCRETE MIX DESIGN FORMAT FOR COMPUTERS AS PER IS10262-2009

Sankara G.1., and Sivapullaiah P V .2

1. Professor, RR Institute of Technology, Bengaluru, 2. Rtd Professor, Indian Institute of Science, Bengaluru

1.0 INTRODUCTION

Concrete is one of the most widely used construction material across the globe. It is used in various civil engineering infrastructure projects like Dams, Bridges, flyovers, Sky scrapers, industrial structures, highways, tunnels, water treatment facilities, ports, airports and stadiums etc. It is very versatile material and can be moulded in any shapes like square, rectangular, circular and into a variety of architecture features. All types of structural elements like footings, columns, walls, beams, slabs, floors, piers and piles etc can be casted with concrete. Concrete is the most popular material used in foundations for all types of structures because it is strong, durable and can sustain the attack by moisture.  Concrete is a composite material consisting of a cementitious paste (cement+ water) and inert aggregate (coarse and fine) filler materials. Cast in place and precast concrete are two methods of application of concrete.  Cast in place concrete or poured concrete is the common method of application of concrete in construction. Precast concrete can be adopted when space and time are constrained and for achieving better quality. Concrete is exposed to static and dynamic loads like self weight, floor loads, wind, seismic, wave and machine and floor loads etc in several combinations. Plain concrete is used in structural elements subjected to compressive stresses. In members subjected to tensile stresses, concrete is inserted with reinforcement and is called reinforced concrete.  Whether it is plain or reinforced concrete or cast in place or precast, the quantitative proportions of its ingredients plays a vital role in achieving its intended purpose and objectives.

2.0 MIX DESIGN – AN OVERVIEW

Unlike cement which is a homogeneous material, concrete is considered as a heterogeneous mixture. Preparing the concrete that meets the requirements is not a pure science as preparing a chemical mixture in laboratory. Ratio of the quantities of ingredients per unit quantity of specified concrete is not a universally fixed one. It depends not only on the nature and quality of ingredients and desired properties of output. Storage of ingredients, method of mixing – manual or machine mixing, degree of supervision and control, transportation, placing and compacting the concrete, curing and workmanship etc also influences the mix proportions.    Concrete mix design consist a series of steps to arrive at most economical ratio of quantities - choosing suitable ingredients, determination of their properties, assuming certain parameters based on code and project provisions and past experience, estimating material quantities, preparing trial mixes,  testing in laboratory and field, adjusting quantities based on test results etc.

Concrete is made up of cement, water, fine and coarse aggregates in various percentages. Chemical and mineral admixtures are also being added to concrete some times to alter its properties. Cement and admixtures are factory made. There are more than ten varieties of cement like ordinary Portland cement (OPC), Portland pozzolona cement (PPC) etc. In OPC , there 3 grades viz., 33, 43 and 53 based on its compressive strength. Aggregates and water are locally available materials. The source, particle size distribution and shape of grains of aggregates vary from place to place. Water shall also meet certain specifications. Freshly prepared concrete is liquid and hardens quickly due to chemical reaction between cement and water.  The ingredients are mixed in different proportions to produce a concrete that meets the objectives specified by the codes and project requirements. Sufficient workability is the criteria to be met during mixing, transporting, placing and compacting the concrete. In the hardened state, it shall possess i)  the strength and stability requirement of ultimate limit state (ULS) ii) meet the deflection and cracking criteria of  serviceability limit state (SLS) and iii) durable enough to resist weathering action and chemical attacks etc during its life time in various exposure conditions.  Required minimum compressive strength of concrete at 28 days in MPa (N/mm2) is represented by the grade of concrete viz., M20, M30, and so on. The “M” point to Mix and Number after M (M20, M30) refers the compressive strength of concrete after 28 days of curing and testing.

This wide variety of ingredients and various desired requirements of output concrete makes the mix design a tricky task. A lot of data need to be handled, adjustments need to be made based on deviations in properties of ingredients and iteration need to be performed based on test results etc. Computer software tools can be employed if procedures with a series of steps incorporating relevant data and suggesting necessary adjustments are developed. In this chapter mix design flowchart based on IS 10262-2009 and procedure with illustrative examples is presented so that readers can develop their own computer applications with ease.

- 3.0 FACTORS GUIDING MIX DESIGN

- The desired traits of output concrete in fresh and hardened state like workability, bleeding, segregation, uniformity, strength, permeability  and durability etc., are the main guiding factors that influence the concrete mix design. Properties of ingredients, workmanship and quality control in mixing, placing, compacting and finishing, water cement ratio, quantity of cement etc., also play a vital role in the design mix. Mix design used for fresh concrete affect the properties of hardened concrete also. Weather conditions during in the initial stages and exposure conditions during working life also affect the mix design. Code specifications, past experience, testing laboratory and field specimens help in arriving at optimum mix design.

- 3.1 Exposure Conditions

- Concrete structures whether they are build above or below the ground or submerged in water come across variety of environmental conditions and chemical attacks. Severe rain, alternate wet and dry conditions, freeze and thaw, saline water and sulfate attack etc fall under these conditions. IS 456 has classified them into mild, moderate, severe, very severe and extreme exposure conditions as described in Table 1. Concrete may undergo deterioration and may require repair and maintenance to perform its function during its life cycle. Lower water-cement ratio, maintaining minimum cement content, using special cements and cementitious materials etc can reduce the impact of these exposure conditions on the durability of concrete.

Table 1 Environmental exposure conditions (clauses 8.2.2.1 and 35.3.2 of IS 456-2000)

Environment	Exposure conditions for concrete surfaces

Environment	• Protected from weather or other aggressive conditions

Moderate	• Sheltered from severe rain or freezing whilst wet

• Exposed to condensation and rain

• Continuous contact with water

• In contact with or buried under non-aggressive soil/ground water

• Sheltered from saturated salt air in coastal areas

Severe	• Exposed to severe rain, alternate wetting and drying or occasional freezing

whilst wet or severe condensation

• Completely immersed in sea water

• Exposed to coastal environment

Very severe	• Exposed to sea water sprays, corrosive fumes, or serve freezing conditions

whilst wet

• In contact with or buried under aggressive subsoil/ground water

Extreme	• Surfaces of members in tidal zones

• Members in direct contact with liquid/solid aggressive chemicals

- 3.2 Compressive strength

- Concrete whether plain or reinforced shall possess minimum compressive strength prescribed by the project specifications. It is called characteristic compressive strength and described as grade of concrete like M30 etc as shown in Table 2. IS 456 recommends the minimum grade of concrete to be used in various exposure conditions as shown in Table 3.

Table 2 Grade of Concrete (clauses 6.1,9.2.2, 15.1.1 and 36.1 of IS 456-2000)

Group	Grade designation*	   Specified characteristics compressive

strength of a 150-mm cube at 28 days(N/mm2)

Ordinary concrete		M10	       10

M15	       15

M20	       20

Ordinary concrete		M25	       25

M30	       30

M35	       35

M40	       40

M45	       45

M50	       50

M55	       55

High-strength concrete	M60	       60

M65	       65

M70	       70

M75	         75

M80	         80

*In the designation of concrete, M refers to the mix and the number refers to the specified compressive strength of a 150-mm cube at 28 days, expressed in N/mm2.

For concrete of compressive strength greater than M55, the design parameters given in IS: 456-2000 may not be applicable. This has been discussed in a later chapter on high – strength concrete

- The term mean compressive strength to describe strength higher than characteristic compressive strength is also used in some codes. It is calculated using standard deviations given in Table 4 as explained in solved examples.

Table 3  Minimum cement content according to IS:456-2002 (clauses 6.1.2,8.2.4.1 and 9.1.2)

- Minimum cement content * , maximum water-cement ratio, and minimum grade of concrete for different exposures with normal-weight aggregrates of 20mm nominal maximum size

Exposure                      Plain concrete                                      Reinforced concrete

Minimum     Maximum   Minimum      Minimum    Maximum   Minimum

cement         free water-   grade of	        cement	    free water-  grade of

content            cement       concrete           content        cement       concrete

(kg/m3)              ratio                                   (kg/m3)          ratio

Mild 		220		0.60		 +		300		0.55	     M20

Moderate	240		0.60		M15		300		0.50	     M25

Severe 		250		0.50		M20		300		0.45	     M30

Very severe 	260		0.45		M20		340		0.45	     M35

Mild 		280		0.40		M25		360		0.40	     M40

*The cement contents prescribed in this table are irrespective of the grades of cement and inclusive of mineral admixture additions. Additions such as fly ash or ground, granulated blast –furnace slag may be taken into account in concrete composition with respect to the cement content and water- cement ratio if the suitability is established, and as long as the maximum amounts taken into account do not exceed the limit of pozzolana and a slag specified in IS :1489 (part 1) and IS:455, respectively .The maximum cement content is restricted to 450kg/m3.

- + The minimum grade for plain concrete under mild exposure under mild exposure conditions is not specified.

Table 4  Assumed standard deviations* (clause 9.2.4.2 and Table 11 of  IS:456-2000)

Grade of concrete                                        Assumed standard deviation (N/mm2)

M10   								3.5

M15

M20								4.0

M25

M30

M35

M40								5.0

M45

M50

- Strength development in concrete is influenced by type and quantity of cement, water –cement ratio, maximum size, grading and shape of aggregates, admixtures and curing etc. Strength is inversely proportional to water-cement ratio, when other parameters are fixed. The maximum water-cement ratio shall not exceed the limit mentioned in IS 456 as shown in Table 3 as it affects the other properties. Strength of concrete can be increase by reducing water-cement ratio, using higher cementitious materials, adding admixtures, minimizing bleeding and segregation, adopting proper finishing and curing measures etc.

- 3.3 Durability

- Life span and performance of concrete deteriorates when exposed to harsh weather and harmful environments. Sulfate attacks, Alkali-silica reactions, corrosion and freeze-thaw cycles etc are some examples for these environmental conditions. Lower water cement ratio, cement content not less than prescribed in Table 2, use of special cements and cementitious materials and suitable aggregate composition can help in enhancing the durability.

- 3.4 Workability

- The ease of mixing, placing, compacting and finishing of concrete and mortar is reflected in its workability. Concrete having low workability is difficult to use in narrow beams and columns, beam –column intersections and other congested places etc. It results in insufficient compaction and affects the strength and durability. Higher water cement ratio produces high workable concrete mixture which is prone to bleeding and segregation. Workability needs adjustment based on applied conditions like amount and spacing of reinforcement and accessibility of point of application etc. Water content plays crucial role in modifying workability. Instead of increasing water content to achieve higher workability, water reducing admixtures can be employed. Spherical shaped aggregates can also enhance workability. Workability is popularly expressed in slump test measurements. Degree of workability for various placing conditions is given in IS 456.

- 3.5 Water

- Water suitable for drinking can be used in concrete. Non potable water whch does not contain chlorides, sulfates, alkalies, solids and oils etc in harmful quamtities  can also be used.  Strength,  durability and setting time will be altered , corrosion, staining and efflorescence etc are the other ill effects of  impurities in water. Higher water quantity may facilitate workability but reduce strength and durability. Maximum water based on nominal maximum size of aggregate is specified in IS10262 as shown in Table 5.

Table 5  Maximum Water Content per Cubic Metre of Concrete for Nominal Maximum Size of Aggregate (Clauses 4.2. A-5 and B-5 – IS 10262-2009)

| Sl No | Nominal Maximum Size of Aggregate mm | Maximum Water Content I) kg |
| --- | --- | --- |
| (1) | (2) | (3) |
| i) ii) iii) | 10 20 40 | 208 186 165 |
| NOTE - These quantities of mixing water are for use in computing cementitious material contents for trial batches. |  |  |
| 1) Water content corresponding to saturated surface dry aggregate. |  |  |

- 3.6 Cement

- Cement is the most expensive ingredient in concrete and it shoul be used judiciously. Higher workability and smooth surface finish can be achieved by increasing cement. At the same time higher cement content can generate cracks in the concrete. Reduction of cement content affects the strength and durability of concrete. Minimum and maximum cement quantities are usually specified in project requirements. Variety of cements are available to meet the end use and exposure environments.

- 3.7 Water – Cement ratio

- The binding agents of cement paste i.e., water and cement are added in a certain proportion in a concrete mix. The ratio of water to cement by weight is called water-cement ratio, w/c ratio. It is a critical parameter in mix design as it impacts all properties of concrete. Lower w/c ratio increases strength and durability.  Higher w/c ratio increases workability and permeability. Maximum w/c ratio is specified in the range of 0.4 to 0.6 by IS 10262 as shown in Table 2 based on exposure condition. It is decreasing with increasing severity. W/C ratio can be optimized by adding water reducing admixtures.

- 3.8 Aggregates

- Locally available materials such as gravel, crushed stone and sand etc are used as aggregates in concrete mix. They are inert materials but their surface should be clean from any chemical coatings. Their properties such as size, shape and texture varies from site to site. Hence it is difficult to produce uniform concrete across any state or country. Naturally available sand is more popular as fine aggregate. Manufactured sand (M-sand) with proper gradation obtained by crushing hard stones is gaining adaptability.  Proper combination of well graded coarse and fine aggregates improves the strength and durability. Uniform gradation produces a dense concrete with a better packing of particles. It reduces the water requirement and enhances workability. Gap graded aggregates require more water and tend to cause segregation and shrinkage cracks. The volume of coarse aggregate based on its nominal maximum size and grading zone of fine aggregate per unit volume of concrete is given in IS 10262 as shown in Table 6.

Table 6 Volume of Coarse Aggregate per Unit Volume of Total Aggregate for Different Zones of Fine Aggregate (Clauses 4.4, A-7 and B-7 - IS 10262-2009)

| Sl No | Nominal maximum size of aggregate | Volume of Coarse Aggregate1) per Unit Volume of Total Aggregate for Different Zones of Fine Aggregate |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | mm | Zone IV | Zone III | Zone II | Zone I |
| (1) | (2) | (3) | (4) | (5) | (6) |
| i) | 10 | 0.50 | 0.48 | 0.46 | 0.44 |
| ii) | 20 | 0.66 | 0.64 | 0.62 | 0.60 |
| iii) | 40 | 0.75 | 0.73 | 0.71 | 0.69 |
| I ) Volumes are based on aggregates in saturated surface dry condition |  |  |  |  |  |

- Bigger size particles requires less cement and produce a leaner mix where as small size particles increases surface area and induce higher strength due to better bonding with cement paste. In case of reinforced concrete, maximum size of the particles shall be less than the spacing between reinforcement bars.

- 3.9 M-Sand – Quantity of Manufactured sand (M-sand) as fine aggregate can be estimated based on grading zone and making allowance for its Free (surface) water  and moisture absorption

- 3.10 Admixtures

- Performance of concrete can be enhanced by altering its properties through addition of some substances called admixtures to concrte mix. Chemical admixtures help in redcuing water content (plasticizers, super plasticizers), Accelerating and retarding the setting time (accelerators and set retardors), slow down corrosion (corrosion inhibiting), control drying shrinkage and cracking (shrinkage reducing) etc. Mineral admixtures also called as cementitious materials can partially replace cement quantity. Fly ash, silica fume and blast furnace slag etc are mineral admixtures added to concrete to improve its strength, workability and durability. The quantities of these admixture to be used in concrete mix depends manufacturer recommendations and relevant codes.  Proportions of concrete mix design need to be adjusted when these admixtures are added to the concrete.

3.11 Quality control

Quality control in choosing right materials, batching, mixing , workmanship and supervision etc can influnce the properties of concrte in fresh and hardened state. It can observed from testing of specimens. The deviation of results from the mean strength shall be with in specified limits.

4.0 MIX DESIGN FLOWCHART AND PROCEDURES AS PER IS 10262-2009

Mix design requires input data from engineers, design parameters as per project specifications and data from testing of materials. Using this data calculations are carried out in sequential  steps. The results of the calculations need to be verified and modified with respect to the limits specified in the relevant codes and material properties. Trial mixes are casted and tested at specified time intervals. If the test results do not satisfy mean strength criteria, the design calculations are repeated with changes in materials or their quantities or both till the desired results are achieved. All these steps, design parameters and checks and corrections are illustrated in a flowchart and procedures in detail as shown below. Based on this flow chart and procedures engineers can develop computer models and calculation spread sheets for easy and repeated calculations.

4.1 FLOWCHART

CONCRETE MIX DESIGN AS PER IS 10262 -2009 – FLOWCHART

DESIGN PARAMETERS / TEST DATA REQUIRED

STEPS

CHECKS/CORRECTIONS

Type of cement, Sieve analysis report of Coarse aggregate, Degree of Supervision

TARGET STRENGTH

Concrete grade designation, Standard deviation (SD) from test data/Table 1 of IS 10262

SELECTION OF WATER / CEMENT (W/C) RATIO

W/C ratio test data/ Exposure condition and maximum W/C ratio from IS 456

W/C ratio shall be < Maximum W/C ratio from IS456

1. The slump assumed in Table 2 of IS 10262 is 25-50 mm. Increase water content by 3% for every 25 mm rise in slump.   2. The water content in Table 2 is for angular coarse aggregate.  Reduce water content by approximately 10 kg for sub-angular aggregates, 20 kg for gravel with some crushed particles and 25 kg for rounded gravel.  3. Lower water content by 5 to 10 percent for water reducing admixtures and 20 percent and above for super plasticizing admixtures at appropriate dosages.   4. Saturated surface dry (SSD) condition is assumed for aggregates. Reduce water content based on the free (surface) moisture contributed by the fine and coarse aggregates.  In case of dry aggregates, increase the water content equal to their water absorption capacities.

SELECTION/ESTIMATION OF WATER CONTENT

Maximum Water Content from Table 2 of IS 10262, Nominal maximum  size of aggregate , shape of aggregate,  Degree of Workability / slump based on placing conditions (IS 1199), Type of admixture , The surface water and percent water absorption of aggregates

CALCULATION OF CEMENT CONTENT

1.Shall be > minimum and <  maximum Cement content specified   in  IS 456  . 2. If cernentitious material content is increased recalculate the W/C ratio

Type and percentage of mineral admixture like fly ash,  Increase in cernentitious material content

ESTIMATION OF VOLUME OF FINE AGGREGATE

ESTIMATION OF VOLUME OF COARSE AGGREGATE (CA)

CALCULATION OF QUANTITIES  OF MIX COMPONENTS

TRIAL MIXES

Table 3 of IS 10262, Zone of Fine Aggregate, , Nominal maximum  size of aggregate, W/C ratio, shape of coarse aggregate , method of placing of concrete,

Specific gravity of  Cement , Coarse aggregate ,  Fine aggregate and admixture

1. The W/C ratio assumed in Table 3 is 0.5. The  volume of coarse aggregate is modified at the rate of decrease/increase ( -/+) of 0.01 for every  increase/decrease (±) of 0.05 change in W/C ratio.                                             2. Reduce volume CA by 10 percent for pumpable concrete .   3. Volume may be required to be increased suitably, based on experience, for non angular coarse aggregates

Mass of aggregates need to be adjusted for surface  free water of moist aggregates and water absorption capacities of dry aggregates

Trial 1. As per above quantities. Free from segregation and bleeding. Check the slump.                                                                                                  Trial 2. In case mismatch of slump, adjust the water content and dosage of admixture till the specified slump is achieved. Re estimate the mix proportions  based on the revised water content. Check for durability requirements.  Trial 3 and  Trial 4. Conduct with a variation of ±10 percent of water-cement ratio to Trial 2 W/C ratio.  Plot W/C ratio vs Strength and choose the optimum W/C ratio and corresponding mix proportions for field trials.

- 4.2 Procedure

- Step 1  Collect all the required project specifications and test data as shown below

| - Item |  | - Data |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| - Concrete | - Grade designation |  |  |  |  |  |  |
|  | - Type of Concrete |  |  |  |  |  |  |
| - Cement | - Type of Cement |  |  |  |  |  |  |
|  | - Minimum cement content |  |  |  |  |  |  |
|  | - Maximum cement content |  |  |  |  |  |  |
|  | - Specific gravity |  |  |  |  |  |  |
| - Mineral admixture | - Type |  |  |  |  |  |  |
|  | - Specific gravity |  |  |  |  |  |  |
| - Aggregate | - Maximum nominal size |  |  |  |  |  |  |
|  | - Type and Shape of aggregate |  |  |  |  |  |  |
|  |  | - Coarse aggregate |  |  |  |  | - Fine aggregate |
|  | Specific gravity |  |  |  |  |  |  |
|  | Water absorption |  |  |  |  |  |  |
|  | Free (surface) moisture |  |  |  |  |  |  |
|  | Sieve analysis gradation | - IS Sive size mm | - Analysis of Coarse Aggregate Fraction |  |  | - Remarks |  |
|  |  |  | - I | - II | - Combined (x% of I + y% of II) | - Conforming to IS 383 |  |
|  |  | - 20 |  |  |  |  |  |
|  |  | - 10 |  |  |  |  |  |
|  |  | - 4.75 |  |  |  |  |  |
|  |  | - 2.36 |  |  |  |  |  |
| Maximum water-cement ratio |  |  |  |  |  |  |  |
| Workability |  |  |  |  |  |  |  |
| Exposure condition |  |  |  |  |  |  |  |
| Method of concrete placing |  |  |  |  |  |  |  |
| Degree of supervision |  |  |  |  |  |  |  |
| Chemical admixture type conforming to IS 9103 |  |  |  |  |  |  |  |

Step 2   Calculate Target mean strength of Concrete

f’ck =f ck + 1.65 s

where f’ck = target mean compressive strength at 28 days,

fck = characteristic compressive strength at 28 days corresponding to grade of concrete. Minimum grade of concrete can be chosen from IS 456 based on exposure condition and type of concrete (Plain/Reinforced) and

s = standard deviation,  From Table 1 of IS 10262-2009

Values of s are to be increase by 1N/mm2 if proper supervision and control in storage of cement, weigh batching of all materials and controlled addition of water etc are not followed

Step 3 Decide Water-Cement ratio

From IS 456, based on exposure condition and type of concrete (Plain/Reinforced), Maximum permissible water-cement ratio can be picked.   Based on experience and test data, water-cement ratio less than max W-C ratio can also be adopted.

Step 4 Determination of Water content

Table 2 of IS 10262-2009 stipulates maximum water content for angular coarse and saturated surface dry aggregate and for a slump of  25 to 50 mm without any admixtures.

a). If the slump is more than 50 mm increase water content by 3% for every 25 mm rise in slump.

b). Reduce water content by approximately 10 kg for sub-angular aggregates, 20 kg for gravel with some crushed particles and 25 kg for rounded gravel.

c). Lower water content by 5 to 10 percent for water reducing admixtures and 20 percent and above for super plasticizing admixtures at appropriate dosages.

d). Saturated surface dry (SSD) condition is assumed for aggregates. Reduce water content based on the free (surface) moisture contributed by the fine and coarse aggregates.  In case of dry aggregates, increase the water content equal to their water absorption capacities.

Step 5 Calculation of Cement/Cementitious (cement +mineral admixture) material Content

Cement/Cementitious material content in kg/m3 = water content in litres determined in step 4 / water-cement ratio decided in step 3

It shall not be less than the minimum cement content and not more than maximum cement content specified in IS 456 and  by the project.

If mineral admixture is used

In some special conditions,  cementitious content is increased based on experience and trial.

Then calculate the revised cementitious content and modified water-cement ratio.

Revised cementitious content = Cementitious material content * [1+ (%increase/100)]

Modified water-cement ratio = water content/ Revised cementitious content

Select the percentage xx of mineral admixture to be used based on project requirement and quality of materials.

Mineral admixture content @ xx% of total cementitious material content =  Revised cementitious material content * xx/100

Cement content = Revised cementitious material content - Mineral admixture content

Step 6  Fractions of  Coarse and Fine aggregate content by volume

From Table 3 of IS 10262-2009 volume of coarse aggregate can be obtained corresponding to 20 mm size aggregate and zone of fine aggregate  for a water-cement ratio of 0.50 .

a) Modify the proportion of volume of coarse aggregate at the rate of 0.01 decrease/increase ( -/+) for every  increase/decrease (±) of 0.05 change in W/C ratio.

b)  Reduce the volume CA by 10 percent for pumpable concrete

c). Volume may be required to be increased suitably, based on experience, for non angular coarse aggregates

fraction of volume of fine aggregate content = I – proportion of volume of coarse aggregate

Step 7  Calculation of quantities of ingredients

The mix calculations per unit volume of concrete shall be as follows:

a) Volume of concrete = 1 m3

b) Volume of cement m3 = (Mass of cement calculated as in step 5 * 1) /( Specific gravity of cement  *I 000)

c) Volume of water m3 = (Mass of water calculated as  in step 4 * 1) /( Specific gravity of water  *I 000)

d) Volume of chemical admixture (superplasticizer) (@ 2.0 percent by mass of cementitious material)

Mass of admixture  kg = Mass of cement calculated as in step 5 *0.02

Volume  m3 = (Mass of admixture * 1) /( Specific gravity of admixture *I 000)

e) Volume of aggregates (coarse + fine) = [Volume of concrete – (Volume of cement + Volume of water + Volume of admixture)]

= [a- (b +c +d)]

f) Mass of coarse aggregate kg = volume of aggregates calculated in step e x fraction of coarse aggregate calculated as in step 6  x Specific

gravity of coarse aggregate x I 000

g) Mass of fine aggregate kg  =  volume of aggregates calculated in step e x fraction of fine  aggregate calculated as in step 6  x Specific

gravity of fine aggregate x I 000

Step 8  Trial Mixes

Conduct 4 trials. Check the slump, durability requirements and strength. Plot Water-Cement ratio vs Strength and choose the optimum   W-C  ratio and corresponding mix proportions for field trials.

Trial 1  Quantities for Mix as calculated above

Cement  =   kg/m3

Water  =    kg/m3 or litres/ m3

Fine aggregate =  kg/m3

Coarse aggregate = kg/m3

Chemical admixture = kg/m3

Water-cement ratio =

Concrete should be free from segregation and bleeding.   Check the slump.

Trial 2. In case mismatch of slump, adjust the water content and dosage of admixture till the specified slump is achieved. Re estimate the mix proportions based on the revised water content. Check for durability requirements.

Trial 3 and Trial 4. Conduct with a variation of ±10 percent of water-cement ratio to Trial 2 W-C ratio.

- 5.0   SOLVED EXAMPLES

- Mix design examples using different types and shapes of coarse aggregates and with and without addition of fly ash are explained below. They will help in application of various steps and verification of results if calculations are done in computer models developed based on the flowchart presented earlier

- Example 1 Design M25 concrete as per the data given below.

- Step 1  Collect all the required project specifications and test data as shown below

| Item |  |  | Data |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Concrete | Grade designation |  | M25 |  |  |  |  |  |
|  | Type of Concrete |  | Reinforced Cement Concrete |  |  |  |  |  |
| Cement | Type of Cement |  | Grade 53 conforming to IS 12269 |  |  |  |  |  |
|  | Minimum cement content |  | 300 |  |  |  |  |  |
|  | Maximum cement content |  | 450 kg/m3 |  |  |  |  |  |
|  | Specific gravity |  | 3.15 |  |  |  |  |  |
| Mineral admixture | Type |  | Nil |  |  |  |  |  |
|  | Specific gravity |  | - |  |  |  |  |  |
| Aggregate | Maximum nominal size |  | 20 |  |  |  |  |  |
|  | Type and Shape of aggregate |  | Crushed granite and Sub angular |  |  |  |  |  |
|  |  |  | Coarse aggregate |  |  |  |  | Fine aggregate |
|  | Specific gravity |  | 2.67 |  |  |  |  | 2.6 |
|  | Water absorption |  | 0.5% |  |  |  |  | nil |
|  | Free (surface) moisture |  | nil |  |  |  |  | 2% |
|  | Sieve analysis gradation |  | IS Sieve size mm | Analysis of Coarse Aggregate Fraction |  |  | Remarks | Conforming to Zone I IS 383 |
|  |  |  |  | I | II | Combined (55% of I + 45% of II) | Conforming to IS 383 |  |
|  |  |  | 20 | 100 | 100 | 100 |  |  |
|  |  |  | 10 | 10 | 50 | 28 |  |  |
|  |  |  | 4.75 |  | 10 | 4.5 |  |  |
|  |  |  | 2.36 |  |  |  |  |  |
| Maximum water-cement ratio |  |  | 0.50 |  |  |  |  |  |
| Workability |  |  | 75 mm |  |  |  |  |  |
| Exposure condition |  |  | moderate |  |  |  |  |  |
| Method of concrete placing |  |  | pumpable |  |  |  |  |  |
| Degree of supervision |  |  | Intermittent supervision |  |  |  |  |  |
| Chemical admixture type conforming to IS 9103 |  | Type | High range water reducing admixture – HRWR @ 2% of Cement wt |  |  |  |  |  |
|  |  | Specific gravity | 1.145 |  |  |  |  |  |

Step 2   Calculate Target mean strength of Concrete

f’ck =f ck + 1.65 s

Target strength = 25 + 1.65 *5  = 33.25 N/mm2

s= 4 from Table1 of IS 10262-2009; Add 1N/mm2 as supervision is intermittent

Step 3 Decide Water-Cement ratio

From IS 456, for moderate exposure condition and Reinforced concrete (Plain/), Maximum permissible water-cement ratio is 0.5.   Consider 0.45 as water-cement ratio. It is less than 0.50.

Step 4 Determination of Water content

From Table 2 of IS 10262-2009  maximum water content = 186 litre for angular coarse and saturated surface dry aggregate and for a slump of  25 to 50 mm without any admixtures.

a). slump is 75 mm. Hence increase water content by 3%. Water content = 186 *1.03 = 192 litre

b). Reduce water content by approximately 10 kg for sub-angular aggregates, water content = 192-10 = 182 litre

c). Lower water content by 25 percent for High range water reducing admixture. = 182*0.75 = 137 litre

d). Saturated surface dry (SSD) condition is assumed for aggregates.

Step 5 Calculation of Cement Content

Cement content in kg/m3 = 137/0.45 = 304 kg.  It is more than minimum cement content of 300 kg

Step 6  Fractions of  Coarse and Fine aggregate content by volume

From Table 3 of IS 10262-2009 volume of coarse aggregate is 0.60 corresponding to 20 mm size aggregate and zone of fine aggregate I  for a water-cement ratio of 0.50

a) Modify the proportion of volume of coarse aggregate at the rate of 0.01 decrease/increase ( -/+) for every  increase/decrease (±) of 0.05 change in W/C ratio.

For 0.45 W/C ratio   Volume of CA = 0.60+(0.01*0.05/0.05) =0.61

b)  Reduce the volume CA by 10 percent for pumpable concrete,  Volume of CA = 0.61*0.9 = 0.55

Fraction of volume of fine aggregate content = I – 0.55=0.45

Step 7  Calculation of quantities of ingredients

The mix calculations per unit volume of concrete shall be as follows:

a) Volume of concrete = 1 m3

b) Volume of cement m3 = (304 * 1) /( 3.15  *I 000) = 0.097 m3

c) Volume of water m3 = (137 * 1) /( 1  *I 000) = 0.137 m3

d) Volume of chemical admixture (superplasticizer) (@ 2.0 percent by mass of cementitious material)

Mass of admixture  kg = 304 *0.02 = 6.08 kg

Volume  m3 = (6.08 * 1) /( 1.145 *I 000) = 0.005 m3

e) Volume of aggregates (coarse + fine) = [a- (b +c +d)] = 1- (0.097+0.137+0.005) = 0.761 m3

f) Mass of coarse aggregate kg = volume of aggregates calculated in step e x fraction of coarse aggregate calculated as in step 6  x Specific  gravity of coarse aggregate x I 000 = 0.761*0.55*2.67*1000 = 1118 kg

g) Mass of fine aggregate kg  =  volume of aggregates calculated in step e x fraction of fine  aggregate calculated as in step 6  x Specific gravity of fine aggregate x I 000 = 0.761*0.45*2.6*1000 = 890 kg

h) Adjustment of  for free moisture content on fine aggregate.

a) Reduce water content based on the free (surface) moisture content 2% for fine aggregates = 890*0.02 = 18 kg or  litre

Hence water content = 137-18 = 119 litre

b) Increase fine aggregate  based on the free (surface) moisture content 2% for fine aggregates.

Hence fine aggregate quantity =     890+18 =  908 kg

Trial 1  Quantities for Mix as calculated above

Cement  =   304 kg/m3

Water  =  119  kg/m3 or litre / m3

Fine aggregate =  908 kg/m3

Coarse aggregate = 1118 kg/m3

Chemical admixture =  6.08 kg/m3

Water-cement ratio = 0.45

Concrete should be free from segregation and bleeding.   Check the slump.

Trial 2. In case mismatch of slump, adjust the water content and dosage of admixture till the specified slump is achieved. Re estimate the mix proportions based on the revised water content. Check for durability requirements.

Trial 3 and Trial 4. Conduct with a variation of ±10 percent of water-cement ratio to Trial 2 W-C ratio.

Example 2  Design M25 concrete using fly ash and as per the data given below.

Step 1.  Collect all the required project specifications and test data as shown below

| Item |  |  | Data |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Concrete | Grade designation |  | M25 |  |  |  |  |  |
|  | Type of Concrete |  | Reinforced Cement Concrete |  |  |  |  |  |
| Cement | Type of Cement |  | Grade 53 conforming to IS 12269 |  |  |  |  |  |
|  | Minimum cement content |  | 300 |  |  |  |  |  |
|  | Maximum cement content |  | 450 kg/m3 |  |  |  |  |  |
|  | Specific gravity |  | 3.15 |  |  |  |  |  |
| Mineral admixture | Type |  | Fly ash Conforming to IS 3812 (Part I) |  |  |  |  |  |
|  | Specific gravity |  | 2.2 |  |  |  |  |  |
| Aggregate | Maximum nominal size |  | 20 |  |  |  |  |  |
|  | Type and Shape of aggregate |  | Crushed granite and Sub angular |  |  |  |  |  |
|  |  |  | Coarse aggregate |  |  |  |  | Fine aggregate |
|  | Specific gravity |  | 2.67 |  |  |  |  | 2.6 |
|  | Water absorption |  | 0.5% |  |  |  |  | nil |
|  | Free (surface) moisture |  | nil |  |  |  |  | 2% |
|  | Sieve analysis gradation |  | IS Sieve size mm | Analysis of Coarse Aggregate Fraction |  |  | Remarks | Conforming to Zone I IS 383 |
|  |  |  |  | I | II | Combined (55% of I + 45% of II) | Conforming to IS 383 |  |
|  |  |  | 20 | 100 | 100 | 100 |  |  |
|  |  |  | 10 | 10 | 50 | 28 |  |  |
|  |  |  | 4.75 |  | 10 | 4.5 |  |  |
|  |  |  | 2.36 |  |  |  |  |  |
| Maximum water-cement ratio |  |  | 0.50 |  |  |  |  |  |
| Workability |  |  | 75 mm |  |  |  |  |  |
| Exposure condition |  |  | moderate |  |  |  |  |  |
| Method of concrete placing |  |  | pumpable |  |  |  |  |  |
| Degree of supervision |  |  | Intermittent supervision |  |  |  |  |  |
| Chemical admixture type conforming to IS 9103 |  | Type | High range water reducing admixture - HRWR |  |  |  |  |  |
|  |  | Specific gravity | 1.145 |  |  |  |  |  |

Step 2   Calculate Target mean strength of Concrete

f’ck =f ck + 1.65 s

Target strength = 25 + 1.65 *5 = 33.25 N/mm2

s= 4 from Table1 of IS 10262-2009; Add 1N/mm2 as supervision is intermittent

Step 3 Decide Water-Cement ratio

From IS 456, for moderate exposure condition and Reinforced concrete, Maximum permissible water-cement ratio is 0.5.   Consider 0.45 as water-cement ratio. It is less than 0.50.

Step 4 Determination of Water content

From Table 2 of IS 10262-2009  maximum water content = 186 litre for angular coarse and saturated surface dry aggregate and for a slump of  25 to 50 mm without any admixtures.

a). slump is 75 mm. Hence increase water content by 3%. Water content = 186 *1.03 = 192 litres

b). Reduce water content by approximately 10 kg for sub-angular aggregates, water content = 192-10 = 182 litres

c). Lower water content by 25 percent for High range water reducing admixture. = 182*0.75 = 137 litres

d). Saturated surface dry (SSD) condition is assumed for aggregates.

Step 5 Calculation of Cementitious (cement + fly ash) material Content

Cementitious (cement + fly ash) material content in kg/m3 = 137/0.45 = 304 kg.  It is more than prescribed minimum cement content of 300 kg

Fly ash proportion and quantity

Based on previous experience and trials, higher cementitious content can be used.

Assume a 12% hike in cementitious material quantity

The revised cementitious content = 304*1.12 = 340  kg/m3

and modified water-cement ratio = 137/340 = 0.40

Consider percentage  of fly ash in cementitious content as 28%   based on project requirement and quality of materials.

Fly ash quantity  =  340 * 0.28 = 95 kg/m3

Cement (OPC) content =  340 – 95 = 245 kg/m3

Step 6  Fractions of  Coarse and Fine aggregate content by volume

From Table 3 of IS 10262-2009 volume of coarse aggregate is 0.60 corresponding to 20 mm size aggregate and zone I of fine aggregate   for a water-cement ratio of 0.50

a) Modify the proportion of volume of coarse aggregate at the rate of 0.01 decrease/increase ( -/+) for every  increase/decrease (±) of 0.05 change in W/C ratio.

For 0.40 W/C ratio   Volume of CA = 0.60+(0.01*0.1/0.05) =0.60+0.02=0.62

b)  Reduce the volume CA by 10 percent for pumpable concrete, Volume of CA = 0.62*0.9 = 0.56

Fraction of volume of fine aggregate content = I – 0.56=0.44

Step 7  Calculation of quantities of ingredients

The mix calculations per unit volume of concrete shall be as follows:

a) Volume of concrete = 1 m3

b) Volume of cement m3 = (245 * 1) /( 3.15  *I 000) = 0.078 m3

c) Volume of fly ash m3 = (95 * 1) /( 2.2*I 000) = 0.043 m3

d) Volume of water m3 = (137 * 1) /( 1  *I 000) = 0.137 m3

e) Volume of chemical admixture (superplasticizer) (@ 2.0 percent by mass of cementitious material)

Mass of admixture  kg = 340 *0.02 = 6.8 kg

Volume  m3 = (6.8 * 1) /( 1.145 *I 000) = 0.006 m3

f) Volume of aggregates (coarse + fine) = [a- (b +c +d+e)] = 1- (0.078+0.043+0.137+0.006) = 0.736 m3

g) Mass of coarse aggregate kg = volume of aggregates calculated in step e x fraction of coarse aggregate calculated as in step 6  x Specific  gravity of coarse aggregate x I 000 = 0.736*0.56*2.67*1000 = 1100 kg

h) Mass of fine aggregate kg  =  volume of aggregates calculated in step e x fraction of fine  aggregate calculated as in step 6  x Specific gravity of fine aggregate x I 000 = 0.736*0.44*2.6*1000 = 842 kg

i) Adjustment of  for free moisture content on fine aggregate.

a) Reduce water content based on the free (surface) moisture content 2% for fine aggregates = 842*0.02 = 17 kg or  litres

Hence water content = 137-17 = 120 litres

b) Increase fine aggregate  based on the free (surface) moisture content 2% for fine aggregates.

Hence fine aggregate quantity =     842+17 =  859 kg

Trial 1  Quantities for Mix as calculated above

Cement  =   245 kg/m3

Fly ash = 95 kg/m3

Water  =  120  kg/m3 or litres / m3

Fine aggregate =  859 kg/m3

Coarse aggregate = 1100 kg/m3

Chemical admixture =  6.8 kg/m3

Water-cement ratio = 0.40

Concrete should be free from segregation and bleeding.   Check the slump.

Trial 2. In case mismatch of slump, adjust the water content and dosage of admixture till the specified slump is achieved. Re estimate the mix proportions based on the revised water content. Check for durability requirements.

Trial 3 and Trial 4. Conduct with a variation of ±10 percent of water-cement ratio to Trial 2 W-C ratio.

Note – Final strength, Water-cement ratio and Slump properties of concrete need to be consistent with stipulations of IS 456 and project specifications.

REFERENCES

Gambhir, M L, 2011, Concrete Technology Theory and Practice, Tata McGraw Hill

IS 10262: 2009,  Concrete mix proportioning- Guidelines

IS 383 : 1970, Specification for coarse and fine aggregates from natural sources for concrete (second revision)

IS 456: 2000, Code of practice fur plain and reinforced concrete (fourth revision)

IS 2386 (Part 3): 1963, Methods of test for aggregates for concrete: Part 3 Specific gravity, density, voids, absorption and bulking

IS 3812 (Part I) : 2003, Specification for pulverized fuel ash: Part I . For use as pozzolana in cement, cement mortar and concrete (second revision)

IS 8112: 1989, Specification for 43 grade ordinary Portland cement (first revision)

IS 9103: 1999, Specification for admixtures for concrete (first revision)

Santhakumar A R, 2013, Concrete Technology, Oxford University Press

.