Adsorption of heavymetal Fe by birdbone particles from the Industry effluent

Dr.S.M. Jearmeen*

*Departmentof Advanced Zoology and Biotechnology,GuruNanakCollege, 
Chennai – 600 042, Tamil Nadu, India.

Abstract

Birdbone particles can remove heavymetal Fe from the titanium industry effluent. 
The adsorption of Fe by birdbone was mainly influenced by pH, birdbone absorbed the highest quantity of iron at pH 7, and when 5g of adsorbent was leaving only 278.27+0.93 ppm of Fe in the raw untreated effluent. The adsorption of metal Fe by birdbone particles was maximum at room temperature and 254.71+0.84 ppm of Fe was left in the effluent and increasing temperatures decreased the Fe adsorption.

Keywords: Biosorption, Fe uptake, birdbone particles, titanium industry effluent.

Introduction

Heavy metals released into the environment by industrial activities, circulating and eventually accumulating through the food chain, becoming a serious environmental threat ( Kuppusamy et al., 2004).

Bone charcoal is also used to adsorb radioisotopes of antimony from radioactive wastes and in the sugar refining industry to remove the color from sugar solutions (Gary et al., 2007; Ofomaja and Ho, 2007).

Bonechar as an adsorbent iseffective and can be easily adaptedto remove heavy metals from large amounts of industrial wastewater at a low cost. Poorly crystallized apatite, such as bone carapatite, might represent a low-cost and readily available phosphate source that could be used as an adsorbent. Bone char, a mixed absorbent containing around 10 percent carbon and 90 percent calcium phosphate, is mainly produced by the carbonization of bone (Choy and Mckay, 2005; Smiciklas et al., 2008).

The study’s main objective was to find out how efficient birdbone powder was in adsorbing heavy metal Fe in various parameters such as pH and temperature.

Materials and Methods

Preparation of bone char

Bird bones were collected from common fowls were boiled for 30 minutes and the meat attached to the bones was completely removed the bone was crushed into small fragments in a mechanical crusher. After it was dried at 60oC in a hot air oven for 24h, bone char was further powdered in an electric blender and sifted inan 80 mesh sieve 
(<180 m)

The experiment was designed to analyze the adsorptive potential of cheap bioresource, capable of adsorbing Fe in the aquatic and semi-aquatic media.The medium was separately maintained at six different pH levels (0.5, 2, 4, 7, 8, and 9). 
The adsorbent was thoroughly mixed with the toxicant solution and the mixture was agitated once in 2 h. 
The powdered adsorbents were mixed with the two different types of effluents (raw and partially treated effluent) in 5 different concentrations of 1, 2, 3, 4, and 5 mg/l. The initial concentrations of Fe were estimated in the two different effluents. The treatment was run for a period of more than 60 days. The Fe content of the effluents was estimated after 60 days of interaction with the adsorbents.The difference between the initial and final metal levels indicated the quantity adsorbed by the bioresource used.

The effect of temperature on the adsorptive potential of the materials used was estimated at 
pH 7. For assessing the effect of temperature, the reaction mixtures were allowed to interact in a 250ml Erhlen – Meyer flask. The flasks were placed inside separate incubators maintained at 42, 32, and 28oC. The experiments were continued for more than 60 days and the quantities of Fe wereanalyzed in the raw and partially treated effluent.

Estimation of heavy metal (Fe)

An Atomic Absorption Spectrophotometer (ELICO) model with Air-C2H2 flame type, with an average fuel flow rate between 0.8 –4.0 L min-1 and a support gas flow rate between 13.5.-17.5 L min-1 was used for sample analysis and operated as per the equipment manual. Calibration curves for various elements obtained from these standards were of a first-order reaction.The single-element hollow cathode lamps for respective metals were of the ELICO Co.Ltd-L series. The Fe analysis sample was aspirated with an Automatic sampler's help. The samples were finally injected into an AAS flame and the reading was directly measured.

Result and Discussion

Bird bone powder adsorbed the highest quantity of iron at pH 7 and when 5g of the absorbent was used leaving behind only 278.27+ 0.93ppm of Fe in the raw untreated effluent. At pH 
0.5, adsorption of Fe was minimum, and at 5g bird bone powder concentration, the Fe concentration of the raw untreated effluent was 291.15 + 0.84 ppm was left in the medium (Table 1).

Thechromium adsorbed at 5g of bird bone which was highestat 28oC was 245.30 + 0.92 and the lowest adsorptionadsorbed at 1g at 42oC was 275.94 + 0.98 of iron left behind in the raw untreated effluent (Table 2).

Higher dosages of the absorbent removed more quantities of Fe compared to low dosages, indicating the additive effect. Bird bone powder effectively adsorbed Fe from the titanium industry effluent. But the effectiveness of the adsorbent is more when administered in lower dosages.

Thus pH plays a vital role in determining the quantity of Fe adsorbed from the medium by bird bone powderat acidic pH levels, the quantity of Fe absorbed is much less compared to neutral and alkaline pH levels. The pH seemed to modify the adsorption potential of bird bone powder and the pH should be maintained at 7.0 to achieve maximum adsorption of Fe.

At higher temperatures (42oC) adsorption was much less compared to lower temperatures (28oC).

Namasivayam and Senthilkumar (1998) reported that the influence of temperature on the model parameters after a certain amount of adsorbents does notincrease.

Olaniyi et al. (2012) observedthat at 30oC, cow bone has the effect of temperature for the removal of metals using an immobilized sorbent.

Ibrahim et al. (2012) studied the effect of maximum metal ion concentration and used cow bone charcoal at 30oCon the adsorption capacity of chromium and lead.

Han et al. (2007) and Jain et al. (2009) pointed out that different chemical functional groups such as carboxyl, hydroxyl, and amide are responsible for the biosorption of metal ions. These groups are the potential sites for adsorption and the uptake of metal.

Chojnacka (2005) and Chenet al. (2006) pointed out that cow bone charcoalwasused as a microporous adsorbent, and metals penetratethese pores when the size of the ion becomes small.

The temperature was another significant factor determining the adsorption of heavy metals. At higher temperatures (42oC), even 1 g of adsorbent has a high percent of Fe from the titanium industry effluent at the ideal pH of 7.

Olaniyi et al. (2012) found that at 30oC, cow bone reported the effect of temperature for the removal of metals using an immobilized sorbent obtained from poultry waste.

Ibrahim et al. (2012) studied the effect of maximum metal ion concentration on the absorption capacity of chromium and lead at 30oC and here cow bone charcoal was used as an adsorbent.

. Below pH 5.1, hydrogen ions are likely to compete with iron, and at pH values above 8, iron might precipitate as hydroxides. Maximum adsorption using cow bone charcoal was observed atabout pH 5.1 and the adsorption is highly pH dependent.Moreno et al. (2010) found that iron removal increased quickly from 0.01 g to 0.02 g cow bone charcoal dosages.Rana et al. (2009) observed the removal efficiency of chitosan for iron was found nearly 58 percent.

Table 1

Fe adsorption from raw treated titanium industry effluent byBird bone powder 
at different temperature levels(at pH 7)

| S. No | Amount (in g)of bird bone powder | Fe in the effluent (ppm) control | Fe concentration (ppm) in effluent |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | pH |  |  |  |  |  |
|  |  |  | 0.5 | 2 | 4 | 7 | 8 | 9 |
| 1 | 1 | 452.25 ± 1.02 | 317.00 ± 0.85 | 312.39 ± 0.54 | 309.55 ± 0.51 | 297.69 ±0.60 (-34.00) | 298.49 ±0.60 | 302.00 ±0.72 |
| 2 | 2 |  | 314.62 ± 0.65 | 307.20 ± 0.84 | 303.37 ± 0.47 | 291.16 ±0.93 (-35.44) | 296.17 ±0.76 | 298.15 ±0.99 |
| 3 | 3 |  | 311.65 ± 0.85 | 302.23 ± 0.65 | 296.85 ± 0.76 | 285.88± 0.73 (-36.60) | 291.41 ±0.98 | 293.68 ±0.92 |
| 4 | 4 |  | 311.10 ± 0.78 | 308.49 ± 0.71 | 306.98 ± 0.65 | 284.23± 0.85 (-36.96) | 286.27 ±0.81 | 289.52 ±0.93 |
| 5 | 5 |  | 291.15 ± 0.84 | 290.31 ± 0.79 | 286.27 + 0.81 | 278.27±0.93 (-38.28) | 281.23 ±0.80 | 283.18 + 0.86 |

Note: Percent decrease in Fe concentration in parentheses

Deviations significant at P <0.05 (t-test)

Table2

Fe adsorption from raw untreated titanium industry effluent at pH 7 by bird bone powder at different temperature levels

| S.No | Amount (in g) of bird bone powder | Fe in effluent (ppm)control | Fe concentration (ppm) in effluent |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Temperature (° C) |  |  |
|  |  |  | 28 | 32 | 42 |
| 1 | 1 |  | 263.45 ± 0.96 (-41.54) | 274.26 + 0.73 | 275.94 + 0.98 |
| 2 | 2 |  | 258.91 +0.70 (-42.53) | 269.31 ± 0.87 | 271.55 ±0.85 |
| 3 | 3 | 452.25 ± 1.02 | 253.82 +0.65 (-43.65) | 265.17 + 0.80 | 267.53 ± 0.89 |
| 4 | 4 |  | 246.39 + 0.57 (-45.29) | 259.91 + 0.72 | 261.63 ±0.92 |
| 5 | 5 |  | 245.30 + 0.92 (-45.53) | 254.71 +0.84 | 257.77 ±0.75 |

Note: Percent decrease in Fe concentration in parentheses

Deviations significant at P <0.05 (t-test)

References

- Chen, S.B., Zhu, Y.C., Ma, Y.B. and Mekay, G. 2006. Effect of bone char application on Pb contaminated soil. Environ. Pollut.,39: 433 – 439

- Chojnacka, K. 2005. Biosorption of Cr(III) ions by egg shells. Journal of Hazardous Materials,121: 167-173.

- Gary, U.K., Kaur, M.P., Garg, V.K. and Sud, D. 2007. Removal of hexavalent chromium from aqueous solution by agricultural waste biomass. 
J Hazard Mater,40: 60-68.

- Han, X., Wong, Y.S., Wong, M.H. and Tama, N.G. 2007. Biosorption and bioreduction of Cr(vi) by a microalgal isolate. J Hazard Mater,146: 
65-72.

- Ibrahim, O., Sunday, M. and Odoh, R. 2012. Adsorption Study of Cr (VI) and Pb (1) from aqueous solution using animal charcoal derived from cow bone. Pelagia Research Library,3 (3): 648-657.

- Jain, M., Garg, V.K. and Kadirvelu, K. 2009. Chromium (VI) removal from aqueous system using H.annuus stem waste. J.Hazard Mater,162 : 
365-372.

- Kana, M.S., Halim, M.A., Safiullah, S. and Mollah, M.M. 2009. Removal of heavy metal from contaminated water by biopolymer crab shell chitosan. Journal of Applied Sciences,9 (5): 2762-2769.

- Kuppusamy, V., Jegan, J.R., Palanivelu, K. and Velan, M. 2004. Copper removal from aqueous solution by the marine green alga. Electronic J. Biotechnol., 7(11): 61-71.

- Moreno, J.C., Gomez, R. and Giraldo, L. 2010. Removal of Mn, Fe, Ni, and Cu ions from wastewater using cow bone charcoal. Materials,3: 452-466.

- Namasivayam, C. and Senthikumar, S. 1998. Removal of arsenic (v) from aqueous solution using industrial solid waste, adsorption rates, and equilibrium studies. Eng. Chem. Res.,37(12): 4816-4822.

- Ofomaja, A.E., Ho, Y.S. 2007. Effect of pH on cadmium biosorption by coconut meal. Hazard Mater,139: 356-362.

- Olaniyi, I., Moses, S. and Odoh, R. 2012. Adsorption study of Cr (VI) and Pb (11) from aqueous solution using animal charcoal derived from cow bone. Pelagia Research Library,3(3): 648-657.

- Rana, M.S., Halim, M.A., Safiullah, S. and Mollah, M.M. 2009. Removal of heavy metal from contaminated water by biopolymer crab shell chitosan. Journal of Applied Sciences,9 (5): 2762-2769.

- Shim, J.J Park, S.J. and Rju, S.K. 2001. Effect of modificatíon with HNO3 and NaOH by pitch-based activated carbon fibers. Carbon,39: 11

- Smiciklas, I., Dimovic, S., Sljivic, M. and Plecas, I. 2008. The batch study of adsorption by bone char. J. Eviron. Sci. Health,43: 210-217